## Slide 1: Localization of field emitter in a 9-cell cavity
Yongming Li1,2, Ari Palczewski1, Rongli Geng1
1 Jefferson Lab
2 Peking University

## Slide 2: Content
      1. Motivation
      2. Localization of field emitter in a 9-cell cavity
      3. Summary

## Slide 3: 1. Motivation
Field emission/dark current issue of concern for SRF cavity performance and SRF linac operation
  ILC, pulsed, pushing high gradient, driven by Epk
  CEBAF and other future CW SRF linacs, driven by DF
Complete understanding and reliable control of the issue is still needed in particular in multicell practical cavities
  Dark current in multicell cavity
    Where are the emitters
    Origin of emitters
    Impact to cryogenic load and machine operation

## Slide 4: Goal
Locate field emitter in multicell cavity
  Develop a generic producer
  Benchmark with vertically multicell cavity test
  Close loop by optical inspection of predict emitter site
  Provide feedback for cavity string assembly
Ultimate goal– to reduce & elemate filed emission in multicell cavity

## Slide 5: 2. Full Scale multicell cavities and FN Law
QM tunneling theory predicts exponential Fowler-Nordheim emission current density
ILC 9cell cavity
TTF shape
CEBAF Upgrade 7cell cavity
LLC shape

## Slide 6: Trajectories of different Emitters

## Slide 7: 9-cell Model and Definition of Coordinate
I5-L
I5-R
(Iris-5 left)
(Iris5- right)
R/m
Z/m
S
-S
iris1
iris2
iris3
iris4
iris5
iris6
iris7
iris8
iris9
iris10
Left flange
Right flange
Z
R
(0,0)
I5 region, 15MV/m
β=150, Φ=4.4eV

## Slide 8: 3 Types of “Long Range” Trajectories
Emission in region
>>> “Reverse type”
Emission in region >>> “Zigzag type”
Emission in region >>> “Forward type”
IR5
Impact position VS impact energy distribution

## Slide 9: Position and phase distribution
Reverse area: (S) 2.2mm~9.9mm
Zigzag area: (S)
9.9mm~12.2mm
Forward (S): 12.2mm ~decided by field
Position distribution
Phase distribution
I5-R

## Slide 10: Ratio of Electrons Escaping Cavity
R2 electron escaping rate is very high (0.5 at s=0.008m)
Most of electrons at hitting at cell 5 ( emitter: IR5_RT)
R1 escaping is low compare with R2 (less than 8%)
Resp=Nesp /Ntotal
Rhc=Nhc /Ntotal
Left Flange
Escape
Cell-5
Right Flange
Escape
Reverse
Zigzag
Forward
Cell-4
Cell-6

## Slide 11: Escaping Ratio
Escaping from Left Flange “Reverse type” trajectory
Escaping from Right Flange “Zigzag type” & “forward type” trajectory

## Slide 12: Energy Deposit in Cavity
Emitter bellow10mm [s] is very important considering the energy deposit in the cavity and escaping ratio of the electron.

## Slide 13: Impact Energy with Iris

## Slide 14
Experiment: 9-cell cavity RI23
② Detector
High Voltage
③ Amplifier
⑥ computer
① Dewar
⑤ DAQ
γ energy spectrum measurement system
② Detector
③ Amplifier
⑤ DAQ
⑥ computer
① Dewar
④ Attenuation
④ Attenuation

## Slide 15: Energy Spectrum from NaI(Tl) Crystal
Pi mode 10MV/m Ep=4.3MeV
Pi mode 11MV/m Ep=6.8MeV
Photon Energy/ MeV
counts
Photon Energy/ MeV
counts
Pi mode 12MV/m Ep=9.4MeV
Photon Energy/ MeV
counts
Photon Energy/ MeV
counts
Pi mode 13.1MV/m Ep=11.14MeV
End Point Energy Fitting

## Slide 16: Correlation between Simulation and Measurements
Calculated impact energy of field emission electrons and measured end point energy in γ spectrum π mode
detector saturated
Identification
Field emission onset
π mode 9MV/m
6/9 π mode 30MV/m
1/9 π mode 5.7MV/m
5/9 π mode 28MV/m
7/9 π 13.5MV/m
Radiation at bottom is much higher than that at top

## Slide 17: Correlation at another Pass-Band Mode
Calculated impact energy of field emission electrons and measured end point energy in γ spectrum 7/9π mode

## Slide 18: Final Answer: Emitter in Cell8/Iris9
Field emission region is: [S] -9.9mm~-12.2mm
@ I9-L-Zigzag region
Field emitter area
top
bottom

## Slide 19: Radiation angular location measurement system
top
bottom
Diode ring
Ring 1
Emitter
Ring 2
Ring 3
Ring 4
Ring 5
Ring 6

## Slide 20: X-ray Angular Distribution
Eacc=14.9 MV/m

## Slide 21: X-ray Angular Distribution
Eacc=17.5 MV/m

## Slide 22: X Ray Data Analysis
0.788
0.119
0.04
0.011
0.004
0.001
0.038
Ratio of e hitting on each cell
Geant 4 to simulate the radiation is still going on.

## Slide 23: Optical Inspection
In standard mode of Kyoto camera, no feature was observed within resolution limitation. This rules out “gross field emitter”. Next inspection using CYCLOPS.
Resolution: 7.4um/pixel
7mm

## Slide 24: Optical inspection for next step
Resolution: 2um

## Slide 25
First demonstration of field emitter localization achieved in a full-scale 9-cell cavity
  End-point gamma ray energy measure + simulation for longitudinal location
  Multiple diode rings for angular location
The method can be generalized for routine use in cavity vertical test or horizontal test
Work also extended to calculate CEBAF 12 GeV upgrade cavities
Summary