## Slide 1: Progress towards an ultra compact LumiCal
Yan Benhammou
Tel Aviv University
On behalf of the FCAL collaboration

## Slide 2: Outline
Introduction
Thin module design
  Mechanical support
  Fan out
Assembly of thin LumiCal module
Test beam
Summary and plans

## Slide 3
LumiCal and Sensor Design
4 sectors:
L2
L1
R1
R2
channels: 1 - 64
Outer active radius R = 195.2 mm
3 x 100 μm guard rings
Inner active radius R = 80.0 mm
Silicon sensor
thickness 320 μm
DC coupled with read-out electronics
p+ implants in n-type bulk
64 radial pads, pitch 1.8 mm
4 azimuthal sectors in one tile, each 7.5°
12 tiles makes full azimuthal coverage

## Slide 4
2014 developments
Tungsten
Tungsten
Tungsten
3.5 mm
3.5 mm
3.5 mm
3.5 mm
Silicon
Silicon
3.5 mm
Sensor glued on a 3.5mm PCB (HV)
Short PCB fan out
Electronic read out : 32 channels (4x8channels)
Test beam @ CERN with electron beam
4 sensor layers in between tungsten planes
(cf Previous talk)

## Slide 5: 2015 goals
Primary aim was to build LumiCal prototype for beam tests and demonstrate the principle of compact electromagnetic calorimeter;
Make the geometry of the detector module closer to the designed for LumiCal at LC experiments;
Reduce the thickness of the sensor layer below 1 mm;
Provide mechanical rigidity for the module to simplify its handling during the assembly of calorimeter prototype;
Try to read-out all pads (256) of the LumiCal sensor.

## Slide 6: Thin LumiCal module design
Current LumiCal modules are based on 3.5 mm thick PCB : compactness is an essential requirement to provide small Molière radius/accurate shower position reconstruction.
In current LumiCal conceptual design the space between absorbers is 1 mm!
Easy to mount on tungsten planes
320 μm
150 μm
650 μm
envelope
Sensor
Kapton HV
50 μm
Kapton fan out (connectors)
100 μm
Kapton HV
Kapton Fan out
Sensor
Envelope

## Slide 7: Mechanical support : the envelope
In collaboration with the CERN mechanics group, we considered two options to produce the envelop :
    3D printing
    carbon fiber
The 3D printing was not rigid and flat enough so we opted for the carbon fiber solution

## Slide 8
HV and Fan-out kapton
The thickness of the HV kapton is 90 μm.
Thickness of fan-out varies in different areas from
129 μm to 158 μm
129
136
139
141
138
158
Thickness, μm
144
90
connectors

## Slide 9
Fake thin LumiCal Prototypes
Procedure was destructive for wire bonding connections.
Total assembly thickness:
less then 900 μm for carbon fiber
less then 800 μm for 3d printing
Gluing of the fake sensor inside the envelope

## Slide 10
Module assembly and Tests
HV kapton is glued to the n-side of the sensor using conductive glue;
Fanout with Panasonic connector soldered was glued to the p-side of the sensor;
Traditional ultrasonic wire bonding was used to connect sensor pads to fanout traces;

## Slide 11
Module 17, current measurements
...
...
61
63
62
64
Sector R2
Grounding the adjacent pin in Panasonic connector reduces the measured dark current from the pad.
There is some essential conductivity between Panasonic connector pins.
Further tests confirmed that the problem was created by soldering flux.

## Slide 12: low-height contact between sensor and readout electronics
Approaches :
  wirebonding
  conventional, currently used, minimum height ~100μm
  Flat loop wire bonding
  staggered pcb required
  Conductive glue
  tested at DESY, Krakow,TAU : not satisfying …
  Laser bonding
  tested by TAU : not possible because aluminum pads
  tape automated bonding (TAB)
  first enquiries by TAU
  bonding wedge & dedicated fanout sample received
  Spring loaded contact
    technology tests by ZEUTHEN

## Slide 13
Wire bonding : loop size

## Slide 14
Sensor gluing to the Envelope
support
Envelope
Module
adhesive
Wire bonding loops does not allow to apply uniformly distributed pressure on top of the module using simple weight;
Applying the pressure with simple weight increase the risk of sensor damage;
Possible solutions:
  Support which eliminates contact with sensitive areas of the module (wire loops, soldering balls);
  Support which creates vacuum below.
This method was successfully realized to glue the envelope

## Slide 15
Module 18 tests @ CERN

## Slide 16: Readout
The aim was to read the whole sensor (256 pads)
Different candidates were tested : APV, VMM1 and VMM2
APV is a good candidate :
  Pre amplifier shaper, 192-cell analog pipeline and an analog pulse shape processor per channel, 128 channels
  Easy to find
  Intensively used by different collaborations
  Problem : gain is not adjustable and not a important dynamic range; good for MIP, saturated for electromagnetic shower

## Slide 17: DESY test beam (12-19/10)
4 planes with thin sensor scotched on tungsten
FEB : APV chip based
DAQ : SRS system, designed by RD51 collaboration.
Silicon telescope : 6 planes with MIMOSA chip
Synchronization using TLU and fake SRS busy signal (generated by dual timer)
Online and “light” offline

## Slide 19
APV 0 (master)
APV 1 (slave)
1
2
3
62
63
64
61
65
66
67
68
128
127
126
129
130
131
256
255
254
196
195
194
193
189
190
191
192
132
133
134
135
136
DAQ NUMBERING

## Slide 20: Pedestals
1
2
3
62
63
64
61
65
66
67
68
128
127
126
129
130
131
256
255
254
196
195
194
193
189
190
191
192
132
133
134
135
136

## Slide 21
XY Scan occupancy, run 110
Plane 1,
Module 18
Plane 2,
Module 20
Plane 3,
Module 17
Plane 4,
Module 21

## Slide 22: XY scan

## Slide 23
1st plane
2nd plane
3rd plane
4th plane
Channel 247 (700)
Channel 247(1100),248(400)
Channel 247(1500),248(1000)
Channel 9 (250)
Alignment ? Channel 10 ?
Shower development

## Slide 24
Summary and plans
Thin LumiCal detector modules (~800 mm) have been developed, produced and tested in test beam
Assembly procedure was constantly optimized during the production of 3.5 modules to improve its reliability.
Further developments are ongoing to decrease the thickness of the silicon layer
Test beam analysis just started (charge and shower study, cross talk, …)

## Slide 25: Thank you !

## Slide 26
Wedge Bonding
Relative motion of wire and substrate in combination with friction on their interface facilitates the relative sliding of the wire on the pad causing bond area cleaning from the native oxide layers at the interface and bond formation.
To provide relative motion between the wire and bonding pad the last one in our case must be fixed well by the glue.

## Slide 27
TAB Technology
Stable contact between sensor and readout electronics which meets LumiCal geometrical (compactness) requirement
sensor / chip
Al / Cu
kapton
Bond
Single point Tape Automated Bonding (TAB):
No wire loop;
The bond can be covered by the glue for better protection;
It is difficult to repair bonding defects;
Fanout was shipped by manufacture.

## Slide 28
TAB Fanout Geometry
Photo overlapped by two versions of drawings:
The last version:
Yellow - traces,
Grey – window in kapton,
Blue - fanout edge position.

## Slide 29
Combined occupancy
Plane 1,
Module 18
Plane 2,
Module 20
Plane 3,
Module 17
Plane 4,
Module 21

## Slide 30
RUN 221

## Slide 31
 | 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10 | 11 | 12 | 13 | 14 | 15
env 1 | 720 | 142 | 708 |  | 698 | 123 | 676 | 129 | 700 |  | 712 | 134 | 101 | 660 | 687
env 2 | 720 | 118 | 701 |  | 729 | 129 | 689 | 133 | 699 |  | 691 | 107 | 100 | 700 | 692
env 3 | 700 | 125 | 703 |  | 742 | 130 | 697 | 127 | 705 |  | 703 | 126 | 110 | 713 | 704
env 4 | 717 | 136 | 677 |  | 679 | 132 | 727 | 131 | 706 |  | 693 | 134 | 104 | 693 | 692
env 5 | 716 | 155 | 753 |  | 758 | 126 | 705 | 160 | 717 |  | 739 | 123 | 100 | 699 | 708
1
2
3
4
5
6
14
8
7
15
9
10
11
12
13

## Slide 32: Luminosity at e+e- collider
Bhabha scattering at low polar angles is used
e+e- e+e- (g)
L = N / s
Count Bhabha events
From theory

## Slide 33: Luminosity at e+e- collider
Precise measurement of the luminosity
Low angle physics
Lumical composed of silicon and tungsten planes.