## Slide 1
High-Gradient X-Band Structure Prototypes for CLIC: Lessons from a Decade of High-Power Tests
P. Alonso Arias, on behalf of the Xboxes team (RF-MKS)
International Workshop on Future Linear Colliders
Valencia, 2025

## Slide 2
INTRODUCTION ON CLIC
- A study for a next generation Higgs factory
- Accelerating structures requirements
- Structures up to date
HIGH POWER TESTS OF CLIC STRUCTURES
-Xband test benches
-XBoxes at CERN
15 YEARS OF TESTING: TESTS RESULTS
- Gradient & BDR: an empirical law
- Gradient & BDR: scaled gradient
- Gradient & BDR: final performance of CLIC prototypes
- Conditioning : dark current and field emission
15 YEARS OF TESTING: LESSONS LEARNED
- Operational aspects: conditioning programmes
-Operational aspects: BD clustering
_Feedback to manufacturing: vacuum bake-out
-Feedback to manufacturing: Joining
CONCLUSIONS
1
OUTLOOK
LCWS 2025

## Slide 3
A STUDY FOR A NEXT GENERATION HIGGS FACTORY
The Compact Linear Collider is a study for an e+ e- collider at energies from 380 GeV to 1.5 TeV
Main linac designed for compactness: high-gradient solution to reduce number of structures (spoiler: still large but imagine with 5 MV/m LHC cavities!)
Normal conducting X-band (12 GHz) accelerating structures operating at gradients up to 100 MV/m
CLIC
1
LCWS 2025

## Slide 4
A STUDY FOR A NEXT GENERATION HIGGS FACTORY
1
LCWS 2025
Risky and expensive part of CLIC project
CLIC
The Compact Linear Collider is a study for an e+ e- collider at energies from 380 GeV to 1.5 TeV
Main linac designed for compactness: high-gradient solution to reduce number of structures (spoiler: still large but imagine with 5 MV/m LHC cavities!)
Normal conducting X-band (12 GHz) accelerating structures operating at gradients up to 100 MV/m

## Slide 5
High gradient operation up to 72 MV/m
Active length of acceleration is 5.3 km
Breakdown rate must be limited to
0.01 events/pulse x 5.3×103 m= 1.8×10−6 events/pulse
High gradient operation up to 100 MV/m
Active length of acceleration is 30 km
Breakdown rate must be limited to
0.01 events/pulse x 3×104 m= 3×10−7 events/pulse”
“the conservative estimate is used in the current CLIC design which assumes that kicks due to breakdown will result in a full loss of luminosity of the pulse in which the breakdown occurs. CLIC parameters budget a 1% luminosity loss due to this effect. “
CLIC380
CLIC 1.5TeV
12 GHz operation frequency
Manufacturing at micron-level tolerances to avoid degradation by beam-to-structure misalignment effects
CLIC
ACCELERATING STRUCTURES REQUIREMENTS
2
LCWS 2025

## Slide 6
CLIC
17 YEARS OF STRUCTURE PROTOTYPES
3
LCWS 2025

## Slide 7
X-BAND TEST BENCHES
1st test benches to test 12 GHz structures in KEK and SLAC. From 2012, Xboxes at CERN (Xbox1, Xbox2 and Xbox3)
Capabilities for simultaneous testing of up to 7 prototypes
XBOX2
XBOX3
  50 MW, 1.5 us
  150 MW, 250 ns
  50 Hz
  2x 6-10 MW, 5 us
  40-60 MW, 200 ns
  Up to 400 Hz (200 Hz/line)
4
LCWS 2025
HIGH-POWER TESTS

## Slide 8
High-power pulsed RF generation + monitoring of relevant signals along the RF distribution line
Dark current signals
Upstream
Downstream
RF signals
Incident
Reflected
Vacuum signals
Flow
Temperature
Conditioning algorithm based on vacuum/ BDR +
Breakdown and field emission studies
5
LCWS 2025
XBOXES AT CERN
HIGH-POWER TESTS

## Slide 9
AN EMPIRICAL LAW TO COMPARE PERFORMANCE
Different test conditions limit our capability to compare prototype performance (pulse width, available power…)
Measuring BDRs of 10−7 bpp would take months!
An empirical law (2006) has been observed among the different structures:
BDR
6
LCWS 2025
TEST RESULTS

## Slide 10
Prototypes tested at different test stands are compared on the same basis by using the scaling law
Scaled accelerating gradient is calculated in relation to the CLIC380 reference values of BDR and pulse length (1.8×10−6 bpp, 180 ns)
SCALED GRADIENT
TEST RESULTS
7
LCWS 2025

## Slide 11
Around 30 prototypes tested. Most reached >80 MV/m at CLIC380 BDR specification
Some prototypes surpass 110 MV/m and 120 MV/m, confirming potential of X-band
Variability among prototypes with same design highlights the impact of manufacturing
P. Alonso-Arias et al. High Gradient RF Testing of X-band structures. A comprehensive review (in prep.)
CLIC380
CLIC 3TeV
FINAL PERFORMANCE
TEST RESULTS
8
LCWS 2025

## Slide 12
DC is high during the initial pulses, with occasional stochastic jumps after BDs
Decrease of DC after conditioning
Observations during conditioning
CONDITIONING, DARK CURRENT & FIELD EMISSION
TEST RESULTS
9
LCWS 2025

## Slide 13
Short power scans used to see progress and emission reduction during conditioning
Observations across tested prototypes: a progressive reduction in the field enhancement factor β
Field emitted electrons produce dark current (DC) following the Fowler-Nordheim law:
Conditioning progress
CONDITIONING, DARK CURRENT & FIELD EMISSION
TEST RESULTS
10
LCWS 2025

## Slide 14
Thousands of structures to condition -> time consuming
Observations. Air vented structures have been found to condition faster if they had previously been conditioned at the required gradient
11
LCWS 2025
OPERATIONAL ASPECTS: CONDITIONING PROGRAMMES
LESSONS LEARNED

## Slide 15
Temporal clustering
Two superimposed exponentials -> two BD processes
Primary BDs set the limit for the structure for achievable gradient
Secondary BDs set a limit for recovery time during operation
Spatial clustering
Clusters of BDs appear in small regions during short periods of time
Residual surface damage, material degradation…
Alter conditioning dynamics
OPERATIONAL ASPECTS: BD CLUSTERING
LESSONS LEARNED
12
LCWS 2025

## Slide 16
Progress and performance is comparable!
Similar levels of dark current measured
TD24N5 (TD24UBO) assembled and installed without the bake-out, and TD24N4 (TD24BO) for control
For CLIC prototypes, the nominal vacuum baking procedure (introduced by NLC/GLC) involves heating the assembled structure at 650 °C for 1–3 days.
FEEDBACK TO MANUFACTURING: BAKE-OUT
LESSONS LEARNED
13
LCWS 2025

## Slide 17
FEEDBACK TO MANUFACTURING: JOINING
LESSONS LEARNED
14
LCWS 2025

## Slide 18
35 X-band structure prototypes + 15 years of high-power testing and studies of breakdown mechanisms and conditioning processes let us:
Optimise RF design parameters
Verify an empirical law expressing the
correlation between Eacc, pulse length, and BDR allowing:
Comparison of prototypes with common reference frame
Analysis of high-gradient performance limits
Get insight into conditioning and the
implications for linac operation
Refine fabrication strategies
CONCLUSIONS
15
LCWS 2025

## Slide 19
Special thanks to all the people who have contributed with their work and advice during this year, including N. Catalán-Lasheras, A. Baig, M. Boronat, A. Chauchet, S. Curt, A. Grudiev, S. González-Antón, C. Marrelli, P. Martínez-Reviriego, L. Millar, P. Morales Sánchez, D. Soriano, I. Syratchev, M. Volpi, P. Wang, B. Woolley, W. Wuensch…
International Workshop on Future Linear Colliders 2025
High-Gradient X-Band Structure Prototypes for CLIC: Lessons from a Decade of High-Power Tests

## Slide 20
BREAKDOWN LOCALISATION
BD time =
There are other methods to localise BD (e.g. using phase) not being used at the moment
XBOXES
LCWS 2025

## Slide 21
More info here: P. Morales, Normal Conducting High Gradient prototype manufacturing
Disk in production, will be assembled this year 2025
The new design integrates the RF area, HOM loads, the cooling circuits, and part of the vacuum system in one part
Redesigned to evolve from pure bonding to bonding+brazing and reducing steps
LCWS 2025
CLIC
CLICK: SMARTCELL PROTOTYPE

## Slide 22
LCWS 2025
CLIC
CLICK: SMARTCELL PROTOTYPE
Redesigned to evolve from pure bonding to bonding+brazing and reducing steps
More info here: P. Morales, Normal Conducting High Gradient prototype manufacturing

## Slide 23
LCWS 2025
OPERATIONAL ASPECTS: RECOVER AFTER BD
LESSONS LEARNED