## Slide 1: High-Q/high-G Developments at FNAL
Daniel Bafia
Associate Scientist
October 21st, 2025
FERMILAB-SLIDES-25-0281-SQMS-TD

## Slide 2: State-of-the-Art Nb SRF Cavity Performance for Accelerators
Larger Q0/higher gradient  lower $$
RF field
State-of-the-Art FNAL Cavities Post Various Treatments
50 MV/m
6e10

## Slide 3: Materials Science to Identify Origins of Limitations
Cavity RF Measurements
(Cryo) Material Studies
XPS
ToF-SIMS
SEM

## Slide 4: Exploring the Role of Impurities in Nb: Nitrogen
Why does dilute N enhance Q0?
SRF Cavity Studies
D. Bafia et al. PRAppl 23, 054052 (2025)
T. Kubo PRAppl 17, 014018 (2022)
New Theoretical Models
F. Herman and R. Hlubina PRB 104, 094519 (2021)
Studies highlight the importance of N in optimal inelastic scattering
Dilute impurities yield homogenized gap  higher Q0
N-Doped
EP
Nb Cavity Conductivity

## Slide 5: Exploring the Role of Impurities in Nb: Oxygen
Why does baking enable performance tuning?
Cavity Performance Post Various in situ Baking
Mid-T Bake
75/120 C
120 C
TE1RI003 Post Sequential 120C Baking
Calculated O Depth Profile
T = 2K
f0 = 1.3 GHz
Diffusion Depth
D. Bafia et al. Proc. of SRF’21
Tracking Quench Field of 1.3 GHz Cavities with O Diffusion Depth
A. Romanenko et al. Proc. of SRF’19
ToF SIMS Studies on Cutouts
Baking drives the inward diffusion of O  reduces H!
D. Bafia et al. Proc. of SRF’21
Able to tune performance by diffusing O via baking
  Tune between high Q0 and high G
Do O and N perform the same function in Nb?

## Slide 6: Comparing Effectiveness of O vs N Impurities
Parametrically compared RBCS @ 16 MV/m and measured N and O concentrations in sample post various surface treatments
Surface Resistance vs Average Concentration of Impurities
H. Hu et al. arXiv:2509.18564
RF and Materials Science Studies Post Various O or N Based Treatments
N is 10x more effective than O at reducing BCS!
Oxygen
Nitrogen

## Slide 7: Model for Improved Performance: H Capture
N interstitial yields a simultaneous reduction in MFP and increase in SCing gap
Binding energy of N to H > O to H1
Surface Resistance vs Mean Free Path: Comparison with BCS Theory
[1] D.C. Ford et al., Supercond. Sci. Technol. 26, 095002 (2013).
N might better prevent the formation of hydrides in Nb!
Nitrogen is a promising impurity for higher Q0/G!
H. Hu et al. arXiv:2509.18564

## Slide 8: Optimized EP: Unlocking the Full Potential of Impurity Tailoring
Optimized EP + 120C baking on HB 650 MHz
Cathode-N
+50 MV/m!
+50 MV/m!
V. Chouhan et al., NIMPRA 1051, 168234 (2023)
Cold EP + 75/120C Baking on 1.3 GHz Cavity
Require optimized EP parameters/design to reduce H uptake and surface roughness
Optimized EP enables benefit of impurity tailoring
75/120 C

## Slide 9: High Q₀ and G via O-Tailoring and Optimized EP
Mid-T baking: Diffuses O and gives high Q0;
EP Nano-removal treatment: Removes 100 nm from surface
1.3 GHz Nb SRF Cavity Post Various Surface Treatments
V. Chouhan et al., THP83, SRF2025
V. Chouhan et al., WEP065, NAPAC2025
Issue: Forms lossy Nb-carbides
 Removes NbC!

## Slide 10: High Q₀ and G via O-Tailoring and Optimized EP
1.3 GHz Nb SRF Cavity Post Various Surface Treatments
650 MHz Nb SRF Cavity Post Various Surface Treatments
Removing NbC results in dramatic increase in Q0 and G!
Demonstrated also on 650 MHz!
V. Chouhan et al., THP83, SRF2025
V. Chouhan et al., WEP065, NAPAC2025
Mid-T baking: Diffuses O and gives high Q0;
EP Nano-removal treatment: Removes 100 nm from surface
Issue: Forms lossy Nb-carbides
 Removes NbC!

## Slide 11: Beyond Bulk: Improving Nb Film Performance – A Fix for MFQS
Nb film on copper cavities exhibit “medium-field Q-slope”  why?
B. Abdisatarov et al SUST 38, 075006 (2025)
DC HiPIMS Deposition System @ CERN
Performance of Nb Film on Nb Cavity Post Subsequent Annealing
Materials Studies on Nb Film on Nb Samples Post Baking
ToF-SIMS studies reveal reduction in H upon annealing
 Less NbH
EBSD reveals reduction in LMAD upon annealing
 Heals defects
Subsequent annealing reduces MFQS!

## Slide 12: Conclusions
Coupled RF and materials science studies advance microscopic understanding of SRF materials, revealing how impurities and defects govern performance.
Impurity (N or O) tailoring tunes SRF properties
  N is ~10× more effective than O at lowering RBCS​.
Optimized EP is critical to realize impurity-tailoring benefits
  Minimizes H uptake, smooths surface and removes lossy inclusions.
H and lattice defects identified as key loss sources in Nb films
  Annealing mitigates these losses and improves film performance.

## Slide 13: Thank you!

## Slide 14: Backup Slides

## Slide 15: Surface Resistance
1.3 GHz Single-cell Cavity
650 MHz Single-cell Cavity
Surface contaminants, such as niobium carbides, are likely contributors to the relatively higher residual resistance (Rres) after mid-T baking.
Ultralight material removal reduced Rres and BCS resistance (RBCS) of both mid-T baked cavities.
V. Chouhan et al., WEP065, NAPAC2025
V. Chouhan et al., THP83, SRF2025