## Slide 1: CERN-KEK collaboration on hydroformed Nb-on-Cu cavities
Akira Yamamoto, Carlota Pereira Carlos, Caroline Hain, Franck Peauger, Gilles Favre, Guillaume Jonathan Rosaz, Hayato Araki, Joanna Sylwia Swieszek, Kristóf Brunner, Laura Helene Hannemann, Marco Garlaschè, Masashi Yamanaka, Said Atieh, Valentin Giglia, Walter Venturini Delsolaro

## Slide 2: Outline
  Motivation for developing better Nb-on-Cu cavities
  Seamless substrate development
  Hydroforming process and Nb coating
  RF measurement results
  Possible improvement directions
  Summary

## Slide 3: Nb-on-Cu cavities
Advantages:
  By adjusting the coating process very high Q0 is achievable
  Allows operation up to 4.5 K, significantly increasing the cryogenic efficiency
  Less sensitive to trapped magnetic flux
  Cost of the cavity is significantly reduced
Disadvantages:
  The Q slope limits the usefulness at higher than medium gradient
  It is outperformed by N-doped / mid-T baked bulk Nb

## Slide 4: Motivation for developing better Nb-on-Cu cavities
FCC baseline:
  2-cell, 400 MHz, Nb-on-Cu
    264 cavities, operated at 4.5 K
  6-cell, 800 MHz, bulk Nb
    408 cavities, operated at 2 K
  Performance requirement:
    Q = 3.3 x 109 (~3.7 x 108 at 1.3 GHz)
    Eacc = 13 MV/m
  FCC feasibility report
Improvements required
  Substrate improvement
  Nb film improvement
  Production industrialization
FCC requirement
LHC
Studied on 1.3 GHz cavities

## Slide 5: Seamless substrate development
The weld at the equator can create porosity reducing the reliability of the Nb film
4 possibilities studied:
  Bulk machined
  Electroforming
  Internally welded
  Hydroformed
Bulk machined cavity
Hydroformed cavity
Produced and tested at CERN
In collaboration with KEK

## Slide 6: Seamless substrate development
Bulk machined substrate
  Higher material cost
  Perfect cavity geometry and inner surface quality
  Homogeneous wall thickness
Hydroformed substrate
  Industrial process, easily scalable
  Upfront investment into the dies
    Per cavity cost drops sharply at high cavity count
  Seamless cut-off tube is possible
  Uneven thickness profile
  Inner surface is much rougher
Bulk machined substrate
Hydroformed substrate

## Slide 7: Hydroforming process
  Forming was performed at NEURON, Japan
  Two-step forming process
  Annealing at 500 C for 2h between the steps
  A single forming step is ~1 minute
Article on the process

## Slide 8: Hydroforming results
  Original tube thickness = 5 mm
    Final equator thickness = 2.6 mm
  The final profile is significantly different from the design geometry, but it can be corrected for the next batch
Article on the process

## Slide 9: Hydroforming results
  The inner surface roughness increased significantly in the cell
    Ratube = 1.0 µm
    Racut-off = 1.0 µm
    Racell = 2.9 µm
  Roughness is not removed by electropolishing
Article on the process
“Orange peel” surface after electrolytic polishing

## Slide 10: Nb coating process
  Preparation and coating at CERN
    Identical process to bulk machined cavities
  Surface prepared using electrolytic polishing (removing ~12 µm)
    Then rinsed and dried before coating
  Coated using High Power Impulse Magnetron Sputtering (HiPIMS)
  Targeting 6 µm Nb layer thickness
Baseline recipe:
  bakeout at 200 C, 24h.
  unbiased HiPIMS in cut-offs (6 positions / cut-off)
  -75 V biased HiPIMS in the cell
  150 C, 2.3.10-3 mbar Kr
  Dry air venting at room temperature
Cathode
Magnet

## Slide 11: RF measurements
Two identical cavities (C1 and C1b) were measured at both KEK and CERN
  Allowing cross validation of our results, and sharing measurement experience
 | KEK | CERN
Measured at | 2024-03 | 2024-11, 2025-02
Mobile coupler | ✔️ | ✔️
Coupler location | Bottom | Top
T-mapping | ✔️ | ✖️
High precision T-sensor | 8 | 2
The cavity is surrounded by | Solenoid coil | Copper shield
KEK setup
CERN setup

## Slide 12: RF measurements 4.2 K
  The performance was slightly below FCC requirement at 4.2 K
  Around 35% worse than bulk machined cavities
BM2.11
4.2 K
(One of the best) Bulk machined

## Slide 13: RF measurements 1.85 K
  Multiple Q-switches were observed
  Above 6 MV/m steep Q-slope on all cavities
    Observed already on 6 different hydroformed cavities
    Originally thought to be caused by the inner surface quality
    But our latest result makes us rethink this evaluation
Q-switch

## Slide 14: Comparison with bulk machined Nb-Cu results
BM2.11
4.2 K
Radiation detected
Hydroformed
(One of the best) Bulk machined

## Slide 15: Comparison with bulk machined Nb-Cu results
BM2.11
Radiation detected
1.85 K
Hydroformed
(One of the best) Bulk machined

## Slide 16: Thermal gradient during cooldown
  Sensitivity to thermal gradient during cooldown
    Studied at both institute, with identical findings
  The residual resistance (and quality factor) at 1.85 K is very sensitive to ∆T
    Low ∆T can be achieved with slow cooldown and heater control (at least in bare cavity tests…)
  Also relevant for Nb3Sn-on-Nb
    see Felix Kramer’s talk on SRF 2025 (link)

## Slide 17: Thermal gradient during cooldown
  Sensitivity to thermal gradient during cooldown
    Studied at both institute, with identical findings
  The residual resistance (and quality factor) at 1.85 K is very sensitive to ∆T
    Low ∆T can be achieved with slow cooldown and heater control (at least in bare cavity tests…)
  Also relevant for Nb3Sn-on-Nb
    see Felix Kramer’s talk on SRF 2025 (link)

## Slide 18: Surface quality improvement
  Improving the surface quality of the substrate is of highest importance
    Internal machining after hydroforming
    Plasma electrolytic polishing (INFN, website)
      First cavity was prepared and tested
      It showed slightly better Q-slope compared to the other hydroformed cavities
    Mechanical polishing (KEK)
      Cu tube mechanically polished then electropolished BEFORE hydroforming
      The hydroforming process still introduces “orange peel”
PEP cavity

## Slide 19: PRELIMINARY RESULTS
Two cavities (C3, C3b) hydroformed after mechanical polishing of the Cu tube
    They both show low field Q0 of 5x1010
    One of them suffered several Q switches
    The other showed the best Q-slope recorded on ANY of our Nb-on-Cu 1.3 GHz cavities at 1.85 K

## Slide 20: PRELIMINARY RESULTS
Two cavities (C3, C3b) hydroformed after mechanical polishing of the Cu tube
    They both show low field Q0 of 5x1010
    One of them suffered several Q switches
    The other showed the best Q-slope recorded on ANY of our Nb-on-Cu 1.3 GHz cavities at 1.85 K
    At 4.2 K C3b is the best of the hydroformed cavities, but it is still ~20% worse than bulk machined cavities

## Slide 21: Summary
  We had a very successful 3-year collaboration between KEK and CERN
    Resulting in the forming, coating and measurement of the first “full seamless” hydroformed 1.3 GHz Nb-on-Cu cavities
    The substrate and coating showed reproducible results
      Across 7 cavities
      Two different measurement stands
    By improving the surface quality, we are certain to increase the performance at 4.2 K
    The latest result shows mostly mitigated Q-slope at 1.85 K
      New record performance of Nb-on-Cu
      (Now it needs to be reproduced…)
  Thanks to the successful demonstration of the technology on 1.3 GHz cavities, hydroforming is regarded as a potential method for producing 400 MHz FCC cavities

## Slide 22
Thank you for your attention!