## Slide 1: Crystals (and Other) Measurements
Adam Para
February 6, 2009

## Slide 2: Crystals for Dual Readout
Need to measure (separately) the scintillation and Cherenkov light
Step 1: get Cherenkov light out of the crystal good transmission for short wavelength
Step 2: separate scintillation and Cherenkov: time and emission spectrum
Important crystal properties:
  transmission as a function of wavelength
  Emission spectrum
  Scintillation decay time
Crystals: modified PbWO4 (PbW04/PbMoO4) and PbF2

## Slide 3: Lead Tungstate/Molybdenate Transmission
Chart: Transmission, PbW(Mo)O4

## Slide 4: Lead Tungstate/Molybdenate Emission Spectrum
Chart: PbWO4 emission spectrum, UV stimulated

## Slide 5: Lead Tungstate/Molybdenate
UV cutoff around 370 nm
Scintillation starts around 400 nm
Decay time still needs to be measured
Rather limited window for the Cherenkov light measurement
Light yield (including collection efficiency and photodetectors) need to be measured
Separation efficiency and purity needs to be measured

## Slide 6: Lead Fluoride
Chart: Transmission, PbF2

## Slide 7: Lead Fluride
Very good transmission at short wavelength, low UV cutoff  very good Cherenkov yield
Cherenkov only. Need to dope with a scintillating agent :
  Challenge
  Opportunity to tune the scintillation light yield/timing

## Slide 8: Measuring Temperature Dependence of MPPC’s
We study the variation of the response and/or characteristics of the MPPC with temperature
Our measuring setup includes the amplifier, which is places inside the temperature stabilized box, alongside with the detector
We measure a convolution of the temperature dependence of the detector and the amplifier
Need to calibrate the amplifier by itself

## Slide 9: Amplifier Testing Setup
Pulser: triangular pulse, ~ 5ns base
Split into two signals:
  Fed into the scope
  Attenuated, fed into thcycled frome amplifier, and fed into the scope. Amplifier inside the temperature chamber, everything else at room temperature. Attenuator adjusted to ensure that the amplified signal size matches that of the original pulse
Scope programmed to measure the amplitude and the charge (area) of both signals simultaneously.
Chamber cycled from -60C to 50 C

## Slide 10: Charge Amplification
Chart: Q(ampl)/Q(pulser)
| -60 | -40 | -40 | -20 | -20 | 0 | 0 | 20 | 40 | 50
Q/Qtest | 1.0502 | 1.0431 | 1.043 | 1.0426 | 1.043 | 1.0516 | 1.052 | 1.0681 | 1.089 | 1.1015

## Slide 11: Amplitude Amplification
Chart: A(ampl)/A(pulser)
| -60 | -40 | -40 | -20 | -20 | 0 | 0 | 20 | 40 | 50
Q/Qtest | 1.069 | 1.0557 | 1.0387 | 1.0539 | 1.0415 | 1.0568 | 1.0342 | 1.0676 | 1.0444 | 1.0713 | 1.0925 | 1.083

## Slide 12: Results
Amplitude of the amplified pulse is stable with the temperature at the level ~1-2%
Charge of the amplified signal rises by ~5% between T=-20C and T=+50C