## Slide 1: Single cell coordination

## Slide 2
Number | Current location | Main purpose | Latest Activity | Current status | Notes
TE1AES004 | FNAL/A0 | Equator quenching, T-map | RF test | Test more with 2nd sound | 
TE1AES005 | FNAL ICB | CMP, EP, ABLE |  | To be HF rinsed | 
TE1ACC001 | ANL | FE |  | HPR to clean away FE | 
TE1ACC002 | CABOT | CMP |  | RF test done, to be polished at CABOT | 
TE1ACC003 | IB1 | laser remelting | RF tested | To be RF tested | 
TE1ACC004 | IB1 | Tumbling | Quench located | To be RF tested with T-map | 
TE1ACC005 | ANL | Eddy current scanning |  | EP completed, to be HPR and test | 
TE1ACC006 | FNAL_ICB | Eddy current scanning |  | To be progressive EP | 
NR-1 | IB1 | APS Furnace qualification | RF tested | Pumping, waiting to transport to ANL | 
NR-4 | A0 | ABLE EP |  | 120C Baking | 
NR-5 | FNAL/ICB | E-beam remelting on Pit |  | inspected, to be processed | 
NR-6 | FNAL/ICB | Tumble |  | Tumble polishing | 
TE1PAV001 | PAVAC |  |  |  | 
TE1PAV002 | PAVAC |  |  |  | 
TE1PAV003 | PAVAC |  |  |  | 
TE1PAV004 | PAVAC |  |  |  | 
TE1PAV005 | PAVAC |  |  |  | 
TE1PAV006 | PAVAC |  |  |  | 
TE1PAV007 |  |  |  |  | 
TE1CAT001&002 | RRCAT | RRCAT collaboration |  |  | 
TW1AES001 | MDTL | Traveling wave prototype |  | Cavity inspection, Tooling design for BCP | 
TW1AES002 | MDTL | Traveling wave prototype |  | Cavity Inspection | 
Single cell list

## Slide 3: Summary
TE1ACC004, tested again with T-map, quench location identified
TE1ACC003, tested, 39.5 MV/m
NR-1, tested with Q-disease measurement, no Q-disease, no performance degradation
TE1AES004, tested more at A0
NR-4, in progress, Baking at A0, RF test pending
TW1AES001&002 BCP tooling in design
TE1CAT001&002 being shipped.
TE1ACC001&005, in queue at ANL