## Slide 1: Laser re-melting pit technique for single-cell SRF cavity gradient pushing
Mingqi Ge, Genfa Wu, Jinhao Ruan, Thomas nicol, Lance Cooley

## Slide 2
2
Laser source
Ar gas cylinder
CCD camera
Laser beam deliver line
Laser focus platform
X-Y stage
V-block with rollers
Monitor
Gas nozzle holder
Rotation stage
Mirror
LED light
Nozzle
Cavity

## Slide 3: Profile Comparison before and after laser re-melting
3
After re-melting the pit depth changed for 120um to 30 um
Manmade pit

## Slide 4
4
Laser processing of 1.3GHz single-cell cavity TE1ACC003
The Pit before re-melting
After re-melting
400 micron in Diameter
60 Micron in depth

## Slide 5
5
The Pit before re-melting
After re-melting
Images was taken from Kyoto Optical Inspection machine

## Slide 6: Cavity TE1ACC003 vertical test result after laser processing (Eacc=39.5MV/m)