## Slide 1: Single cell coordination

## Slide 2: Summary
TE1ACC004, molding applied
TE1ACC003, tested, verified the flux trapping
NR-1, transported to ANL for VTS.
TE1AES004, tested more at A0
NR-4, Tested, H concentration verified, quenched at 33.1 MV/m, location briefly verified.
TW1AES001&002 BCP tooling being fabricated.
TE1CAT001&002 optically inspected
TE1ACC001&005, in queue at ANL

## Slide 3
Number | Current location | Main purpose | Latest Activity | Current status | Notes
TE1AES004 | FNAL/A0 | Equator quenching, T-map | RF test | Test more with 2nd sound | 
TE1AES005 | FNAL ICB | CMP, EP, ABLE |  | To be HF rinsed | 
TE1ACC001 | ANL | FE |  | HPR to clean away FE | 
TE1ACC002 | CABOT | CMP |  | RF test done, to be polished at CABOT | 
TE1ACC003 | IB1 | laser remelting | RF tested | Flux trapping verified, to be decided | 
TE1ACC004 | IB1 | Tumbling | Inspected/replicated | To ABLE EP | 
TE1ACC005 | ANL | Eddy current scanning |  | EP completed, to be HPR and test | 
TE1ACC006 | FNAL_ICB | Eddy current scanning |  | To be progressive EP | 
NR-1 | IB1 | APS Furnace qualification | RF tested | Pumping, waiting to transport to ANL | 
NR-4 | A0 | ABLE EP | RF tested | Tumble polishing | 
NR-5 | FNAL/ICB | E-beam remelting on Pit |  | inspected, to be processed | 
NR-6 | FNAL/ICB | Tumble |  | Tumble polishing | 
TE1PAV001 | PAVAC |  |  |  | 
TE1PAV002 | PAVAC |  |  |  | 
TE1PAV003 | PAVAC |  |  |  | 
TE1PAV004 | PAVAC |  |  |  | 
TE1PAV005 | PAVAC |  |  |  | 
TE1PAV006 | PAVAC |  |  |  | 
TE1PAV007 |  |  |  |  | 
TE1CAT001 | RRCAT | RRCAT collaboration | Inspected | Tumble polishing | 
TE1CAT002 | RRCAT | RRCAT collaboration | Inspected | Bulk EP | 
TW1AES001 | MDTL | Traveling wave prototype |  | Cavity inspection, Tooling design for BCP | 
TW1AES002 | MDTL | Traveling wave prototype |  | Cavity Inspection | 
Single cell list