## Slide 1: Single cell coordination

## Slide 2
Single Cell Cavity Activity Plan
ANL EP optimization (TE1AES005, TE1ACC001)
R&D cavities A. Tumble, 2 cavities (TE1ACC004, NR-6, TE1CAT001) B. Laser re-melting, 2 cavities (TE1ACC003) C. CMP process, 1-2 cavities D. ECS investigation, 2 cavities (TE1ACC005, TE1ACC006) E. manufacturing optimization, 2 cavities F. Atomic Layer Deposition (ALD) cavities
  G. Traveling wave cavity, 2 cavities
Vendor qualification RRCAT, 2 cavities (TE1CAT001, TE1CAT002)
ABLE EP 2 cavities
Infrastructure support Furnace verification, 1 cavity. (completed) Diode T-map and second sound development 1 cavity ANL HPR water verification 1 cavity
Basic R&D
A. EP cavity Q-slope studies
B. General Q-slope studies (TE1AES002)

## Slide 3: Summary
TE1ACC003 (Laser), 120C Baking completed, in queue for RF test.
TE1ACC005&006 (ECS), Replica in progress.
TW1AES001&002 (traveling wave), in queue for BCP this week.
TE1CAT001/NR-6, tumble polishing completed, in queue for EP.
TE1CAT002 (India collab.), RF test done, quenched at 21 MV/m, quench area identified with two thermometer bands
TE1AES004 (basic SRF), in queue for HPR/Assy.

## Slide 4
Number | Current location | Main purpose | Latest Activity | Current status | Notes
TE1AES004 | ANL | Equator quenching, T-map |  | In queue for HPR/assy. | 
TE1AES005 | MDTL | CMP, EP, ABLE |  | To be HF rinsed | 
TE1ACC001 | IB1 | FE |  |  | 
TE1ACC002 | CABOT | CMP |  | RF test done, to be polished at CABOT | 
TE1ACC003 | IB1 | laser remelting | 120C baking | In queue for RF test. | 
TE1ACC004 | MDTL | Tumbling | Inspected/replicated | To ABLE EP | 
TE1ACC005 | IMDTL | Eddy current scanning | Molding | Optical inspection and one final EP (40micon) | 
TE1ACC006 | MDTL | Eddy current scanning | Molding | To be progressive EP | 
NR-1 | ANL | ANL RF commissioning | RF tested |  | 
NR-4 | IB1 | ABLE EP | RF tested | One more RF test for Q-disease study | 
NR-5 | FNAL/ICB | E-beam remelting on Pit |  | inspected, to be processed | 
NR-6 | FNAL/ICB | Tumble | Tumble polishing | In queue for EP | 
TE1PAV001 | PAVAC |  |  |  | 
TE1PAV002 | PAVAC |  |  |  | 
TE1PAV003 | PAVAC |  |  |  | 
TE1PAV004 | PAVAC |  |  |  | 
TE1PAV005 | PAVAC |  |  |  | 
TE1PAV006 | PAVAC |  |  |  | 
TE1CAT001 | ICB | RRCAT collaboration | Tumble polishing | In queue for EP | 
TE1CAT002 | IB1 | RRCAT collaboration | RF test | Visual inspection | 
TW1AES001 | ANL | Traveling wave prototype |  | Cavity inspection, Tooling design for BCP | 
TW1AES002 | ANL | Traveling wave prototype |  | Cavity Inspection | 
Single cell list

## Slide 5
Chart: TE1CAT002 - Q vs E Test on 3/3/2010
| 3.3298545399999995 | 3.32073946 | 3.31722055 | 3.2934003700000001 | 3.2966103699999998 | 2.6808645100000001 | 2.22543311 | 1.9796412899999996 | 1.7139203799999998 | 1.43030722 | 1.18492745 | 1.0594870000000001 | 0.82247315099999996 | 2.85732031 | 3.1264021599999996 | 3.3572291799999996 | 3.5966763799999995 | 3.9535016700000001 | 4.2377226400000003 | 4.536701690000001 | 4.9673729399999988 | 5.1909808899999978 | 5.5431908599999993 | 6.0560039899999998 | 6.4807355499999995 | 6.919561390000001 | 7.3532583999999996 | 7.6269503299999979 | 7.9437643199999997 | 8.2997475100000013 | 8.4635110100000013 | 9.1387168699999997 | 8.9255531300000008 | 8.756685130000001 | 9.2322283199999973 | 9.6227041800000013 | 10.0178455 | 10.3743908 | 10.984875000000001 | 11.631062099999999 | 12.0923658 | 12.7855279 | 13.244103999999998 | 13.877061100000001 | 14.331020799999999 | 15.018213399999997 | 15.741213899999996 | 16.446034099999995 | 17.254276900000001 | 17.991795499999995 | 18.351627700000005 | 19.043035700000001 | 19.803149599999998 | 20.222639999999988 | 20.770319599999997 | 20.965282299999988 | 20.958699399999997
3/5/2010 | 22588471300 | 22221321000 | 22193801800 | 22059495100 | 22044941400 | 21826628300 | 21423125300 | 20877407100 | 20390957700 | 19961358900 | 19322018200 | 19125223300 | 18416831000 | 21851640300 | 21763314200 | 21978042700 | 22183194700 | 22313824200 | 22380982700 | 22328730700 | 21992540400 | 21889430300 | 21613414700 | 21549160700 | 21341193000 | 21016965800 | 20676400100 | 20474348900 | 20197745800 | 19835934600 | 19669915200 | 19130695800 | 19295146500 | 19496755900 | 18952369200 | 18783670400 | 18562038600 | 18280187200 | 17806980200 | 17373696500 | 17083260800 | 16575924100 | 16313630200 | 15989460600 | 15974665500 | 15609544800 | 15341115800 | 15039974800 | 14792838700 | 14551236500 | 14432294200 | 14252400700 | 14082934300 | 13826686300 | 13722342300 | 12944487000 | 13003201900
Ozelis, Wu
Quench at 21 MV/m

## Slide 6
Band 1
Band 2
TE1CAT002 T-map data at 21 MV/m