## Slide 1: Single cell coordination

## Slide 2
Single Cell Cavity Activity Outline
ANL EP optimization (TE1AES005)
R&D cavities A. Tumble, 2 cavities (TE1ACC004, NR-6, TE1CAT001, TE1CAT002) B. Laser re-melting, 2 cavities (TE1ACC003) C. CMP process, 1-2 cavities D. ECS investigation, 2 cavities (TE1ACC005, TE1ACC006) E. manufacturing optimization, 2 cavities F. Atomic Layer Deposition (ALD) cavities
  G. Traveling wave cavity, 2 cavities (TW1AES001, TW1AES002)
Vendor qualification RRCAT Collaboration, 2 cavities (TE1CAT001, TE1CAT002)
ABLE EP 2 cavities (NR-4)
Infrastructure support Furnace verification, 1 cavity. (completed) Diode T-map and second sound development 1 cavity (TE1ACC001) ANL HPR water verification 1 cavity (TE1ACC001)
Basic R&D
A. EP cavity Q-slope studies
B. General Q-slope studies (TE1AES002)

## Slide 3
Number | Current location | Main purpose | Latest Activity | Current status | Notes
TE1AES004 | ANL | Equator quenching, T-map |  | In queue for HPR/assy. | 
TE1AES005 | ICB | CMP, EP, ABLE |  | To be HF rinsed | 
TE1ACC001 | ICB |  |  |  | 
TE1ACC002 | CABOT | CMP |  | RF test done, to be polished at CABOT | 
TE1ACC003 | A0 | laser remelting | RF test | A0 2nd sound, surface molding | 
TE1ACC004 | ICB | Tumbling | Inspected/replicated |  | 
TE1ACC005 | ICB | Eddy current scanning | Molding | Optical inspected and one final EP (40micon) | 
TE1ACC006 | ICB | Eddy current scanning | Molding | To receive progressive EP | 
NR-1 | ANL | ANL RF commissioning | RF tested |  | 
NR-4 | ABLE | ABLE EP | Immersion EP | To be returned to FNAL | 
NR-5 | FNAL/ICB | E-beam remelting on Pit |  | inspected, to be processed | 
NR-6 | FNAL/ICB | Tumble | 20micron EP | In queue for H bakeout | 
TE1PAV001 | PAVAC |  | Incoming inspection | three inside weld | This wk
TE1PAV002 | PAVAC |  | Incoming inspection |  | 
TE1PAV003 | PAVAC |  | Incoming inspection |  | 
TE1PAV004 | PAVAC |  |  | Three normal weld | 
TE1PAV005 | PAVAC |  |  |  | 
TE1PAV006 | PAVAC |  |  |  | 
TE1CAT001 | ICB | RRCAT collaboration | 20 micron EP | In queue for H bakeout | 
TE1CAT002 | ICB | RRCAT collaboration | Tumble polishing | Final pass tumble polishing | 
TW1AES001 | ICB | Traveling wave prototype | RF test |  | 
TW1AES002 | IB1 | Traveling wave prototype | RF test | RF test with more T-map, and NbTi flanges | 
Single cell list

## Slide 4: For two weeks
TE1ACC003 (Laser)
  Create a low field quench pit, test before & after laser re-melting.
TE1ACC005&006 (ECS)
  Replica done, brief inspection, then in queue for EP (ANL)
TW1AES001&002 (traveling wave)
  TW2 in queue for second RF test(IB1)
TE1CAT001/NR-6 (Tumble Polishing)
  In queue for H-bake, 20 µm EP, RF test
TE1CAT002 (RRCAT collaboration)
  Tumble polishing
TE1AES004 (basic SRF)
  in queue for HPR/Assy. Direct to A0
NR-4 (ABLE electropolishing)
TE1PAVxxx incoming inspection and optical insp.

## Slide 5
Chart: TW1AES002 - Q vs Epk Test on 3/30/2010
| 57.43871976820035 | 57.484270145559577 | 57.460807748227772 | 56.491678937786254 | 55.442297839461091 | 54.264355802541907 | 53.492054644280152 | 52.340747484835475 | 51.070352804436453 | 49.808037378023023 | 48.965199772656852 | 48.039848518209176 | 46.528909394514415 | 45.645781442619594 | 44.356851606643723 | 43.519647227389925 | 42.304899816301585 | 40.984157549209876 | 40.158007489756592 | 38.959004667057229 | 38.11896988959019 | 37.036752298240913 | 35.841069500891237 | 34.416175870879442 | 33.699786433932005 | 32.625324657046846 | 31.299029747405502 | 30.335314318042094 | 29.331642141538669 | 28.135673657230271 | 27.255340772142002 | 26.122459190225296 | 25.098044097569158 | 22.646035673927582 | 23.543469245276359 | 22.03335555446473 | 20.686504098799329 | 19.440431460170171 | 18.624396501023092 | 17.467544746566279 | 16.344318814230888 | 14.133925630766418 | 12.946090174867534 | 11.936172648413962 | 10.918869377745056 | 9.8126035368219142 | 8.8326775230589547 | 7.8132677506444335 | 6.5137707840455024 | 5.521436302320387 | 4.6890510828755705
TW1AES002 | 4585987017.5175 | 4607796375.2888 | 4598475460.892 | 4762062066.8718 | 4916663611.1059 | 5067149429.7401 | 5166010545.2643 | 5297916611.6125 | 5422201643.5905 | 5532665673.1317 | 5591889828.0001 | 5645615628.5661 | 5720855348.207 | 5773567213.9433 | 5839172432.4361 | 5871931909.6156 | 5915895265.1729 | 5964619165.8716 | 5993218870.7456 | 6030377886.7603 | 6049831132.908 | 6073558131.9095 | 6102638870.1323 | 6120607658.5082 | 6128205045.1314 | 6154728464.3247 | 6196922017.1959 | 6218680498.9485 | 6241022875.6244 | 6288108740.8352 | 6332131557.1987 | 6381663310.1782 | 6459603099.7301 | 6630379101.9289 | 6534581878.7162 | 6562747584.3388 | 6620414183.9914 | 6723637371.7051 | 6793876040.7279 | 6885181519.6801 | 6910116427.6725 | 6956867279.6719 | 7034799572.9033 | 7130698843.6054 | 7182582791.5682 | 7299081906.5082 | 7355014221.8224 | 7347890470.158 | 7368065282.7005 | 7419276644.1635 | 7405740299.6317 | 7421043458.8348
TW1AES001 | 6238365107.6152 | 6210931545.3699 | 6221937146.3683 | 6124556181.5369 | 6119538184.8384 | 6136608035.4243 | 6139960868.2143 | 6136770610.6435 | 6083188414.1013 | 6168879135.5073 | 6274509010.3157 | 6138183467.7946 | 6058561821.9413 | 5949813847.0036 | 5921813981.7326 | 5911348083.2369 | 5907865096.3322 | 5786107369.9715 | 5594764802.8626 | 5538308538.9908 | 5489225936.6565 | 5406958696.574 | 5296291988.0267 | 5242328603.021 | 5160282375.5648 | 5073728264.4106 | 5019927825.114 | 4959455336.0731 | 4905771671.026 | 4824505643.281 | 4767058290.4824 | 4703991848.9875 | 4665698788.8994 | 4604066519.4612 | 4556730205.188 | 4479442101.6077 | 4385272523.5706 | 4284658202.4861 | 4244712056.0283 | 4193503498.8383 | 4143591803.2958 | 4055591862.6628 | 4050374593.06 | 3958100989.2992 | 3915267822.2071 | 3894768389.5748 | 3862871960.6884 | 3791655499.9795 | 3721138798.963 | 3631208119.1054 | 3467504097.1233 | 3471664036.6228 | 3524005518.2305
TW2 Waveguide mode | 1548522034.4065 | 1613592858.1625 | 1625097382.9731 | 1664908227.2327 | 1689773047.6111 | 1722503365.0982 | 1741046412.4428 | 1756556829.2035 | 1777593168.329 | 1793176738.0945 | 1811039377.6101 | 1826077563.0554 | 1837897846.8687 | 1792478995.4981 | 1763036920.3577 | 1798761615.8257 | 1738154627.1016 | 1751032507.0905 | 1760608851.1855 | 1768053058.8936 | 1776449723.5802 | 1781906524.9745 | 1793050312.2601 | 1806240720.3152 | 1821569600.7562 | 1835570398.2897 | 1848742621.6803 | 1865211624.6387 | 1889640482.8293 | 1914018269.8607 | 1853140838.7516 | 1865156913.0267 | 1872365123.0962 | 2013983378.4754 | 2062104076.3277 | 2032381211.1674 | 2092220316.0601
TE1AES001 | 18200967010.6574 | 23610397520.718 | 22271347561.9619 | 19410320553.8935 | 23499278588.5013 | 27946710055.5976 | 23152788149.2148 | 16846400277.5159 | 13850370846.9073 | 9912611934.9234 | 8544595375.7088
TE1AES002 | 16650388397.2827 | 24227166368.7949 | 22485845184.6082 | 23883032937.7111 | 23258581863.9412 | 16539955464.245 | 22212879208.1963 | 13094611218.9973 | 10654324354.3224 | 5879484687.2079 | 5101615824.9236 | 3316191776.3987 | 4728108460.1051 | 5922922507.749 | 7108746373.5471 | 7743213077.9083 | 8569649130.5038 | 8401381132.2983 | 8448595942.5048 | 8387987672.4618 | 18445281509.5936
TE1AES003 | 13176635587.0858 | 12726255645.3106 | 14133898361.8337 | 13748377014.5143 | 13426924133.2221 | 13212054849.9733 | 12484497237.5666 | 11526958284.3896 | 11774205549.8212 | 11234010316.6222 | 9847395715.6398 | 8075049479.8654 | 7403019128.0198 | 6571817959.1293 | 5350626988.029 | 3766489307.0009 | 2533802442.0841 | 1783840343.1345 | 1244931906.4541 | 1095392079.5765
TE1AES004 | 24151358239.1292 | 22973425181.1728 | 20786245570.462 | 19937315906.3634 | 19593765753.9676 | 18556664186.9328 | 18021446664.2356 | 17303221271.0754 | 15599872189.9702 | 14864479979.6398 | 13984375047.853 | 12259484603.8538 | 11044394854.372 | 9353685682.4529 | 7914706368.8707 | 7096533560.0428 | 4505099419.3966 | 3045181257.6968 | 1913171180.3562 | 1401658788.4712
TE1AES005 | 10843763153.0474 | 10575594023.5654 | 10462758885.9053 | 10376523162.4895 | 10245143335.7998 | 10115771703.0229 | 10659378883.0661 | 10641164325.5249 | 10430658618.6284 | 9649917749.4631 | 7490386699.612 | 7255996816.1061 | 6620870387.8217 | 5930621336.3989 | 4157952768.9527 | 2795218893.3148 | 2083299448.8903 | 1680920621.3925 | 1418828029.2196 | 1418828029.2196 | 1210823318.2357 | 6679459890.7996 | 8044068552.8033
Traveling wave cavity summary

## Slide 6
Traveling wave cavity summary
Chart: TW1AES002 - Q vs Bpk Test on 3/30/2010
| 94.428734312800827 | 94.503618720024249 | 94.465046751621529 | 92.871807777539615 | 91.146634770089079 | 89.210108745675413 | 87.940452646492332 | 86.047714119060686 | 83.959196787338897 | 81.883961675888187 | 80.498344297451567 | 78.977075228348426 | 76.493105013657413 | 75.041250670973398 | 72.922261711602616 | 71.545905305799778 | 69.548871580087678 | 67.377583272510549 | 66.019400068194102 | 64.04825030298538 | 62.667240748192491 | 60.888084844046844 | 58.922393170399559 | 56.579880966865225 | 55.402143230387061 | 53.635737814872996 | 51.455321013308321 | 49.870981588617873 | 48.220953634048904 | 46.254792293632484 | 44.807533015426195 | 42.945085970325067 | 41.260956849745263 | 37.229877241717674 | 38.705249893028061 | 36.22263668251005 | 34.00842510573586 | 31.959892990075712 | 30.618338918915551 | 28.716485127575005 | 26.869911882805884 | 23.236045538108037 | 21.283254822628027 | 19.62295956938803 | 17.950522219648889 | 16.131831211328532 | 14.520841732920045 | 12.84494131341771 | 10.708580087149636 | 9.0771911999598185 | 7.7087574491718494
TW1AES002 | 4585987017.5175 | 4607796375.2888 | 4598475460.892 | 4762062066.8718 | 4916663611.1059 | 5067149429.7401 | 5166010545.2643 | 5297916611.6125 | 5422201643.5905 | 5532665673.1317 | 5591889828.0001 | 5645615628.5661 | 5720855348.207 | 5773567213.9433 | 5839172432.4361 | 5871931909.6156 | 5915895265.1729 | 5964619165.8716 | 5993218870.7456 | 6030377886.7603 | 6049831132.908 | 6073558131.9095 | 6102638870.1323 | 6120607658.5082 | 6128205045.1314 | 6154728464.3247 | 6196922017.1959 | 6218680498.9485 | 6241022875.6244 | 6288108740.8352 | 6332131557.1987 | 6381663310.1782 | 6459603099.7301 | 6630379101.9289 | 6534581878.7162 | 6562747584.3388 | 6620414183.9914 | 6723637371.7051 | 6793876040.7279 | 6885181519.6801 | 6910116427.6725 | 6956867279.6719 | 7034799572.9033 | 7130698843.6054 | 7182582791.5682 | 7299081906.5082 | 7355014221.8224 | 7347890470.158 | 7368065282.7005 | 7419276644.1635 | 7405740299.6317 | 7421043458.8348
TW1AES001 | 6238365107.6152 | 6210931545.3699 | 6221937146.3683 | 6124556181.5369 | 6119538184.8384 | 6136608035.4243 | 6139960868.2143 | 6136770610.6435 | 6083188414.1013 | 6168879135.5073 | 6274509010.3157 | 6138183467.7946 | 6058561821.9413 | 5949813847.0036 | 5921813981.7326 | 5911348083.2369 | 5907865096.3322 | 5786107369.9715 | 5594764802.8626 | 5538308538.9908 | 5489225936.6565 | 5406958696.574 | 5296291988.0267 | 5242328603.021 | 5160282375.5648 | 5073728264.4106 | 5019927825.114 | 4959455336.0731 | 4905771671.026 | 4824505643.281 | 4767058290.4824 | 4703991848.9875 | 4665698788.8994 | 4604066519.4612 | 4556730205.188 | 4479442101.6077 | 4385272523.5706 | 4284658202.4861 | 4244712056.0283 | 4193503498.8383 | 4143591803.2958 | 4055591862.6628 | 4050374593.06 | 3958100989.2992 | 3915267822.2071 | 3894768389.5748 | 3862871960.6884 | 3791655499.9795 | 3721138798.963 | 3631208119.1054 | 3467504097.1233 | 3471664036.6228 | 3524005518.2305
TW2 Waveguide mode | 1548522034.4065 | 1613592858.1625 | 1625097382.9731 | 1664908227.2327 | 1689773047.6111 | 1722503365.0982 | 1741046412.4428 | 1756556829.2035 | 1777593168.329 | 1793176738.0945 | 1811039377.6101 | 1826077563.0554 | 1837897846.8687 | 1792478995.4981 | 1763036920.3577 | 1798761615.8257 | 1738154627.1016 | 1751032507.0905 | 1760608851.1855 | 1768053058.8936 | 1776449723.5802 | 1781906524.9745 | 1793050312.2601 | 1806240720.3152 | 1821569600.7562 | 1835570398.2897 | 1848742621.6803 | 1865211624.6387 | 1889640482.8293 | 1914018269.8607 | 1853140838.7516 | 1865156913.0267 | 1872365123.0962 | 2013983378.4754 | 2062104076.3277 | 2032381211.1674 | 2092220316.0601
TE1AES001 | 18200967010.6574 | 23610397520.718 | 22271347561.9619 | 19410320553.8935 | 23499278588.5013 | 27946710055.5976 | 23152788149.2148 | 16846400277.5159 | 13850370846.9073 | 9912611934.9234 | 8544595375.7088
TE1AES002 | 16650388397.2827 | 24227166368.7949 | 22485845184.6082 | 23883032937.7111 | 23258581863.9412 | 16539955464.245 | 22212879208.1963 | 13094611218.9973 | 10654324354.3224 | 5879484687.2079 | 5101615824.9236 | 3316191776.3987 | 4728108460.1051 | 5922922507.749 | 7108746373.5471 | 7743213077.9083 | 8569649130.5038 | 8401381132.2983 | 8448595942.5048 | 8387987672.4618 | 18445281509.5936
TE1AES003 | 13176635587.0858 | 12726255645.3106 | 14133898361.8337 | 13748377014.5143 | 13426924133.2221 | 13212054849.9733 | 12484497237.5666 | 11526958284.3896 | 11774205549.8212 | 11234010316.6222 | 9847395715.6398 | 8075049479.8654 | 7403019128.0198 | 6571817959.1293 | 5350626988.029 | 3766489307.0009 | 2533802442.0841 | 1783840343.1345 | 1244931906.4541 | 1095392079.5765
TE1AES004 | 24151358239.1292 | 22973425181.1728 | 20786245570.462 | 19937315906.3634 | 19593765753.9676 | 18556664186.9328 | 18021446664.2356 | 17303221271.0754 | 15599872189.9702 | 14864479979.6398 | 13984375047.853 | 12259484603.8538 | 11044394854.372 | 9353685682.4529 | 7914706368.8707 | 7096533560.0428 | 4505099419.3966 | 3045181257.6968 | 1913171180.3562 | 1401658788.4712
TE1AES005 | 10843763153.0474 | 10575594023.5654 | 10462758885.9053 | 10376523162.4895 | 10245143335.7998 | 10115771703.0229 | 10659378883.0661 | 10641164325.5249 | 10430658618.6284 | 9649917749.4631 | 7490386699.612 | 7255996816.1061 | 6620870387.8217 | 5930621336.3989 | 4157952768.9527 | 2795218893.3148 | 2083299448.8903 | 1680920621.3925 | 1418828029.2196 | 1418828029.2196 | 1210823318.2357 | 6679459890.7996 | 8044068552.8033