## Slide 1: PAVAC cavity 001, 002, 003 optical inspection report
Mingqi Ge and Genfa Wu

## Slide 2: TE1PAV001 – area 1

## Slide 3
TE1PAV001 – area 2

## Slide 4
TE1PAV001 – area 3

## Slide 5: TE1PAC002 area 1

## Slide 6
TE1PAC002 area 2

## Slide 7: TE1PAV003 area 1

## Slide 8
TE1PAV003 area 1 replica result
60 µm deep, sharp edged tool mark

## Slide 9
Summary
Cavity equator welds were inside weld
Weld beads appear polished inside at equators and irises
Defect areas are located
No visible geometric defect at Non-RF sides of weld
002 is the best of the three optically
In queue for EP.