## Slide 1: Furnace commissioning cavity test
1-cell cavities
Niobium witness (RRR 300/450) samples
Actively looking partial pressure info: H, O, N, Hydrocarbons
Titanium shield as backup

## Slide 2
Measure Q0/Eacc
Without light EP
Success!
Specific recipe
800 C/2h
1-cell High performance
With Q-desease after
100K/8h hold
600 C/15h
Furnace results senario
1-cell tumble polished
With Q-desease without
100K/8h hold (extreme)
600 C/24h
Light EP, 120C bake
Requires Light EP
Get second 1-cell
H-stays
H-stays
H-stays
bad
H-is gone
H-is gone
H-is gone
degrades
degrades
High Performance
High Performance