## Slide 1: Cavity Test Results : TB9AES002 & TB9NR002
27th ILC Cavity Grp Mtg. 11/9/2010 J.Ozelis
TB9AES002 (aka AES002) : dressed cavity that received light EP, after limited in 3 vertical tests to 20MV/m (hard quench) TB9NR002 : first cavity fabricated by Niowave/Roarke to be processed/tested

## Slide 2
Chart: ILC- TB9AES002 - Q vs E
Early FE onset (9 MV/m), processed away. FE returned at 18MV/m. Limited by FE-induced quench at 27.3MV/m. LF Q0 1.9 x 1010 (“hump”), strong Q0 drop due to FE loading at 20MV/m. Improvement from previous 19.8MV/m (hard) quench limit, but FE much worse, and overall Q0 is lower (LF and HF).

## Slide 3
Chart: ILC-TB9NR002 - Q vs E
After 1st quench | 1
First N/R cavity to be tested. Full processing at FNAL/ANL. Quench limited to 28.5 MV/m (with Q0 there 1.2 x 1010). Also good LF Q0 (2.1 x 1010), no FE. At 1.8K, Q0 improves by 30-40% (typical).

## Slide 4
Mode meas & OST data indicate cell #2 as limiting cell. Others do better : 30– 43MV/m. Recent re-tests w/ thermometry and optimized placement of OST’s indicate cells 1 and 2 are limiting performance at the 28-29 MV/m level.

## Slide 5
Residual surface resistance ~7nW.
Chart: ILC-TB9NR002 - Rs vs T
| 0.50371489736808972 | 0.55355660116246885 | 0.57208237986270027 | 0.58309037900874638 | 0.60551014229488342 | 0.62053986968662733 | 0.63806029669803799 | 0.65284804961645182 | 0.66082934082273248 | 0.66137566137566139
 | 12.7808 | 9.4073 | 8.6841 | 8.243 | 7.8238 | 7.5338 | 7.1859 | 7.0486 | 7.0367 | 7.1235