## Slide 1: Dynamic Loss Measurement
 | C-4 Z109 Nov. 16, 17 | C-1 AES004 Nov. 18, 19 | A-3 MHI07 Nov. 23 | A-2 MHI06 Nov. 24 | A-2 MHI06 Nov. 25
Measured Gradient | 28 MV/m | 25.2 MV/m | 32.3 MV/m | 38 MV/m | 32 MV/m
Dynamic Loss | 0.84 W | 1.44 W | 2.77 W | 4.76 W | 2.55 W
Detuned Loss | 0.09 W | 0.18 W | 0.73 W | 1.84 W | 1.22 W
Dynamic Loss at Cavity | 0.75 W | 1.26 W | 2.04 W | 2.92 W | 1.33 W
Q0 | 8.8E9 | 4.3E9 | 4.3E9 | 4.2E9 | 6.5E9
Dynamic Loss measurements were performed on C-4, C-1, A-3 and A-2.
Detuned 4 cavities dynamic Loss measurement at 32 MV/m.
  Measurements of heat loss for DESY and KEK input couplers.
  Measurement for DESY input couplers was performed at Nov. 26.
  Measurement for KEK input couplers is scheduled at Nov. 30.

## Slide 2: C4 Dynamic Loss Measurement
28MV/m
Detuned
28MV/m
Static Loss Meas.
No RF
Static Loss Meas.
Static Loss Meas.

## Slide 3: C1 Dynamic Loss Measurement
25.2MV/m
Detuned
25.2 MV/m
Static Loss Meas.
Static Loss Meas.

## Slide 4: A3 Dynamic Loss Measurement
32.3 MV/m
Detuned
32.3 MV/m
No RF
Static Loss Meas.
Static Loss Meas.

## Slide 5: A2 Dynamic Loss Measurement
38 MV/m
Detuned
38 MV/m
Static Loss Meas.
Static Loss Meas.

## Slide 6: A2 Dynamic Loss Measurement
32 MV/m
Detuned
32 MV/m
Static Loss Meas.
Static Loss Meas.

## Slide 7: Detuned four cavities (FNAL/DESY)
Detuned 32 MV/m
Static Loss Meas.
17.4 m3/h
16.9 m3/h
m= 17.4－16.9 = 0.5 m3/h (= 0.5W)