## Slide 1
Chart: A10 (VEP) Performance Compared to RI 28 (HEP) Both Cavities Tested at 2K
| 2.11 | 3.04 | 4.01 | 5.09 | 5.95 | 6.99 | 8.08 | 8.0300000000000011 | 9.0400000000000009 | 10.1 | 11.1 | 12 | 13 | 14.2 | 15 | 16.2 | 17.100000000000001 | 18.100000000000001 | 19.2 | 19.899999999999999 | 21.2 | 22.1 | 23.1 | 24.1 | 24.1 | 25.3 | 26 | 27.2 | 28.1 | 29.2 | 30.1 | 30.1 | 30.2 | 31.1 | 32.1 | 33.200000000000003 | 34.200000000000003 | 35.4 | 35.5 | 36 | 36.5 | 36.700000000000003 | 36.9 | 37.300000000000004 | 37.6 | 38.1 | 38.4 | 38.700000000000003 | 38.800000000000004
RI 28 18oct10_JLab | 23600000000 | 23900000000 | 23500000000 | 22900000000 | 22700000000 | 22300000000 | 21900000000 | 21900000000 | 21400000000 | 20800000000 | 20200000000 | 19600000000 | 19000000000 | 18300000000 | 17800000000 | 17300000000 | 17000000000 | 16600000000 | 16300000000 | 16300000000 | 16000000000 | 15900000000 | 15800000000 | 15800000000 | 15900000000 | 15800000000 | 15800000000 | 15700000000 | 15700000000 | 15600000000 | 15500000000 | 15500000000 | 15500000000 | 15400000000 | 15400000000 | 15200000000 | 15100000000 | 15000000000 | 15000000000 | 14900000000 | 14800000000 | 14800000000 | 14800000000 | 14700000000 | 14600000000 | 14500000000 | 14400000000 | 14200000000 | 14100000000
A 10_22nov10_Cornell | 27443531189.5292 | 26906528497.1976 | 26602085741.8447 | 25024068522.4521 | 21638798027.597 | 20049730699.8 | 18189529191.5528 | 16702522882.6792 | 15513344625.4322
A10 Treatment:
Slow tumbling -50 µm
VEP -120 µm
800C x 2 hours
HPR
110C x 48 hours
RF test
ACrawford
Cornell SRF
7dec10

## Slide 2
Chart: A10_22dec10
| 3.7485087686756655 | 5.2349520372717562 | 7.4721517390426575 | 10.220290311732814 | 13.55668819760653 | 16.069469925985789 | 19.050323762952384 | 21.040664717028946 | 22.980156943691071
A10_22dec10 | 0.012 | 0.012 | 0.012 | 0.012 | 0.012 | 0.014 | 11 | 30 | 73

## Slide 3
AES_5 will get its final EP next week
A_9 will be tested in January before its final EP
A_10 will be retested with OSTs
  RG174 cables used for OST readout in previous Cornell tests were magnetic and were eliminated from the A_10 test of 22nov10. They will be replaced with all copper RG174 cables for future tests
  Mode analysis is inconclusive for this cavity. The quench could be in cells 1,2,7 or 8
ACrawford
Cornell SRF
7dec10

## Slide 4
ACrawford 7dec10
Modified Titanium Ptrans Feedthrough
Antenna is Niobium

## Slide 5
1-72 Thread
ACrawford 7dec10
Modified Titanium Ptrans Feedthrough
Antenna is Niobium