## Slide 1
Cavity status; recent KEK activities
2011.01.11: Hayano
(1) MHI-012, MHI-013 ; 9 cell cavities field measurements
MHI-012: 1st VT 37.5MV/m @ Q0=5.5E09 Nov 11,2010
MHI-013: 1st VT 36.5MV/m @ Q0=7.5E09 Nov 25,2010,
it was reported in the last S0-meeting.
After then,
MHI-012: 2nd VT 40.7MV/m @ Q0=6.2E09 Dec 08,2010
MHI-013: 2nd VT 32.2MV/m @ Q0=8.8E09 Dec 22,2010,

## Slide 2
MHI-012 2nd VT reached 40.7MV/m
Intentional power stop at 40MV/m
ILC specification

## Slide 3
MHI-013 2nd VT reaches 32.2MV/m
Vacuum leak at beam-pipe flange during antenna assy.
Helico-flex was exchanged.
Quench at #2-cell 90-120degree.

## Slide 4
MHI-012 X-ray

## Slide 5
MHI-013 X-ray