## Slide 1: Proposal to include future 9-cell cavity test results from FNAL and KEK in ILC global data base for ILC gradient yield analysis
Rongli Geng
January 11, 2011
ILC Cavity Group Meeting

## Slide 2: FNAL/ANL processing and testing results
High quality test results reported due to high quality processing and joint ANL/FNAL facilities.
TB9RI29, 5/21/2010, 34.6 MV/m, qt Q0=1.2E10, 1st pass.
TB9RI20, 11/23/2010, 36.1 MV/m at Q0=1.1E10, 2nd pass after re-EP.
TB9RI24, 12/14/2010, 36.0 MV/m at Q0=1.1E10, 3rd pass after 2 x re-EP.
TB9ACC015, 12/21/2010, 34.5 MV/m at Q0=1.4E10, 2nd pass after resetting by mechanical polishing and re-processing.

## Slide 3: Include FNAL/ANL processed cavity test results in ILC database
High quality results validates FNAL/ANL processing facilities and procedures.
Future test results of RI built and AES built cavities should be included without bias in ILC global database and included for yield analysis.
Cavities originated from other builders should not be included until vendor becomes “certified”.

## Slide 4: KEK processing and testing results
MHI-12, 11/11/2010, 37.5 MV/m at Q0=5.5E9, 1st pass.
MHI-13, 11/25/2010, 36.5 MV/m at Q0=7.5E9, 1st pass.

## Slide 5: Include KEK processed cavity test results in ILC database
High quality results validates KEK processing facilities and procedures.
High quality result validates MHI as a certified vendor for ILC cavities.
Future KEK test results of MHI built cavities should be included without bias in ILC global database and included for yield analysis.
Cavities originated from other builders should not be included until vendor becomes “certified”.

## Slide 6: For consistent yield analysis
1st pass result following regular processing and testing consistent with ILC baseline recipe.
Stop processing if cavity meets ILC vertical test spec.
IF 1st pass fails meeting spec, THEN data driven 2nd pass processing (re-HPR, re-EP, repair…).