## Slide 1: (An Introduction to) Characterization of Crystals for Dual Readout Calorimetry
Adam Para
July 15, 2011

## Slide 2: Need of Crystals
We want to construct very large calorimeter from scintillating crystals.
Cherenkov light is in UV/blue: need good transmission for short wavelength.
We want to read out, and distinguish the scintillation and Cherenkov light. It is desirable that the scintillation light is ~green/yellow and slow
We need large quantities of crystals: they need to be inexpensive

## Slide 3: Candidate Crystal: PbF2
PbF2 is an excellent Cherenkov radiator (good transparency down to l=250nm)
It is potentially an inexpensive crystal (melting temperature ~850C)
It needs to be doped to make it scintillate. This is in principle an advantage:
  Tailor the scintillating agent to match our requirements (emission spectrum, response time)
Challenges:
  Find the scintillating dopants which are compatible with PbF2 crystals production
  Find dopants which do not affect (in a major way) transparency to Cherenkov light

## Slide 4
 | Doping |  | Doping |  |  |  | Doping
1 | none | 11 | 0.5% BaF2 +0.25%EuF3 | 21 | 0.2% BiF3 | 31 | 5% BaF2 +0.25%EuF3
2 | 0.05% CaF2 +0.5%EuF3 | 12 | 5% BaF2 | 22 | 0.75% BiF3 +0.35%EuF3 | 32 | 0.5% CaF2 +1%EuF3
3 | 1% CaF2 + 1%EuF3 | 13 | 10% BaF2 +0.25%EuF3 | 23 | 0.75% BiF3 +0.35%EuF3 +0.07%NaF | 33 | 1% CaF2 +0.25%EuF3
4 | 0.2% CaF2 +0.25%EuF3 | 14 | 1% BaF2 | 24 | 1% BaF2 +0.25%EuF3 | 34 | 0.05% CaF2 +0.25%EuF3
5 | 1% CaF2 | 15 | 0.25%ErF3 | 25 | 1.5% BiF3 +0.7%HoF3 +0.15%NaF | 35 | (213-B) +0.1%Tb
6 | 0.2% CaF2 +0.25%EuF3 +0.025%YF3 | 16 | 0.2% CaF2 | 26 | 0.75% BiF3 +0.35%ErF3 +0.07%NaF | 36 | (93302-3) +0.1%Pr
7 | 0.2% SrF2 | 17 | 0.25% SmF3 | 27 | 0.75% BiF3 +0.35%SmF3 +0.07%NaF | 37 | (93302-4) +0.1%Nd
8 | 0.5% SrF2 +0.25%EuF3 | 18 | 0.25% HoF3 | 28 | 0.35%HoF3 +0.07%NaF | 38 | (93302-3) +0.1%Yb
9 | 0.5% SrF2 +1%EuF3 | 19 | 0.25% GdF3 | 29 | 0.35%ErF3 +0.07%NaF | 39 | (93307-6)) +0.1%Sm
10 | 0.2% BaF2 | 20 | 0.25% PrF3 | 30 | 0.35%SmF3 +0.07%NaF | 40 | (P983309-4) +5000ppmTb +100ppmCe

## Slide 5: Sample Crystals Under UV excitation

## Slide 6: Transmission Measurement
Photodetector
Diffraction
grating
Crystal

## Slide 7: Emission Spectrum Measurement
Photodetector
Diffraction
grating
Crystal

## Slide 8: Excitation Spectrum Measurement
Photodetector
Diffraction
grating
Crystal

## Slide 9: A Complete Picture

## Slide 10: (Examples of) Emission Spectra

## Slide 11
Analysis requires comparisons and finding correlations between large number of plots. Image browser utility of great help.
Browsing the image data base extremely helpful to find various defects and errors in labeling and presentation. They can (and are) fixed. But we need some cleanup utility to remove (or mark to be invisible) unwanted versions of the plots.