## Slide 1: Preliminary Studies for future hanronic calorimeter
I. Vasilas , A.Para, P. Rubinov, H.Wenzel, F. Ptochos
University of Cyprus , Fermilab
IEEE Valencia, 2011

## Slide 2: Introduction
future hadronic calorimeters require energy resolution below 10%/√E (ΔΕ/Ε)
e-
π+
π-
p+n
γ
e-
p
n
- nuclei binding energy
hadron
γ+γ
πo
e+
γ
γ
γ
Nuclei binding energy lost = bad energy resolution in hadrons calorimeters
  Dual Readout techniques are plausible to achieve this kind of resolution.
the main disadvantage for presents hadronic calorimeter is the bad energy resolution ~60%/√E (ΔΕ/Ε)

## Slide 3: Motivation
  using data from 120 GeV proton beam we evaluate the performance of
  different size SiPM ‘s
  different Geometries of BGO and PbF2 crystal samples
  compare the results with light production in crystals simulations
  to optimize the collection of Cherenkov and Scintillation light components for application of the Dual Readout technique
  require an excellent Cherenkov light collection,
Dual Readout techniques : are based on the connected relationship of EM showers created by charged and neutral pions ~ 1. Measuring Cherenkov and Scintillation radiation light (depocit by neutral pions) , an event by event precise energy correction is possible.

## Slide 4: motivation
  using data from 120 GeV proton beam we evaluate the performance of
  different size SiPM ‘s
  different Geometries of BGO and PbF2 crystal samples
  Dual Readout techniques are plausible to achieve this kind of resolution.
future hadronic calorimeter requires energy resolution below 20%/√E (ΔΕ/Ε)
  compare the results with GEANT 4 light production simulations in crystals
  to optimize the collection of Cherenkov and Scintillation light components for application of the Dual Readout technique
  require an excellent Cherenkov light collection, so you can be able to correct the nuclei energy lost in hadronic calorimeter volume

## Slide 5: Test beam setup
all exposure to a 120GeV proton beam
BGO crystal 5x5x5 cm
all sides equipped with visible or UV filters
two opposite sides, one with UV and one with visible filter viewed by conventional PMT’s
4 sides viewed by 9 SiPM’s 1mm2 Hamamatsu 25, 50 and 100 microns size pixels
BGO and PbF2 crystals 4x4x5, 3x3x5, and 2x2x5 cm
all equipped with a 3 mm2 Hamamatsu SiPM (on the side of the beam)
crystals wrapped using black and white Tyvek
crystals with different surface finish
Setup 2
Setup 1
Beam
Beam

## Slide 6: Data readout
For data readout we use TB4 readout boards build at Fermilab (Paul Rubinov).
Each board has 4 individual readout channels
gain 40db
bandwidth 100Mhz
50ohm input
pedestal is around 8200 counts
Support with USB 100 mbit Ethernet
Each channel can provide bias voltage to SiPM’s (until 100 Volts)
we took data for 11 different operating bias voltage (+/-) 1 volt from nominal bias voltage with step of 25 mvolts)
the gate window for each waveform was 2 μsec = 400 time slots *5 ns
Works on Win(XP,Vista,2000) using Ms .net
with C# express edition (free software)

## Slide 7: SiPM’s calibration
From data without beam
For all detectors, we observe events waveforms for all operating bias voltages steps
Optimal Bias Voltage
Low Bias Voltage
Clean single pulse shapes indicates the optimal bias voltage
Determination of optimal operating bias voltage
High Bias Voltage
Event Waveform
Event Waveform
Event Waveform

## Slide 8: SiPM’s calibration
Determination of Electronic Noise And Threshold
Any value between first peak and first step is a suitable for threshold
first peak corresponds to noise, second step to 1 pe, third step to 2 pe etc
for every channel we subtract the electronic noise from every events time slot
constructed the distribution of events waveforms values
mean value of the fit correspond to electronic noise
Waveforms are assembled from 400 time slots. For each channel, we construct the Gaussian distribution from for each time slots value using all the events.
noise
1pe
2pe
Slot Values Distribution
Wfm Values Distribution
Wfm Values Distribution

## Slide 9: Sipm’s Calibration
We want to calculate the charge corresponds to a single avalanche.
isolate the pulse shape using a 100 ns window (25ns before and 75 ns after maximum peak) and we integrate to find single pe charge.
for every event, we found the maximum value of the waveform above threshold.
we compare the values of the sidebands
if were significantly different we rejected the event from further analysis.
if were not different we subtract their average value from single pe charge
for each channel we constructed the distribution of single pe charge for all the events and fit a Gaussian function.
Determination of a Single Avalanche Charge
with the same time window we isolate sidebands regions to find charge causes from noise.
charge = 617.5
Signal Wfm
Single pe Charge Distribution

## Slide 10: Test - Beam Data Analysis
average number of photons
we divide total charge with the value corresponds to 1 pe charge to find the average number of photons detected.
for each channel we found the average waveforms with and without beam conditions.
Setup 2 ( small crystals)
we subtract them and integrate to find total charge.
An example of Cherenkov light detected (67,4 photons) from PbF2 crystal. This is the first Cherenkov photons reported measurement with SiPM’s .
Average Number of Photons Detected

## Slide 11: Test - Beam Results
Geometry Dependence
BGO | 
Geometry (cm) | Numbers of Photons
4x4 | 650,58
3x3 | 1121,35
2x2 | 1503,88
2x2 | 1595,22
PbF2 | 
4x4 | 52,74
3x3 | 61,36
2x2 | 68,36
2x2 | 67,38
From our results, on average, we detect more photons by using smaller crystal.

## Slide 12: Test - Beam Results
Surface Finish Dependence
BGO |  | 
Surface | Geometry (cm) | Numbers of Photons
no polish | 2x2 | 1503,88
polish | 2x2 | 1595,22
We use 2x2x5 cm BGO crystals, with polished and no polished surface
We detected small difference ~6 % in the average number of photons detected between polished crystals and crystals without surface finish

## Slide 13: Test - Beam Results
Wrapping Dependence
material | BGO | 
 | Geometry (cm) | Numbers of Photons
Black | 4x4 | 650,58
 | 3x3 | 1121,35
White | 4x4 | 793,37
 | 3x3 | 1453,59
BGO crystals wrapped with white and black Tyvec
(22 % for 4x4 and 30 % for 3x3 crystals)
the average number of photons detected are consistently bigger in crystals wrapped in white paper, than in black Tyvec

## Slide 14: c/s Separation
Setup 1 5x5x5 cm BGO crystal
we compare the average signal light waveform coming from PbF2 crystal (only Cherenkov) and the average signal light waveform coming from the BGO crystal thru UV filter
The presence of a filter is not enough to collect pure Cherenkov light so we have to find a way separate Cherenkov from scintillation light
From the average signal light waveform coming form BGO crystal thru visible filter we see that scintillation light is passing through UV filters and we collect it as Cherenkov light
we can see an extended tail not consisted with Cherenkov light signal
BGO UV filter
BGO visible filter
PbF2
Average Wfm
Average Wfm
Average Wfm

## Slide 15: C/S Separation
We integrate the waveforms using a window (150 ns) free from Cherenkov light and we divide them to find a scale factor.
We integrate the new waveforms, we subtract them and divide by the UV signal waveforms integral .
We choose symmetrically placed detectors (behind visible and UV filter)
We multiply the Scintillation shape with the scale factor.
With this curve we can determine the fraction of pure Cherenkov light detected from BGO crystal with this particular filter (UV-11) with this particular detectors(SiPM 3 mm2 50 microns)
C/S Separation

## Slide 16: FUTURE PLANS
Much to be done
Data analysis is still in progress
we need to polish our results
we will continue with data not analyzed yet, for example we need to analyze data taken by scanning, with the beam, the 5x5x5 BGO crystal in various places
Simulations are on the way, we are going to simulate crystals light yield and compare with our results
Once we finish analysis and understand the results, we are planning to proceed to a second test beam experiment using several other kind of crystals, and SiPM’s.
a new setup (telescope) is almost ready to take data by exposure BGO and PbF2 crystals of various shapes, Geometries and surface into Cosmic Rays beam

## Slide 17: Back up