Scanning Electron Microscope (SEM) in situ field emission measurement in Uppsala Univ.
Tomoko Muranaka
CERN, Switzerland
25 October 2012, LCWS12
This work is Supported by the 7th European Framework program (FP7) EuCARD, No. 227579

---
Background
Location: Developments & Experiments in Uppsala Univ. (UU).
Motivation: CLIC feasibility study / fundamental interest of understanding FE and BD phenomena, of material science.
Purpose: Find dependencies (field, time, gap, geometry, material, treatment, …, crystal orientation,…)
Speciality 1: Local filed emission and breakdown measurements inside an SEM.
Speciality 2: Post-breakdown surface & sub-surface analyses by Focused Ion Beam (FIB) and SEM.

---
Ideas – What we can do
Speciality 1: Local filed emission and breakdown measurements inside an SEM.
Reproduce high-gradient electric field condition in µm range (1kV/µm = 1GV/m)
2D scan with controlled gap distance.
Measurement and observations in one instrument.
Compact & transportable experimental setup.
Complementary work with Wuppertal Univ.
[Speaker Notes: Scanning Electron Microscopes (SEM) open an opportunity to investigate local processes during breakdown]

---
Courtesy of Stefan Lagotzky, Günter Müller, Berg. Universität Wuppertal
FE & SEM measurement techniques
- localisation of emitters
- FE properties
Field emission scanning microscope (FESM):
500 MV/m
10-7 mbar
10-9 mbar
Regulated V(x,y) scans for FE current I=1 nA & gap ∆z  emitter density at E=U/∆z
Spatially resolved I(E) measurements of single emitters  Eon, βFN, S
Ion bombardment (Ar, Eion= 0 – 5 kV) and SEM (low res.)
In-situ heat treatments up to 1000°C
Ex-situ SEM + EDX
Identification of emitting defects
Correlation of surface features to FE properties (positioning accuracy ~ ±100 µm)

---
Courtesy of Stefan Lagotzky, Günter Müller, Berg. Universität Wuppertal
Samples
Two flat Cu samples
Diameter: ~11 mm
One hole as mark to identify the position in different systems
Diamond turned and glued to a sample holder at CERN
Mounted to an adapter for the FESM at BUW
Surface cleaned with ionized N2, cleanroom condition (class 100) with 5 bar pressure
Teflon protection cap to avoid damage and contaminations after polishing and cleaning
Only 1 sample measured yet
Protection cap
Investigated
surface
sample
holder
FESM adapter

---
Courtesy of Stefan Lagotzky, Günter Müller, Berg. Universität Wuppertal
FESM results
Regulated E(x,y) maps for I = 1 nA , ∆z ≈ 50 µm of the same area
130 MV/m
160 MV/m
190 MV/m
Possible explanations:
Surface oxide
adsorbates
EFE starts at 130MV/m and not 500MV/m
Emitter density increases exponentially with field
Activated emitters: Eact=(1,2 – 1,4)∙Eon
2nd measurement: shifted to lower fields
Eon = 120 MV/m

---
Experiment setup in UU
Keithley
6517A
A
Cathode: Cu samples provided by CERN, 12mm-D, XY-stage
Anode: W tip commercially available, 5μm-R, Z-stage
Gap: 1.0 ± 0.1 μm
Background current ≈0.02pA

---
SmarAct Piezo positionner http://www.smaract.de/

---
Real life
W tip
Cu
surface
The new scanning stages installed this week
W tip
Cu sample
Piezo Z-stage
Piezo XY-stage
Targeted scan
Emission “SPOT” (≠area)
Surface observation before&after
Built-in SEM sample stage

---
Example:
Grain orientation dependence
(done with the old setup)
1. Approach W tip to the sample surface ~1μm
2. Take SEM images of target area
3. Apply HV on W tip from 0V up to 1kV with 1V step
4. Measure emission current from Cu sample
5. Stop HV supply once the current exceeds 10 nA (onset voltage)
6. Repeat 5 runs at the same spot
7. Move sliders to a new spot (blind)
8. Analyses: Comparison of onset voltage of each spots, Electron Backscatter Diffraction (EBSD) in order to identify grain orientations of spots.

---
Cathode: Cu, without etching, heated with H2 at 1040°C
1.2mm
Location of spots
1
10
13 14 15
3
4
6
2
5
9 8 7
12 11

---
Grain orientations of measured area
G6
G3
G2
G7
G4
G1
G5
EBSD image: courtesy of M. Aicheler, CERN
G6
G3
G2
G7
G4
G1
G5

---
Grain orientation dependence
Spot No.
12
S6 (110)
8
10
9
11
S3 (100)
7
2
1
6
14
15
3
5
Green: 110
Red: 100
Pink: 100-111
S14 (111-001)

---
Summary
The onset voltages where the measured current exceeded 10 nA were varied from 300 V to over 1000 V.
The onset voltages were decreased at subsequent runs at most of spots (cf. Wuppertal's result).
In order to study any dependences of emission behavior, more statistics are required.
We are now almost ready to perform local field emission measurements with piezo scanners.

---
Co-workers
Volker Ziemann, volker.ziemann@physics.uu.se
Klaus Leifer, Klaus.Leifer@Angstrom.uu.se
Mechanical drawing and manufacture
Masih Noor
Lars-Erik Lindquist
 25 Feb. 2012, Abisko, Sweden

---
Backups
04/10/2012
MeVArc12, Albuquerque NM, T. Muranaka

---
Emission stability measurement
1. Approach W tip to the sample surface ~1μm
2. Take SEM images of target area
3. Apply HV on W tip from 0V up to 1kV with 1V step
4. Measure emission current from Cu sample
5. Once the measured current exceeds 1pA, keep the voltage and continue current measurement for 20 minutes
6. Repeat 3-5
7. Stop measurement once the measured current exceeds 10nA.

---
Emission stability measurement
1000 points at 273V
10-12
1200 points at 217V
10-9
2
6
3
4
No emission >1pA
between 218-272V
4
2
`
3
3
2
Measured Current [A]
1
3
4
2
2
1
1
Step
Step
1. Measured current exceeded 1pA
2. Decreased to the bg-level
3. Spikes ~1nA
5. Emissions > nA then exceeded 10nA
1. Measured current exceeded 1pA
2. Up to 6 pA
3. Decreased to the bg-level
4. Stayed at the bg-level

---
Summary: Emission stability
Spikes appeared and disappeared as if field emitters were growing and evaporating.
Still the tendency is that higher the E-field, higher the current.
Macroscopic emission current that follows Fowler-Nordheim might be an average of (unstable) local emissions.
The assumption above could be tested by statistical measurements and/or measurements with anodes of various sizes.

---
Gap determination
1. Find a target site by approaching the tip to the surface with the SEM stage tilted 30 degrees.
2. Take the target site surface images at 0 degree. Low magnification images are used for finding the position on the surface and high magnification images are for comparing surface condition before/after measurements. (the tip should be retracted in order to avoid shadows)
3. Set the tip on the measurement position. The stage is tilted 30 degrees and rotated to be in a plane perpendicular to the SEM detector.
4. Comparing with a reference image and a marked transparent sheet, the gap can be set in less than 10% accuracy.