## Slide 1: SC Quadrupole Magnets in ILC Cryomodules
Reported by Akira Yamamoto
CM Meeting, Feb. 28, 2012

## Slide 2: Concerns and Actions
Beam handling capacity after energy upgrade
  Change beam dynamics
Field instability in lowest energy (< 10 %) operation
  Provide a shorter magnet design with separation of dipole from quadrupole,
Stability of axis and Ramping property
  To be confirmd by condcution cooling test

## Slide 3: Requirements to SC Quad. And Dipole
Provided by K. Yokoya and K. Kubo
 | Nominal length | Nominal field (G.) | Static Field in max. | Ramping
Quad | ~ 0.6 m | 50 T/m | 30 T/m*m | 0.01 T/m*m/sec (0.03% /sec)
Dipole | ~ 0.6 m | 0.1 T | 0.05 T*m | 3E-4 Tm/sec (0.6 % /sec)
Model Magnet Design: 120 % to nominal design

## Slide 4: Quadrupole Specification & Superconductor
NbTi wire diameter, mm | 0.5
Number of filaments | 7242
Filament diameter, um | 3.7
Copper : Superconductor | 1.5
Insulated wire diameter, mm | 0.54
Insulation | Formvar
Twist pitch, mm | 25
RRR of copper matrix | 100
Critical current Ic @ 4.2K, at 5T | 204 A
Integrated gradient, T | 36
Aperture, mm | 78
Effective length, mm | 666
Peak gradient, T/m | 54
Peak current, A | 100
Field non-linearity at 5 mm radius, % | 0.05
Quadrupole strength adjustment for BBA, % | -20
Magnetic center stability at BBA, um | 5
Liquid Helium temperature, K | 2
Quantity required | 560

## Slide 5: A possibility: Combined Function
Main Quadrupole
  Positive: 1, 3,
  Negative: 2, 4,
Corrector Dipole
  Positive: 1, 4
  Negative: 2, 3

## Slide 6: Fermilab Model Magnet

## Slide 7: SC Quadrupole Design in TDR, Proposed
The SC quadrupole magnet design needs to satisfy very wide range of beam energy (i.e. magnetic field strength) including energy upgrade to 1 TeV
A standard magnet design:
  optimized to cover the energy range of approximately 10 to 100 % of 250 GeV operation, based on the requirements of a FoDo like lattice. The same magnets can be used to accommodate beam energies of 260-500 GeV for the TeV upgrade, using a FoFoDoDo lattice.
An additional magnet design:
  specifically in the lower energy operation below 10 % of the full magnetic field (< 25 GeV beam operation). The magnet field strength may be stronger and the length can be shorter, in order to minimize the associated field instability.
  It is prudent to separate the quadrupole magnet from dipole corrector magnet, placing them adjacent along the beam-line axis. The exact design and configuration of the SCRF magnets remains an important action item.
It is assumed, however, that
  all magnet package solutions will fit the single defined interface conditions in the cryomodule, thus avoiding the need for more than one cold-mass variant.

## Slide 8: SC Quadrupole in Cryomodule
Suspended by GRP

## Slide 9: Cryomodule Cross-Section
Quadrupole cold mass
Thermal leads to LHe supply pipe
LHe supply pipe
V. Kashikhin, FNAL Review, March 2, 2010

## Slide 10: From 500 to 1000 GeV
2.2 km
1.3 km
10.8 km
1.1 km
BDS
Main Linac
e+ src
bunch comp.
<26 km ?
(site length <52 km ?)
Main Linac
<Gcavity> = 31.5 MV/m
Geff ≈ 22.7 MV/m
(fill fact. = 0.72)
IP
central region
<10.8 km ?
Snowmass 2005 baseline recommendation for TeV upgrade:
Gcavity = 36 MV/m ⇒ 9.6 km
(VT ≥ 40 MV/m)
Based on use of low-loss or re-entrant cavity shapes
ultra-high gradient R&D >2012
N. Walker
Quad: FF-DD
Quad: FD-FD

## Slide 11: Quad Strength
Quad strength is defined by quad spacing, required phase advance (μ) and beam energy.
For flexibility quad should provide optics with phase advance μ=90° up to final energy E=250 GeV (~20%)
Extra strength will need for matching.
Lattice with quad spacing s = 38 m (9+8+9 cavities in RF unit)
Lquad (effective) = 0.626 m (in TESLA design)
Final choice for gradient:
Allow to tune up to μ=90° phase advance @ 250 GeV
Additional ~ 20% overhead for lattice matching
or

## Slide 12: Corrector strength
Maximum required strength of corrector is defined from the following assumptions:
Energy = 250 GeV; μ= 90º; (RDR: μx /μy = 75º/60º)
Quad offset: rms = 0.3 mm; (3  0.9 mm)
Max beam offset 3 mm at energy 250 GeV
(<10% of strength needs to deflect beam along the Earth curvature)
Max current: (at 250 GeV) = 40A
Stability: same as for quads.
Field change: by a few percent in 0.2 s, every 0.2 s
Change step: (equivalent ~1μm of quad center motion)
  2.e-6 T*m at 15 GeV; 3.e-5 T*m at 250 GeV

## Slide 13: Test Circuit

## Slide 14: Main Linac Type-4 Cryomodule
Quad and Correctors
BPM
SCRF
300 mm pipe
Central support
SCRF
TESLA TDR
ILC
Combined or stand alone correctors (Quad center stability issues) ?
Space available for Quad
Total package: ~1.3m, incl.
  BPM: ~170 mm
  Quad: ~ 660 mm
  correctors: 335 mm

## Slide 15: Number of SC quads (RDR and SB2009)
Main linac (15-250 GeV) | # CM | # Quad
Electron Linac* | 846 | 282
Positron Linac | 834 | 278
Overhead (3.5%) | 30+30 | 10+10
Total | 1680+60 | 560+20
Proposed changes in SB2009 lattice:
  Single stage compressor: 6 CM’s (quad in each)
  Post-acceleration 5  15 GeV is part of ML
  Total number of CM’s is reduced by 3, but # quads increases +1
* Incl. 12 CMs to recover 3.23 GeV energy losses in undulator
Note: each quad is combined with vertical corrector, every second quad has also horizontal corrector
RTML(5-15 GeV) | # CM | # Quad
e-/e+ Bunch compressor | 45 / 45 | 17/17
Total | 90 | 34

## Slide 16
J.Tompkins, PAC’07

## Slide 17: Quadrupole R&D Work at Fermilab
Fermilab: V. Kashikhin et al.,
  Test results of superconducting quadrupole model for linear colliders
  This conference, 4LPA01,
SLAC/CIEMAT: C. Adolphsen et al

## Slide 18: Quadrupole R&D Work at Fermilab
Fermilab: V. Kashikhin et al.,
  Test results of superconducting quadrupole model for linear colliders
  This conference, 4LPA01,