## Slide 1
Cavity status; recent KEK activities
2012.05.08: Hayano
(1) STF CM-1 cavities are;
MHI-014: 3-rd VT:36MV/m (finished)
MHI-015: 3-rd VT: 33.5 -> 18.4MV/m F.E. turn ON
MHI-016: 2-nd VT:34MV/m (finished)
MHI-017: 1-st VT: 38MV/m (finished)
MHI-018: 1-st VT: 31MV/m
MHI-019: 1-st VT: 26MV/m
MHI-020: 1-st VT: 9MV/m heavy field-emission
MHI-021: 1-st VT: 38.9MV/m (finished) MHI-022: waiting for 1-st VT in this week
(2) New bender/KEK cavities;
TOS-02(w/o HOM): 1-st VT: 31.2MV/m
HIT-02(with HOM): 1-st VT: 35.2MV/m
KEK-00(w/o HOM): 1-st VT: 26MV/m, 2-nd VT:29MV/m
KEK-01(with HOM): under fabrication
(3) other project cavities;
ERL-2cell cavity #2: 5-th VT: 50.4MV/m

## Slide 2
ERL 2-cell cavity #2 5-th VT
Detail report in the end of slides
March 6

## Slide 3
MHI-020 1-st VT
heavy field emission  input RF cable break happened!
March 15

## Slide 4
KEK-00(w/o HOM) 1-st VT
March 29
limited by input RF cable break-down
(at N-type J-J juction)

## Slide 5
KEK-00(w/o HOM) 2-nd VT
April 5
limited by cell#2 defects, other cells were over 40MV/m

## Slide 6
MHI-021 1-st VT
April 12

## Slide 7
HIT-02(with HOM) 1-st VT
April 26
It has many defects on several Iris and beam pipe, however, it went up 35MV/m.

## Slide 8: History and Recent result of cERL 2-cell cavity #2
K. Watanabe (KEK)
May/2012

## Slide 9: Log
Mar/2009: Fabrication cavity by MHI
July/2009: Bulk EP (5 + 100 um) and Annealing
Feb/2010: Light EP (20 um) and 1st VT
April/2010: Light EP (20 um)
and 2nd VT with HOM pick-up (Type 0 Normal)
July/2010: Light EP (20 um)
Aug/2010: 3rd VT with HOM pick-up (Type 0 Normal)
Sep/2010: Light EP (20 um)
Oct/2010: 4th VT with HOM pick-up (Type 0 Normal)
Feb/2012: Light EP (5um)
Mar/2012: 5th VT with HOM pick-up (Type 2)
1st VT: to check the cavity performance (quality check).
2nd ~ 5th VT: to study a performance of HOM coupler
and HOM pick-ups.
Measurement of sustainable field without
quench at HOM coupler at CW
The field was raised to a rf power limit
or heating limit of HOM pick-ups.
cERL injector 2-cell cavity #2 (Proto-type model)
(With two input coupler port and five loop-type HOM couplers)
Target Gradient is 15 MV/m at CW in Cryomodule.
* Cavity design by E. Kako
* HOM coupler and feed-through design by K. Watanabe
* Optical Inspection was done after each treatment.
Few defects found at Outside weld area.
These defects created by press work.
On the weld area, there are no welding defect.
* The LLRF measurement, HOM study, RF tuning, optical inspection, preparation part, assembly work and VT were done by K. Watanabe with few Technicians.
total EP removal =190µm

## Slide 10: Example: Optical Inspection result (After 1st VT)
Four pit type defect found at Outside weld area.
(defects created by press work)
On the EBW seam, there were no welding defect.

## Slide 11: Relation of defect size and heating detected by thermo-sensors
No heating at 50 MV/m

## Slide 12: Recent result of Vertical tests of #2 cavity: Qo-Eacc

## Slide 13: Cavity Parameters of 2-cell injector and 9-cell cavity
 | cERL 2-cell (KEK) | 9-cell TESLA-like
Frequency | 1300 MHz | 1300 MHz
R/Q | 204.0 | 1016
G | 287.8 | 277
Esp/Eacc | 2.25 | 2.17
Hsp/Eacc [Oe/MV/m] | 42.2 | 41.0
K (coupling) | 1.94 | 2.0
L (effec.) | 0.23 m/cavity | ---
Iris diameter. BP diameter. | 70 mm 88 mm | 70 mm 80 mm
Other | Hsp on Equator 50 MV/m→2110 Oe | Hsp on Equator 45 MV/m→1845 Oe
Calculated by E. Kako (by Superfish)

## Slide 14: Result of Vertical tests of #2 cavity: History and Summary
 | Max Eacc and Cause of limitation | Other
1st VT Mar/2010 | 40.9 MV/m without Quench. The test was stopped because a field exceeded 40MV/m. | Removed material = 125 um
2nd VT April/2010 | Vacuum leak happened during 2K high field measurement, then the test was stopped. No quench at 14 MV/m in Liq He………. Leak location was one ICT 70 flange (Low temperature side). | Removed material = 145 um With HOM pick-up (Type 0 Normal, gap = 0.5 mm)
3rd VT Aug/2010 | 38.6 MV/m with Quench at HOM pick-up. Sustainable field：12 MV/m outside liq. He 17.4 MV/m in liq. He Cause of limitation was a heating of HOM pick-up. | Removed material = 165 um With HOM pick-up (Type 0 Normal, gap = 0.5 mm)
4th VT Oct/2010 | 42.6 MV/m with Quench at HOM pick-up. Sustainable field：13 MV/m outside liq. He 18.4 MV/m in liq. He Cause of limitation was a heating of HOM pick-up. | Removed material = 185 um With HOM pick-up (Type 0 Normal, gap = 2.0 mm)
5th VT Mar/2012 | 50.4 MV/m without Quench and Field Emission (in lig. He). The test was stopped because a field exceeded 50MV/m. (RF power limit) Hsp on Equator is 2127 Oe. | Removed material = 190 um With HOM pick-up (Type 2, gap = 2.0 mm)

## Slide 15: Surface treatment
No. | Amount EP [um] Current density | 1st water rinsing | rinse | HPR [hour] | Other
Bulk EP | 5 + 100 | Idle: 5 min Case 1 | none | 2 | ---
Light EP 1st | 20 26-30 mA/cm2 | Idle: 20 min Case 2 | FM-20 and HOT Bath with Ultra-sonic (1 hour + 1 hour) | 2.5 + 2.5 (with Flange) | In coated Helicoflex 100 C Baking
Light EP 2nd | 20 24-30 mA/cm2 | Idle: 20 min Case 2 | FM-20 and HOT Bath with Ultra-sonic (1 hour + 1 hour) | 2.5 + 2.5 (with Flange) | In coated Helicoflex 100 C Baking
Light EP 3rd | 20 30-40 mA/cm2 | Idle: 20 min Case 2 | FM-20 with Ultra-sonic (2 hours) | 2.5 + 2.5 (with Flange) | In coated Helicoflex 100 C Baking
Light EP 4th | 20 30-40 mA/cm2 | Idle: 20 min Case 2 | FM-20 with Ultra-sonic (2 hours) | 2.5 + 2.5 (with Flange) | In coated Helicoflex 100 C Baking
Light EP 5th | 5 37-38 mA/cm2 | Idle: 30 min Case 3 | End Group cleaning by Brush. FM-20 with Ultra-sonic (30 min) End Group cleaning again by Brush. | 4 + 2 (with Flange) | Sn coated Helicoflex 120 C Baking
Process of 1st water rinsing
* Case 1: Water supply flow (4 min) -> Pump off (2 min) : Repeat this cycle (total 40 min)
* Case 2: Water supply flow (3 min) -> Pump off (1 min) : Repeat this cycle (total 90 min)
* Case 3: water fill-and-close (40 min), water supply flow 20min, and with cavity rotation 40min : total 100min

## Slide 16: Preparation of HOM pick-up (1): Surface Treatment and Cleaning Method
No. | Type | Treatment | Cleaning Method after CP
1st VT | Without |  | 
2nd VT | Type 0 | Feedthrough: only FM-20 with Ultra-sonic Niobium antenna: Chemical polishing (without mechanical polish) | FM-20 with Ultra-sonic ~ 10 min.
3rd VT | Type 0 | Feedthrough: only FM-20 with Ultra-sonic Niobium antenna: Chemical polishing (without mechanical polish) | FM-20 with Ultra-sonic ~ 10 min.
4th VT | Type 0 | Feedthrough: only FM-20 with Ultra-sonic Niobium antenna: Chemical polishing (without mechanical polish) | FM-20 with Ultra-sonic ~ 10 min.
5th VT | Type 2 | Remove a brazing material near Joint point between inner conductor and niobium antenna. Mechanical polishing on niobium antenna after fabrication (mirror finish). Chemical polishing on niobium part (Total: 5 min). | After CP, FM-20 with Ultra-sonic ~ 20 min. Washing by sponge with FM-20. Dry at Class 10.

## Slide 17: Preparation of HOM pick-up (2): Structure of HOM pick-ups
Type 0
Type 2: Improvement of cooling performance and surface conditions
Seal
Nb antenna
Feedthrough
Surface on Nb antenna Tip
“Turn off -> CP”
Not Smooth at antenna tip
In case of “Turn off -> Mechanical Polish -> CP”
Get Smooth surface on antenna tip
Male pin
Images: After Mechanical Polish
Go to CP process

## Slide 18: About 5th VT of #2 cavity

## Slide 19: Process level during 2K high field measurement (5th VT)
Pt (field)
Pref

## Slide 20: Frequency and Qext change during cooldown (5th VT)
Tuning of HOM couplers for accelerating mode was very well.
Resonant Frequency at Room temp (vacuum). is 1297.685 MHz.

## Slide 21: Lorentz force detuning (5th VT)

## Slide 22: Trend during 2K high field (5th VT)
A process happened at 50 MV/m, then X-ray level was degrease. (Final: 50 uSv/h at 50.4 MV/m)
During 2K High field test, the RF power was supplied always on.
Qext of HOM couplers were not changed (no quench observed at HOM pickups).

## Slide 23: Reference of world record of Hsp on Equator