## Slide 1
Cavity status; recent KEK activities
2012.12.11: Hayano
STF CM-1 cavities are;
MHI-014 36.6MV/m for CM-1 ILC cryomodule (3-rd VT)
MHI-015 35.7MV/m for CM-1 ILC cryomodule (4-th VT)
MHI-016 33.8MV/m for CM-1 ILC cryomodule (2-nd VT)
MHI-017 38.4MV/m for CM-1 ILC cryomodule (1-st VT)
MHI-018 36.2MV/m for CM-1 ILC cryomodule (4-th VT)
MHI-019 37.0MV/m for CM-1 ILC cryomodule (2-nd VT)
MHI-020 35.1MV/m for CM-1 ILC cryomodule (3-rd VT)
MHI-021 38.9MV/m for CM-1 ILC cryomodule (1-st VT)
MHI-022 35.8MV/m for CM-1 ILC cryomodule (2-nd VT)
The next 4 cavities for CM-2a are under fabrication.
(2) New bender/KEK cavities/R&D cavities;
TOS-02(w/o HOM): 1-st : 31.2MV/m, 2-nd :32.7MV/m, 3-rd :36MV/m
HIT-02(with HOM): 1-st : 35.2MV/m, 2-nd :40.9MV/m
KEK-00(w/o HOM): 1-st : 26MV/m, 2-nd :29MV/m, 3-rd :24MV/m
KEK-01(with HOM): under fabrication
MHI-C(with HOM): 1-st : 36.1MV/m
They all are under jacketing with HPV qualification.
New results
since last S0 meeting.

## Slide 3
Slide from TTC2012(JLab)