## Slide 1
Cavity status; recent KEK activities
2013.02.19: Hayano
STF CM-1 cavities are;
MHI-014 36.6MV/m for CM-1 ILC cryomodule (3-rd VT)
MHI-015 35.7MV/m for CM-1 ILC cryomodule (4-th VT)
MHI-016 33.8MV/m for CM-1 ILC cryomodule (2-nd VT)
MHI-017 38.4MV/m for CM-1 ILC cryomodule (1-st VT)
MHI-018 36.2MV/m for CM-1 ILC cryomodule (4-th VT)
MHI-019 37.0MV/m for CM-1 ILC cryomodule (2-nd VT)
MHI-020 35.1MV/m for CM-1 ILC cryomodule (3-rd VT)
MHI-021 38.9MV/m for CM-1 ILC cryomodule (1-st VT)
MHI-022 35.8MV/m for CM-1 ILC cryomodule (2-nd VT)
The next 4 cavities for CM-2a are under fabrication.
(2) New bender/KEK cavities/R&D cavities;
TOS-02(w/o HOM): 1-st : 31.2MV/m, 2-nd :32.7MV/m, 3-rd :36MV/m
HIT-02(with HOM): 1-st : 35.2MV/m, 2-nd :40.9MV/m, 3-rd : 32.7MV/m, 4-th : 32.3MV/m
5-th : 38.0MV/m
KEK-00(w/o HOM): 1-st : 26MV/m, 2-nd :29MV/m, 3-rd :24MV/m, 4-th : 22MV/m
KEK-01(with HOM): under fabrication
MHI-C(with HOM): 1-st : 36.1MV/m
They all were jacketed with HPV qualification and waiting for the CM-1 installation.
There are four vertical tests since the last S0 meeting. However there is no new cavity test.
The green figure results are the new test.

## Slide 2
No.1 Cryostat
(Mag Shield is insdie of cryostat: in LHe)
No.2 Cryostat (New)
(Mag Shield is inside of
vacuum insulation part)
Cryostat of STF-Vertical Test Stand

## Slide 3
4-th vertical test :
(add mag shield
inside of cryostat)
2-nd vertical test in the No.1 cryostat:
as a reference
New VT Cryostat (No.2 Cryostat)
commissioning
3-rd vertical test :
(mag shield in
cryostat vacuum layer)
no imrovement of Q ?!
Q slightly lower than No1 cryostat

## Slide 4
5-th vertical test : skip ultrasonic rinsing
radiation was factor 3 higher than before.
2-nd vertical test : as a reference
(radiation was not plotted,
but about one order lower than
5-th test)
Check ultra-sonic rinsing
is effective or not
-> was effective, but not sufficient.
with 2% FM-20 detergent

## Slide 5
Ultrasonic OFF
Ultrasonic ON
set-up of Ultrasonic sensor
Measurement of Ultrasonic amplitude (July 2008)
Ultra-sonic
piezo sensor

## Slide 6
no cavity: Y-direction
no cavity: X-direction
inside of cavity: Y-direction
inside of cavity: X-direction
Comparison of ultrasonic intensity with/without cavity (July 2008)
Intensity was about similer or half for inside of the cavity
depth from water surface
amplitude of sensor output [V]

## Slide 7
STF EP Facility
No.1 EP Bed
No.2 EP Bed
modified to fit ILC cavity
No.2 EP stand is now utilized for ILC cavities
flow test using water
No.2 EP Bed
for 500MHz cavity

## Slide 8
Collaboration with Beijing University
EP process & vertical test for PKU04 (large grain cavity) on a way
vertical test is scheduled on the next week(Feb. 28).

## Slide 9
End of Slide