## Slide 1: FNAL ILC Status
Cavities
  IHEP-Beijing tumbling/test collaboration
    One 1-cell LL LG cavity
    One 9-cell LL LG cavity
    Jiyuan Zhai and Tongxian Zhao will arrive Mon.Feb.25 for ~2 months
  Daresbury vendor qualification collaboration
    One 1-cell cavity inspected, processed (standard EP) and tested – 25.5 MV/m (met Daresbury/Shakespeare spec)
    Tumble and re-test
CM2 re-build complete. Ti bellows on 2-phase pipe leaked at weld joint; leak finally became repeatable. CM2 to complete leak check then transport to NML within a few weeks
  Considering new QC for Ti bellows