## Slide 1: JLab Update
Rongli Geng
April 16, 2013
1st LCC ILC Cavity Group Meeting

## Slide 2: JLab Status: 9-cell Cavities
New 9-cell Low-Surface-Field shape (SLAC design) cavity.
  All niobium cups re-stamped, heat treated in vacuum furnace for stress relief, weld prep machining completed, CMM inspection completed
  Half cell frequency measurement fixture and stiffening machining fixture completed.
  Work will stop after half cell frequency measurements due to budget.
Two large-grain ICHIRO shape cavities processing an testing re-started (JLAB SRF facilities including EP processing, HPR, clean room assembly and VTA testing are back to business)
9-cell cavity NR1 (first “mirror finish” 9-cell polished using JLab in-house mechanical polishing machine) processing and testing stopped due to budget.

## Slide 3: JLab Status: Field Emission and High Q0 at 45 MV/m
X-ray mapping with 9-cell cavity (RI23) new test with additional diode rings completed on April 12, 2013
  New data increased confidence of previous prediction.
  The cavity is warming up now.
  Optical inspection at predicted location of field emitter to be carried out.
Two single-cell large-grain niobium cavities under processing and testing for high Q0 at ultra high gradient regime of > 45 MV/m
  Cavity PJ1-1
    In collaboration with Peking University, Ningxia Large grain material
    Baseline test after BCP etching only 28 MV/m, quench limit
    Second test is next week after more BCP etching
  Cavity G2
    Mirror finish mechanical polishing completed at JLab
    Light EP completed at FNAL
    First RF test in two weeks

## Slide 4: JLab Status: R&D on inexpensive SRF cavity
Seamless cavity
  A 2-cell niobium cavity made by MHI is being processed and tested.
  The cavity has a seamless dumbbell.
  First pass processing using BCP has been completed.
  Extensive optical inspection has been completed at various stages.
  First cold test completed.
Coated cavity
  The 1-cell cooper cavity LSF1-1 (which has mirror finish due to CBP) has been coated with a layer of niobium (1 micron thickness) at AASC.
  First RF test completed following HPR at reduced pressure (200 PSI).
  Low field Q0 in the range of 1E8-1E9.
  Second HPR at standard pressure (1200 PSI) – no film dislodging by visual.
  Cavity is now under vacuum and awaiting cryogenic RF testing.