## Slide 1: FNAL ILC Cavity Status
Camille M. Ginsburg (FNAL)
Jiyuan Zhai (IHEP)
LCC ILC SRF Cavity Group 1st Meeting
16.Apr.2013

## Slide 2: IHEP-02 Cavity
IHEP-02 is a low-loss shape large grain 9-cell cavity with full end groups for ILC R&D
FNAL and IHEP are collaborating to process and test the cavity using FNAL facilities and expertise. Two IHEP staff members (Jiyuan Zhai and Tongxian Zhao) are participating in the work.
The cavity will be dressed and installed in the IHEP ILC Test Cryomodule (containing only one cavity) late this year. The input coupler (two couplers test in KEK last month, reached ILC spec.: 1MW, 1.5ms, 5Hz), tuner and cryomodule are all ready to assemble.

## Slide 3: Process Procedures at FNAL
March – April
Tumbling 200 μm (to mirror surface)
EP 40 μm
Heat treatment 800C 3hr
Pre-tuning
EP 20 μm
HPR
Assembly
Bake
Vertical test scheduled in May