## Slide 1: Full-ceramic InGrids
Yevgen Bilevych
27.01.2014 Bonn

## Slide 2
Detached Ceramic Grid (top view)

## Slide 3
Detached Ceramic Grid (backside view)

## Slide 5
Ceramic grid
Grid cross-section
Metal grid top view

## Slide 6
Ceramic grid short process-flow
Dry etching of silicon
Silicon oxide deposition
Wafer bonding
Wafer grinding
Bottom Grid protection layer
Metal electrode formation
Top protection layer deposition
Ceramic layers patterning
Ceramic Grid releasing

## Slide 7
85-140 mm
200-360 mm
15-20 mm
110 mm
1 mm Si oxidized to 2,17 mm

## Slide 12
?????
Alignment marks – 2 times
Dicing or cracking
2 layers of SixNy or only top-layer
Thickness of SiO2
Thickness of metal layer
Thermal stability of bonding material
Possibility of bonding to chip or to wafer afterwards