## Slide 1: Progress in CMOS post-processing
Jurriaan Schmitz
Pixel Meeting Bonn, 27 January 2014

## Slide 2: Twente in the news: Squeezing transistors really hard generates energy savings
News item early December
Transistor modeling work
Ray Hueting & Tom van Hemert

## Slide 3: CONTENTS
Wafer post-processing: results from my group
Recent achievements
  SiON waveguide material
  Sub-nanometer TiN by atomic layer deposition
Ideas for InGrid / GridPix

## Slide 4: CMOS wafer post-processing
a. Chip manufacturing
b. Dicing and packaging

## Slide 5: Adding new process steps “Above-IC”
b. post-processing
a. Chip manufacturing
c. Dicing and packaging
“pizza” technology

## Slide 6: Solar cells on a CMOS chip
J. Lu et al., IEDM, December 2010
CIGS solar cell
CMOS

## Slide 7: An electrical surface plasmon polariton source on CMOS
Cross section:
SEM top view:
R. J. Walters et al., Nature Materials vol. 9 (Jan. 2010) pp. 21-25.
Notes: 7
Nucleation of islands depends on: deposition materiel, used precursors, temperature and type of substrate (termination).

## Slide 8: Optics on top of CMOS
B. Rangarajan et al., Optics Letters 38 (6) 941 (2013).
B. Rangarajan et al., J. Solid State Sci. Technol. 1, P263 (2012).

## Slide 9: RF MEMS components on top of CMOS
Ayazi et al.
Nguyen et al.
Nguyen et al.
S.N.R. Kazmi et al., IFCS 2012; JSST 2012; Micr. Eng. 2013

## Slide 10: TiN – thinner and thinner

## Slide 11: Atomic layer deposition explained

## Slide 12: Home-built Atomic Layer Deposition system

## Slide 13: New: commercial ALD system

## Slide 14: Resistivity skyrockets – quantum effects

## Slide 15: Going subnanometer: field effect in a metal!
Hao Van Bui et al., Applied Physics Letters 2013

## Slide 16: Prospects at the University of Twente
Atomic Layer Deposition:
“perfect” bi-atomary compounds (Al2O3, TiN, HfO2, ...)
Any use for InGrid/GridPix?
Insulator coating
Outgassing prevention
Reduce photon feedback?
Working on improvement of single-chip processing for TimePix3