## Slide 1: Vertical Electro-Polishing at CEA Saclay: update January 22th 2014
S. Berry, P. Carbonnier, J-P. Charrier, F. Eozénou, L. Maurice, F. Peauger, D. Roudier, C. Servouin

## Slide 2
Last Results on 1Cell
Nice Q0 after VEP on 1AC1 cavity
Chart: Eacc (MV/m)
| 1.6204000000000001 | 1.1196999999999999 | 0.79269999999999996 | 0.48320000000000002 | 2.4245000000000001 | 3.109 | 3.8424999999999998 | 4.8990999999999998 | 6.2031999999999998 | 8.0097000000000005 | 10.002700000000001 | 12.4628 | 13.680999999999999 | 15.139699999999999 | 16.4861 | 18.035 | 19.414100000000001 | 19.6389 | 20.659400000000002 | 20.493500000000001 | 21.164899999999999 | 22.678599999999999 | 22.835799999999999 | 23.421600000000002 | 23.884599999999999 | 24.440899999999999 | 24.695499999999999 | 25.299800000000001 | 24.981400000000001 | 24.440899999999999 | 23.073699999999999 | 22.419 | 21.732900000000001 | 21.043500000000002 | 20.375900000000001 | 19.866299999999999 | 18.9285 | 17.223299999999998 | 14.7271 | 12.1092 | 9.9109999999999996 | 7.9454000000000002 | 6.2103999999999999 | 4.7272999999999996 | 3.8692000000000002 | 2.8224 | 1.8819999999999999
Bulk BCP | 56846373195.9335 | 52614586398.0147 | 49903682509.4278 | 46573431760.2869 | 64681897206.0963 | 66560549270.4159 | 70753386139.2694 | 72603249414.2509 | 73983266044.278 | 76026468622.9416 | 74855170264.1731 | 73653102380.8 | 71305929135.5211 | 66132438876.1665 | 62419324708.9711 | 57929210080.558 | 51799253973.5017 | 39467974283.1493 | 34865272776.1998 | 27044570560.0169 | 24649149302.0982 | 22236790394.1244 | 18506162977.4967 | 15816588385.0976 | 13931830656.1304 | 12187405406.0831 | 10515288320.8437 | 8208058102.0094 | 8124753251.3709 | 8743374193.6488 | 11213278012.1567 | 12771797056.1243 | 14254922796.4476 | 16235991243.3682 | 18503192186.7374 | 21344109880.3871 | 29066453800.7063 | 38623944997.5037 | 46723759974.3196 | 51767964626.55 | 54249883557.2598 | 54234907245.2557 | 56922138531.8682 | 53619666252.0689 | 53263585727.224 | 49863211255.8552 | 47872972853.6026
+120 µm VEP + flash BCP No Baking | 96942050013.7846 | 83112354996.7863 | 69920472764.3836 | 102758751353.379 | 104958982325.947 | 105433689800.754 | 104436605495.44 | 101071374141.974 | 93529585780.7814 | 86248295895.4727 | 79538329076.0058 | 71144583151.3376 | 62205422357.5695 | 51468797167.85 | 41876198617.8173 | 32917356711.4457 | 26623918460.6981 | 21247702636.6089 | 17690544257.1607 | 14045904690.7874 | 11391632721.8987 | 9339344391.3222 | 6605298864.3792 | 4878991970.1702 | 3718075195.5099 | 2843468393.8987 | 2220389283.6628 | 1776646229.6706 | 1615553859.3499 | 5764715829.4796 | 7971644834.6477 | 11388720692.6761 | 17321235627.9618 | 26261745400.3116 | 39490227593.4351 | 54224445657.0079 | 59865482317.0216 | 65507093020.5465 | 69662346224.5977 | 72497666048.6707 | 75128185302.587 | 77484300003.8096 | 81025913299.4432 | 82799127603.8621 | 83953057744.8725 | 83273227530.8994 | 79748588345.3625 | 72644051920.2955 | 65398620637.4759
1AC1 1C cavity 1.3 – 1.7K
1AC1 baked at 115°C Test Week#4
1AC2 baked at 115°C after VEP Test Week#5
1AC3 (Quench at 35MV/m): Replica of the inner surface of the cavity
  Morphology depends on location in the cell
  Outlook: Quench area morphology & Ra at different locations
1AC1 baking at 115°C

## Slide 3
STUDY OF VEP MECHANISM (Flows in cavity)
Set-up to investigate inner surface of the cavity during VEP:
1.3 GHz 1C cavity cut and embedded in resin
Goal: investigate the effect of the acid flow, viscous layer during VEP
Explanation for asymmetry?
First test with acid (Ø30mm rod cathode):
Hydrogen bubbles flow alongside the cathode
Air bubbles might be trapped at the cavity surface if the acid flow is too high during filling

## Slide 4
VEP with 5Cell 704MHz Cavity with parameters derived from 1300MHz optimization:
Low voltage, high acid flow, large rod cathode
Pb during 1st seq: low hydrogen removal because of obstructed exhaust pipe : uncrontrolled EP and high removal at upper cell,
4 sequences with turning of the cavity in between
Exhaust problem discovered (acid condensation) and solved
200 µm average removal
Resulting removal ratio equator/iris ~ 1/2
No thickness
measurement in
this area
Removal (mm) along the cavity after 200µm VEP

## Slide 5
Field flatness of SPL after each VEP sequence
Field flatness modified after uncrontrolled VEP
Once the problem solved, no field flatness modification