## Slide 1: JLab Update
Rongli Geng
April 30, 2014
4th LCC ILC Cavity Group Meeting

## Slide 2: High Gradient SRF Themes
Understand and reduce field emission
  Cavity vertical testing at Epk 100 MV/m
  Gradient and Q0 degradation due to field emission from vertical testing to operation in cryomoudle
    CEBAF upgrade cavity experiences
Improve efficiency at high and very high gradient
  New shape – higher R/Q and lower Hpk/Eacc
  Large-grain material
  Frozen-in flux (and response to thermal cycling)

## Slide 3: JLab Status: Field Emission Instrumentation
Installation X-ray sensors (Hamamatsu S1223-01) at all cavities in full FEL cryomodule
  Compare field emission data at VTA testing with cryomodule testing
  Establish correlation between FE induced X-ray and FE induced Q0 loss and dark current at end of cryomodule
  Cryomoudle in test cave. Test to be started soon.
F100 cryomodule cavity string
being assembled and to be tested
One X-ray sensor for each cavity
near beam tube flange

## Slide 4: JLab Status: High Q0 at 45 MV/m
Two single-cell large-grain niobium cavities under processing and testing for high Q0 at ultra high gradient regime of > 45 MV/m
  New LSF shape 1-cell large-grain cavities (Two each)
    In collaboration with Peking University, Ningxia Large grain material.
    Processing procedure: BCP + 800CX2hr + BCP + 120C bake.
    Test data later slide.
One new single-cell large-grain niobium cavity under processing and testing
  Cavity PJ1-2
    In collaboration with Peking University and OTIC, Ningxia large-grain Nb material and fabrication.
    CEBAF upgrade cavity Low-loss shape, 1.5 GHz.
    Processing procedure: BCP60um+800Cx2hr+BCP60um+HPR+120Cx48hr.
    Max. Eacc 34 MV/m with Q0=1.6E10 at 2K, limited by quench, no FE.
    Max. Eacc 34 MV/m with Q0=2.5E10 at 1.8K, limited by quench, no FE.
    Next is EP and re-test.
    Test data later slide.

## Slide 5
Max. Eacc=38 MV/m with Q0=2E10, no X-ray, quench limit
LSF1-2 Cold Test Result