## Slide 1: Ideas for LC mechanics
(we will work on sensors as well – particular CMOS)

## Slide 2: Current Oxford activities on composite structures
Oxford is contributing to the R&D for the ATLAS strip tracker upgrade
We are involved in the development of the local supports: barrel strip staves
  UHM CF/honeycomb structures with carbon foam (Allcomp) cooling channels with embedded thin-wall Ti tubes
  Kapton/Cu flex circuits co-cured with CF skins
And the design of the global CF support structure for the barrel strip system
Cu/Kapton tape co-cured with K13C2U

## Slide 3: Our vision for future large trackers
Future sensor technologies (thinned down MAPS) promise material down to a few ‰ of a radiation length
  Structures and services need to match this
We do have a strong preference for liquid (evaporative) cooling
  Gas cooling is not a robust technology (difficult to predict)
  Gas cooling has limited capacity (might be ok for linear collider, but not much more)
  For comparison: ATLAS phase II >2.5% X0, LC TDR ~1% X0
  Support/service sandwich layer:
    Structural: UHM fibre (e.g. K13C2U, 4 layers of 45gsm)
    Cooling: Microchannel Kapton cooling
    Electrical services: Al/Kapton multilayer cables
    All the above are co-cured (this saves glue)
  Sensors: Thinned down to 50µm (MAPS)
  This would be a layer less than 1mm thick
3
Of course, we have ignored a few things,
but we think 0.5% is a conceivable aspiration…
Kapton microchannels
UHM CF
0°
90°
0°
90°
UHM CF
Al/Kapton tape
Sensor
→ Challenge: Is 0.5% X0/tracking layer with evaporative cooling possible for a large ((2-3m)3) tracker?

## Slide 4: Kapton microchannel cooling
Developed for ALICE by CERN:
Tested to 10bara with water and C6F14 monophase cooling
Requires scaling to large tracker size, can we achieve higher pressures
At Oxford we have started to look into similar photo-etched and machined structures…
4
G. Fiorenza et al., 5th IEEE International Workshop on Advances in Sensors and Interfaces (IWASI), 2013, p. 81-85, 10.1109/IWASI.2013.6576065.

## Slide 5: First attempts
Prototypes of 40×100mm2
Machined (milled with a tool at 45°)
Photo-etched as ALICE
  One prototype has achieved 10bara (two channels delaminated at 5bara, but ultimate failure at 10bara)
Next step is to co-cure a sample with CF

## Slide 6: How can we achieve stiffness?
The key is design for large moment of inertia (together with high modulus)
  Ladders are poor
  Large cylinders are better
    But: hoop stiffness is now the challenge
    Also: integration of large cylinders has many disadvantages
      Large, valuable objects – difficult to move/transport
      Technologies get challenged late in the integration
Can one make smaller units which are clever structurally?
  Yes, exploit the mouldability of CF (and Kapton-based service elements)!
  Examples exist for vertex/pixel systems, need to scale by 10 in size
And, with 50μm sensors, the structures do not need to be flat…
6
BNL, doi:10.1016/j.nima.2013.07.005
STAR, doi:10.1016/j.nima.2010.12.006
ALICE, doi:10.1016/j.nima.2006.04.093

## Slide 7: How could this look like?
This geometry is for ATLAS upgrade dimensions, but you get the picture
Inner:
3:2
Outer:
4:3