## Slide 1: Future of SRF technology
in the context of LC’s & FCC…
SRF

## Slide 2: Outline of Talk
A BIT OF SRF HISTORY
Current “state of the art” vs ILC needs
Potential for higher gradients for ILC/ILC-upgrade
Cost reduction avenues for ILC and Upgrade
FCC (Future Circular Collider)-
  How to meet the RF needs
  New Developments underway
Conclusion
  Global impact of SRF

## Slide 3: Successes of SRF R&D At the Gradient Frontier
Scientific understanding of performance limiting mechanisms => development of cures

## Slide 4: Performance limitations overcome
3
6
10
25
40
MV/m

## Slide 5: Successes of SRF R&D At the Gradient Frontier
  Multipacting…limited gradient to 3 MV/m (at 1.3 GHz)
  Thermal breakdown of superconductivity…6 MV/m
  Field emission limits 10 – 20 MV/m
  Q disease due to H intake – Q falls at low field
  Q-drop at high fields – 25 MV/m
Major applications at each stage of progress
Now 1.3 GHz 9-cell ILC cavities reach 30 – 40 MV/m
CM gradients reach 30 - 31.5 MV/m

## Slide 6: As Gradients reach 6 – 8 MV/m Applications to
Nuclear Physics
  Ions (total > 1 GeV installed voltage)
    Low Energy Nuclear Physics, Nuclear Astrophysics
      ATLAS, ISAC, ALPI….
  Electrons
    CEBAF (>1 GeV installed)
High Energy Physics- Energy and Luminosity Frontiers
  Electrons (total 12 GeV installed voltage)
    TRISTAN, HERA, LEP-II, CESR, KEK-B, BEPC
  Protons
    LHC
Light Sources
  Electron Storage Rings
    CESR, DIAMOND, CANADIAN-LS, TAIWAN-LS, ESRF, SOLEIL, POHANG
  Free Electron Lasers (FELs)
    JLAB-FEL, JAERI

## Slide 7: As Gradients rise to 10 – 20 MV/m
FEL Light Source
  FLASH at DESY > 1 GeV
  15 – 20 MV/m
Neutron Source
  SNS at Oak Ridge 1 GeV Protons
  15 MV/m
Accelerator Applications of SRF: 7 GeV Installed (500 cavities)

## Slide 8: > 2010: Dawn of a New Age: Major Accelerators Under Construction
CEBAF Upgrade - JLAB (80 cavities)
  Upgrade 6.5 GeV => 12 GeV electrons
XFEL – Hamburg (840 cavities)
  18 GeV electrons – for Xray Free Electron Laser – Pulsed)
LCLS-II – SLAC (300 cavities)
  4 GeV electrons –CW XFEL (Xray Free Electron Laser)
SPIRAL-II – France (28 cavities)
  30 MeV, 5 mA protons -> Heavy Ions
FRIB – MSU (340 cavities)
  500 kW, heavy ion beams for nuclear astrophysics
ESS – Sweden (150 cavities)
  1 – 2 GeV, 5 MW Neutron Source ESS - pulsed
PIP-II – Fermilab – 800 MV (115 cavities)
  High Intensity Proton Linac for Neutrino Beams
ADS (200 cavities)
  China, India
Total ≈ 2000 Nb Cavities,
Installed Voltage will rise from 7 GeV => 25 GeV

## Slide 9: XFEL Largest SRF Application - Model for Future ILC
ILC
16, 000 Nb cavities
1855 Cryomodules
Eu-XFEL
840 Nb cavities
103 Cryomodules

## Slide 10: XFEL: Mass Production of Cavities Need 840

## Slide 11: Cavity Testing at DESY – Hamburg, Germany

## Slide 12: Preparation for test

## Slide 13: Q vs E, Typical Vertical Test Results

## Slide 14: Gradient Yield after First Treatment (as of Sept 2015)
738 cavities
  from two vendors, RI and EZ
EZ vendor used Bulk EP and Final BCP
RI vendor use Bulk EP & Final EP (as for ILC)
Final EP gives 3 – 4 MV/m higher performance
Lesson for highest gradients
  Don’t use BCP
 | Max | Grad | ient | Usable | Grad | ient |  | 
 | RI | EZ | C | RI | EZ | C |  | 
<G>MV/m | 33 | 29.6 | 31.4 | 29.4 | 26.3 | 27.7 |  | 
28MV/m | 86% | 73% | 79% | 66% | 44% | 54% |  | 
Yield at |  |  |  |  |  |  |  | 
< 10%
>30%

## Slide 15: CEBAF 12 GeV Upgrade > 80 cavities: overall performance
72/85 @ admin limit (85%)
Cavities made by RI (Germany);
Reported 11.2012 by F. Pilat
Note: Jlab used bulk BCP (150 µm) followed by Light EP (30 µm)

## Slide 16: Definition of Max and Usable Gradients
For this cavity
Max gradient is 30 MV/m
Usable gradient is 25.5 MV/m limited by bottom x-rays
R&D Needed on Medium Field Q-Slope

## Slide 17: 2nd Treatment Increases Yield
18% of cavities with G < 20 MV/m re-treated
Mostly by HPR
Average gradient increased
From 14.3 to 25.8 MV/m
Re-treatment was not applied to higher gradient cavities
  time/cost pressures

## Slide 18: Effect Of Re-treatment On “High Gradient Cavities” – Special Batch
12 cavities each from RI and EZ for High Gradient R&D
Ave Max gradient for RI cavities rises by about 3 MV/m after re-treatment
Ave Max 35.5 ± 4.7 MV/m
Average yield at 28 MV/m rises by 10%

## Slide 19: Compare XFEL to ILC need
We can anticipate (optimistically)
Ave Max Gradient will rise to from 33 to 36 MV/m on 2nd treatment
  More than 25% re-treatments may be required for ILC
But yield of usable gradient needs to be improved
  We need 90% yield for gradient > 28 MV/m with average of 35 MV/m
Substantial gain possible if Medium Field Q-slope is overcome
  > 50% cavities fall below Q 1010
  Q0 for ILC can be 8x10^9 which increases yield some
Fix medium Field Q-slope
  Proper doping? to be invented?
Next addressable limit is field emission
  limits about 20% of cavities
XFEL results are tantalizingly close to ILC needs!

## Slide 20: How to Counteract Field Emission ?
  Accidental dirt contamination during assembly drops Q due to Field Emission (FE)
  Apply high pulsed power conditioning to lower X-rays and raise field
  Should work for cavities stuck by field emission at lower gradients

## Slide 22: Continued Progress to Target ILC Cavity Gradient Yield R&D
(94+/-6)% acceptable for ILC mass production

## Slide 23: XFEL: 103 Cryomodules
XFEL goal for CM
  23 MV/m
ILC goal 31.5 MV/m
Average gradient of 60 XFEL CM now is 27.4 MV/m
  37% limited by BD
  22% by x-rays (FE)
  41% by power available for test
Several best CM reach/exceed ILC goal

## Slide 24: Average gradient of 60 CM is 27.4 MV/m
Ave CM gradients need to improve!
But best CMs reach ILC goal

## Slide 25
ILC

## Slide 26
ILC

## Slide 27: 8-cavity Cryomodule at Fermilab:

## Slide 29: Q Values in CM at Fermilab

## Slide 30: KEK Cavity RF performance in CM1/CM2a
Module | CM1 |  |  |  |  |  |  |  | CM2a |  |  | 
Cavity # | 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10 | 11 | 12
Cavity name | MHI-14 | MHI-15 | MHI-17 | MHI-18 | MHI-19 | MHI-20 | MHI-21 | MHI-22 | MHI-24 | MHI-23 | MHI-25 | MHI-26
Eacc @V.T. [MV/m] | 36.6 (power limit) | 35.7 (Cell#1 Quench) | 38.4 (power limit) | 36.2 (power limit) | 37.2 (Cell#1 Quench) | 35.1 (power limit) | 38.9 (power limit) | 35.8 (power limit) | 12.0 (heavy F.E.) | 35.9 (Cell#3 Quench) | 32.3 (Cell#1 Quench) | 31.6 (Cell#1 Quench)
Eacc @C.T. (short pulse) [MV/m] | >38.6 (test stop) | 36.8 (Quench) | 35.2 (Quench) |  |  |  |  |  |  |  |  | 
Eacc @C.T. (full pulse) [MV/m] | >38.7 (test stop) | 36.7 (Quench) | 35.3 (Quench) |  |  |  |  |  |  |  |  | 
36MV/m
(last week)
Single cavity power test, now under progress
Room-Temperature Coupler Process : July – September 2015
Cavity Process at 2K : October – November 2015

## Slide 31: Future R&D Areas for ILC and TeV Upgrade
Raise gradients
  Nb cavities of improved shape
  New materials, in particular Nb3Sn
Raise Q
  Improve understanding of Q-drops
  Explore Nitrogen (or other) doping
  Reduce field emission
Lower costs
  Reduce Nb material cost
    Explore Nb-Cu composite
    Large grain Nb
  Reduce cavity fabrication cost
    Hydroforming and Spinning

## Slide 33: Impact of Increasing Gradient and Q on ILC cost
ILC requirements:
G > 35 MV/m/ Q0 > 0.8e10
Improving Q0 from 8e9 to 3e10 has big impact on machine cost.
Optimal gradient moves to
~ (70 - 80) MV/m

## Slide 34: Quest for Higher Gradients
Best gradient in TESLA shape 9-cell cavity is 45 MV/m
Limited by
  surface magnetic field (Hpk) = fundamental rf critical field
=> Improve cavity shapes to reduce Hpk/Eacc
So that critical magnetic field is not a brick wall

## Slide 35: Highest Gradient TESLA Shape cavity, 45 MV/m
D. Reschke et al., SRF2011, THPO046 (2011).
Eacc

## Slide 36: Max surface surface magnetic field reached with TESLA-shape cavities is close to “theoretical limit” Fundamental RF Critical Field (Hsuperheating) Measurement
45 MV/m in best cavity
=> Improve Cavity Shape

## Slide 37: Better Cavity Shapes to Beat the Limit: Lower Hpk even if you have to raise Epk
Eacc = 2000/35.4 = 56 MV/m

## Slide 38: Proof of principle with single cells, 52 MV/m

## Slide 39: Multi-Cell Cavities with Advanced Shapes Developed
But Limited by Field Emission to ~40 MV/m

## Slide 41: Best With Low-Loss shape : 42 MV/m
Field Emission is the problem to solve!

## Slide 42: Higher Gradient with New Materials? Best candidate Nb3Sn
Nb3Sn, Tc = 18K
Higher Q at higher operating T
Higher ultimate field possible?

## Slide 43: A15 Compounds – Nb3Sn
Q vs. Epeak of the 1st two Nb3Sn-coated 1.5GHZ single cell cavities in comparison to pure Nb at 4.2K and 2K from CEBAF
Wuppertal, end ’1980s :
Nb3Sn cavity (1.5 GHz) obtained trough Sn vapour phase diffusion @ 1200˚C

## Slide 44: Nb3Sn Fabrication/Cornell

## Slide 45: Nb3Sn Coating by vapor diffusion
R&D Nb3Sn cavity achieves Eacc and cryogenic efficiency specification of state of the art high Q0 projects!
Still work to be done for high field applications
S. Posen, M. Liepe, and D. L. Hall, Appl. Phys. Lett. 106, 082601 (2015), C. Becker et al., Appl. Phys. Lett. 106, 082602 (2015).
Nb3Sn vs Nb
Nb
Nb3Sn
SEM of Surface
TEM Cross Section

## Slide 46: Expectations for Nb3Sn
Using high power RF (MW) with short pulses, Cornell recently demonstrated (for T>6K)
Nb3Sn follows the expected superheating field of the 18K superconductor.
When extrapolated to 2K this leads to surface magnetic fields of 300 mT
  Nb superheating field 200 mT.
These results suggest that a well prepared Nb3Sn cavity with optimal shape can reach 80-90 MV/m
And high Q (due to higher Tc of Nb3Sn)
With intense R&D, Nb3Sn can outperform Nb.
Superheaing field
Heating at defect/or second phase behavior takes over

## Slide 47: Active Nb3Sn Programs
Fermilab
Jefferson Lab
Cornell

## Slide 48: Recent Breakthroughs in High Q (without FE)
1. Reverse the falling Q-slope!
N doping exceeds familiar Q values!
  But still demands deep physical understanding.
    What is missing in simple BCS calculation for Q?
2. Reduce residual losses by completely expelling dc magnetic flux
  leads to even higher Q values.
R&D in fundamental understanding of both phenomena will reveal
  What are the ultimate limits to the best Q?
  Best parameters to optimize the preparation and cool-down protocol for highest Qs?

## Slide 49: What is N doping? infuse the cavity surface at 800 C with a small concentration of nitrogen (about 50 ppm)
Injection of small nitrogen partial pressure at the end of 800C degassing-> drastic increase in Q

## Slide 50: High Q values obtained by N-Doping doping repeatedly on 9-cell ILC Cavities for LCLS-II
Pre-doping state of the art
Standard treatment Q

## Slide 51: High Q to 30 MV/m (650 MHz)

## Slide 52: High Q Opens Cost Reduction Possibilities: 1.3 => 2.6 GHz
Cons
Larger wakefields
More HOM power
1.3 GHz was originally chosen to avoid the global thermal instability ,(GTI) due to BCS resistance (increases as f2)
Pros for higher frequency
  Material cost savings for cavity and CM parts
  Optimistically 75%
Smaller surface area
  Less defects/field emission
If N-doping can reduce BCS resistance by factor of 3
Global thermal instability due to BCS surface resistance can be managed
GTI ~ 37.5 MV/m
Q = 1/3 BCS
2.6 GHz
Surface Temp
Bsurface
1.3 GHz
GTI > 45 MV/m
GTI ~ 33 MV/m
Q = 1/2 BCS

## Slide 53: Cavity Material-Cost Reduction
Chart: >1000 Cavity Production Cost 1.3 GHz Cavities
| Niobium/NbTi/Ti | Fabrication | Processing | Dressing
 | 0.62939 | 0.17252 | 0.15335 | 0.044728
Nb cost dominates for large scale production
=> Cut Nb cost
Cost of bulk niobium is a major factor
  especially for low frequency (<650 MHz)
  the required Nb per cell scales as 1/f2.

## Slide 54: 1 m2 Nb-Cu Sheet Explosion Bonded
Propose cost reduction -1
  Via Nb-Cu Composites
    Nb 1 mm/Cu 4 mm,
    Material made by explosion bonding Cu with high RRR Nb
    X4 - 5 reduction over Nb
  Cavities made via hydroforming and spinning

## Slide 55: Cavity Fabrication Cost Reduction via Seamless Techniques with Nb-Cu Composites
Eliminate expensive e-beam welding and trim machining of parts
High quality surface preparation possible
  as with bulk Nb cavities that show high performance
Rapid production rate
Hydroformed and Spun 1-cell cavities already proven
  Hydroformed 3-cells Nb proved to > 35 MV/m
  Spun single cell Nb proved to 40 MV/m

## Slide 56: Principles of Hydroforming and Spinning

## Slide 57: Start With Nb Tubes By Flow Forming

## Slide 58: Necking and Hydroforming from Tube

## Slide 59: Proof of Principle 1-cell Nb-Cu Composite Hydroformed Reaches 40 MV/m

## Slide 60: Hydroformed 3-cell Welded into 9-cells 30 – 35 MV/m Proved

## Slide 61
9-cell Nb Cavity Made by Spinning

## Slide 62: 3-cell cavity made from Nb tube by spinning at INFN
T=2K
Test at FNAL
Eacc 34 MV/m

## Slide 63: 500 MHz Cavity via spinning Nb-Cu Composite Cornell/INFN –Legnaro – in progress

## Slide 64: Path 2: Simplify Nb Sheet Production Cost Analysis of Nb Production
50% of the cost is in the e-beam melting
20% cost is in rolling, forging and scrap

## Slide 65: Propose Cost Reduction Path 2
  Via Nb from ingot
    15% reduction possible?
  Go Directly from Ingot to Sheet?
    Large grain Nb
    Performance benefits
    Fewer defects

## Slide 67: Multi-Wire EDM Slicing of Ingot -> Large Grain Nb, fewer defects

## Slide 68
100 sheets production in < 50 hrs.
ILC scale 500 sheets per day can be realized by 3-4 machines.
Uniform sheets within 20-40 μm thickness variation.
The surface roughness is very smooth (about 5μm with Rz).
This method can reduce the material waste to 1/3 of the current production.
Status of Ingot Slicing

## Slide 69: High Q0 via Large Grain Ingot Nb, 45 MV/m
D. Reschke et al., SRF2011, THPO046 (2011).
Eacc

## Slide 70
IPAC15, WEPWI013
JLAB study of single-cell cavities
Shape ( LSF, LL, TTF ), Material; Large grain
TTF shape
1.4K
1.8K
2.0K
1012
1011
1010

## Slide 71: Future of SRF for ILC - Summary
Technology Status
Paths to raise gradients
  ILC and TeV Upgrade
Paths to raise Q
Paths to Lower Costs

## Slide 72
FCC hadron collider with 100TeV proton cm energy
~16 T  100 TeV pp in 100 km
~20 T  100 TeV pp in 80 km
Future Circular Colliders (FCC)
From E. Fermi’s 1954
Fermi’s extrapolation to 1994:
2T magnets, R=8000 km (fixed target!)
Ebeam ~ 5x103 TeV  ECM ~ 3 TeV
Cost : 170 B$
Instead We invented colliders and superconducting magnets …
and built the Tevatron and the LHC

## Slide 73: Possible Future Circular Collider (CERN or China) First Stage could be a circular e+e- collider - Higgs Factory
A 50-70 km tunnel is relatively easier NOW in China

## Slide 74: Short Comparison With ILC
  Completion: 2030 – 2040 ?
  1st Stage Higgs Factory
    250 GeV – 350 GeV?
    CERN 80 – 100 km ring
    China 50 – 70 km ring (650 cavities)
    300 – 350 MW
    Nb-Cu cavity technology needs development
  2nd Stage pp collider
    15 – 20 Tesla SC Magnets! Technology to be developed
    100 TeV collisions, LHC = 14 TeV
    500 - 600 MW AC power
Future Circular Collider (FCC)
  Completion: 2026 – 2030 ?
  500 GeV, Upgrade 1 TeV
  30 km tunnel, 16, 000 Cavities (occupy 22 km)
  Operating power: 165 MW
  LHC = 180 MW = ½ Geneva canton
  Technology close to ready, prototype XFEL under construction
  Higher gradients, cost reduction development for Upgrade to 1 TeV
Linear Colliders

## Slide 75
LEP-II 3 GV
XFEL 16 – 18 GV

## Slide 76: LEP-2, 350 MHz, Sputtered Nb-Cu Thin Films Best 7 MV/m, Q = 2 x 109
Problem to solve!
Much improvement in Nb-Cu technology is needed

## Slide 77: Possible Path: Hints for improvement High Power Impulse Magnetron Sputtering (HiPIMS) produces films with enhanced properties
Target material is partly ionized
Nb ions reach substrate with a higher energy than magnetron sputtering
Produce high-quality homogeneous films.

## Slide 78: Final Conclusions
SRF science and technology has taken the accelerator world by storm!
  See next slide
Enormous scientific and economic potential realized.
Biggest application could be the International Linear Collider.
  Japan is considering.
In the US, The P5 report highlights the potential exciting science if it is constructed.
Many breakthroughs in SRF technology came from R&D associated with the initial development aimed at the ILC.
SRF is an active and exciting field with many more breakthroughs ahead!

## Slide 79: Impact of SRF on Accelerators for Science
Low energy nuclear physics, for nuclear shape, spin, vibration... – - -Heavy ion linacs
Medium energy nuclear physics, structure of nucleus, quark-gluon physics
  – Recirculating linac
Nuclear astrophysics, for understanding the creation of elements
  – Facility for rare isotope beams (FRIB)
X-Ray Light Sources for life science, materials science & engineering – Storage rings, free electron lasers, energy recovery linacs
Spallation neutron source for materials science and engineering, life science, biotechnology, condensed matter physics, chemistry
  – High intensity proton linac
Future High Intensity Proton Sources for
  – Nuclear waste transmutation, energy amplifier, power generation from Thorium
High energy physics for fundamental nature of matter, space-time
  – Electron-positron storage ring colliders, linear collider, proton linacs for neutrinos

## Slide 80: Concluding Thought!
We are little people serving great causes,
but because the cause is great,
something of that greatness falls upon us!
Jawaharlal Nehru

## Slide 81: Back-Up Slides

## Slide 82: Possible Choices among Superconducting Materials
Material | Critical Temp. Tc [K] | Normal-state resistivity ρn(μΩcm) | Critical Field Hc(0) [T] | Lower Critical field Hc1(0) [T] | Upper Critical field Hc2(0) [T] | Penetration depth (0) [nm] |  [meV] | Type
Nb | 9.23 | 2 | 0.2 | 0.18 | 0.28 | 40 | 1.5 | II
Pb | 7.2 |  | 0.08 | N/A | N/A | 48 |  | I
NbN | 16.2 | 70 | 0.23 | 0.02 | 15 | 200-350 | 2.6 | II, B1 comp.
NbTiN | 17.3 | 35 |  | 0.03 |  | 150-200 |  | II, B1 comp.
Nb3Sn | 18 | 20 | 0.54 | 0.05 | 30 | 80-100 | 3.1 | II, A15
V3Si | 17 |  |  |  | 24.5 | 179 |  | II, A15
Mo3Re | 15 |  | 0.43 | 0.03 | 3.5 | 140 |  | II, A15
MgB2 | 40 | 0.1-10 | 0.43 | 0.03 | 3.5-60 | 140 | 2.3/7.2 | II- 2 gaps
YBCO | 93 |  | 1.4 | 0.01 | 100 | 150 | 20 | d-wave
Pnictides | 30-55 |  | 0.5-0.9 | 30 | >100 | 200 | 10-20 | 

## Slide 83: The gap symmetry is important
res

## Slide 84: NIOBIUM COST versus PROCUREMENT YEAR
Data from TJNL material orders over time shows a steady escalation in the cost for RRR niobium. This data is consistent with costs observed from previous FNAL material orders.
650 MHz half-cell blanks from latest FNAL material order for Pavac cost over $400 per pound.
Reactor grade niobium also shows significant increase in cost over time.
NB: Plot courtesy of TJNL.