## Slide 1: SC RF R&D Plans at DESY
Wolf –Dietrich Möller
International Workshop on Future Linear Colliders
4-9 December 2016
Aiina Center & MALIOS in Morioka

## Slide 2: Outline
Introduction
Infrastructure
Project driven R&D
  Repair and restoring for XFEL modules
  FLASH CW and XFEL CW
Fundamental R&D
  N2 infusion
Outlook

## Slide 3: Introduction
XFEL installation is finished
Commissioning of XFEL is started, cool down of linac right now
Test infrastructure for series production (AMTF) is available
A number of cavities, couplers, modules and other components are available at DESY
R&D activities have been re-started this summer

## Slide 4: Infrastructure
Our former R&D test infrastructure from TESLA / TTF times is old and cannot be operated anymore
TESLA / TTF preparation infrastructure is maintained and ready for use: clean room, HPR, EP, BCP, CO2, etc.
Large test infrastructure AMTF was installed for the XFEL series production
The AMTF was designed for fast and efficient series measurements
  R&D instrumentation to be installed
  Measurement
  software to be modified

## Slide 5: Infrastructure, new
We are now in the process to change over the AMTF test stands to meet the R&D requirements:
Vertical test stands:
  adaptive for different cavity types (single cell, 9-cell, gun)
  variable antenna,
  different frequencies
  T-map, field emission-map
  second sound,
  magnetometers,
  in situ RRR measurement,

## Slide 6: Infrastructure, new
Modification of module test stands:
  single cavity measurements (1.3GHz and 3.9GHz),
  3.9GHz modules
  SRF gun,
  New coupler test and conditioning stand
Remark: no change in the 1.3 GHz standard module testing capabilities (XFEL, FLASH)
CMTB module test stand is modified for pulse and CW measurements (IOT)
Cryostat adapter to be used for horizontal single cavity tests at AMTF

## Slide 7: Infrastructure, new
Existing 800 ºC oven is now prepared for N2 infusion
N2 doping is also possible although not favorable; DESY projects require high gradients

## Slide 8: Repair and restoring for XFEL
Defect XFEL modules:
  XM8: leak at 2K circuit
  XM46 and 50: not acceptable cavity performance
  XM99: leak in beam vacuum
  XM100: in XFEL replaced by XM-2, now used as spare module
Modules have to be repaired and re-tested; some require complete disassembly
Re-test RF power coupler showing poor performance
  Some RF PC warm parts showed high dynamic thermal losses
  Parts are re-cleaned and baked and need to be retested
  Investigation of cause
Assembly and test of spare third-harmonic module for XFEL

## Slide 9: FLASH CW and XFEL CW, module tests
Module tests at CW have been performed (on CMBT):
Large grain prototype cryomodule (XM-3)
  Qo at 2K and 1.8K after the fast cool down (FCD) and slow cool down(SCD)
Fine grain production cryomodule (XM4)
  Qo at 2K, 1.8K and 1.56K after the FCD and SCD
  Mechanical vibrations and VS stability
To be continued: XM-3 large grain at CMTB with IOT
IOT:
Pmax = 105kW, CW

## Slide 10: FLASH CW and XFEL CW, module tests
<Qo> summary for XM-3
Jacek Sekutowicz
<Qo> summary for XM4
FCD = fast cool down, SCD = slow cool down
<Qo> summary for fast and slow cool down
On both modules and for different temperatures the slow cool down leads to lower Qo values

## Slide 11: FLASH CW and XFEL CW, module tests
Summary of LG and FG cavities tests in all 3 operation modes
Demonstrated average Gradients
*limit was set at that time for dissipated heat load to 16W.
Demonstrated Qo in long pulse /cw operation at 2K and 1.8K
Jacek Sekutowicz
short pulse
long pulse
long pulse
LG = large grain, FG = fine grain

## Slide 12: FLASH CW and XFEL CW, SRF Gun
The 1.5-cell gun cavity prototype was built at TJNAF. The present plug version has very effective cooling of the cathode.
Plug with LHe channels
Nb/Pb
cathode
1.5-cell , 1.3 GHz gun cavity
Next steps:
Build two new guns with improved plug design
Cathode: improve Pb-coating, Morphology and content of other elements
RF tests
Beam tests
Cathode Laser cleaning
Jacek Sekutowicz

## Slide 13: Project driven R&D, FLASH CW and XFEL CW
Other developments for CW operation
  Develop and build a third harmonic module for CW operation
  1.3 GHz 9-cell end-groups improvement for CW
  RF power coupler, PCW > 5kW
  Modify module cryogenic design

## Slide 14
Fundamental R&D, Overview DESY NanoLab Techniques
Spectroscopy & Growth (H. Noei)
X-ray diffraction (V. Vonk)
Microscopy & Structuring (T. Keller)
Magnetic Characterization (R. Röhlsberger)
Andreas Stierle
Tools available to investigate N2 infusion

## Slide 15: Fundamental R&D at DESY NanoLab
Nb (100) Single-Crystal
UHV Mobile Chamber
Cu Kα source
800°C annealing/2 hours
Cooldown to 120°C, insert 25mTorr of N2
Hold for 23 hours
‘Nitrogen infusion’ experiment on a model sample
Ir film/ sapphire
In-situ x-ray reflectivity (XRR) measurements
Surface sensitive technique
Arti Dangwal Pandey,
Guilherme Semione

## Slide 16: Fundamental R&D at DESY NanoLab
‘Nitrogen infusion’ experiment on Nb(100):
preliminary results, analysis will be published
qz (A-1)
qz (A-1)
qz (A-1)
Nb2O5
NbO2
NbO
Nb
NbO
Nb
Room temperature
During/After 800°C anneal
During infusion
at 120°C
25mTorr N2
Nb
Different nitride and oxide phases formed
qz (A-1)
Natural oxide layers
Intensity (ct)
Intensity (ct)
Intensity (ct)
Intensity (ct)
qz (A-1)
Arti Dangwal Pandey,
Guilherme Semione

## Slide 17: Outlook
Preliminary SRF R&D goals at DESY:
Further development and tests on CW modules
Reproduce the N2 infusion and doping results (during 2017)
  On 1cell cavities, fine grain and large grain
  On 9 cell cavities
Work on fundamental understanding of N2 doping and infusion in collaboration with experts from the DESY Nanolab
Assemble and test a module with high Q / high gradient cavities (ca. 2018)

## Slide 18: Overview, SC RF Cavity R&D at DESY
N. Walker

## Slide 19: End
Thank You for Your attention