## Slide 1: N-dope/N-infusion R&D at KEK
2017/6/27
AWLC17@SLAC
K. Umemori, E. Kako, T. Dohmae, Y. Hori,
T. Konomi, G. Park, H. Sakai(KEK),
J. Kamiya, S. Kurosawa, K. Takeishi (JAEA)

## Slide 2: Contents
Introduction
J-PARC furnace and experimental setup
N-dope
Heat treatment (without EP)
N-infusion
Summary

## Slide 3
N-infusion
N-dope
TTC meeting（2014/Dec） A. Melnychuk 「Update on N doping at Fermilab」
25mTorr N2
@800 deg C, 2min
25mTorr N2
@120 deg C, 48hours
S. Aderhold / A. Grassellino (TTC@Saclay)
High-Q
High-Q &
High-G
A. Romanenco (Linac14)
N goes to several tens um
N goes to around ten nm

## Slide 4
KEK tried following R&D issues using J-PARC furnace
Nitrogen doping
Heat treatment without EP
(Preparation for Nitrogen infusion)
Nitrogen infusion

## Slide 5: N-dope/N-infusion trial using J-PARC furnace
J-PARC has oil-free furnace with cryo-pump and TMP.
Vacuum level reached to ~1e-6 Pa.
Normally used for degassing of beam-duct and components.

## Slide 6
N-injection system
Nitrogen pressure is controlled by variable leak valve
Cryo-pump is closed and TMPs are off during N-injection. Small pump set, TMP and scroll, pump the furnace.

## Slide 7
Cavity preparation for heat treatment
HPR (flange open) 2 hours, drying one night
Cavity was double-packed inside class-1000
Nb cap & foil was ultrasonic cleaned with degreasing, drying inside class-10, packed inside class-1000
Transport to J-PARC
Setup into J-PARC furnace

## Slide 8
N-dope

## Slide 9
N-dope (J-lab parameter)
800 deg, 3 hours
800 deg, 20 min, N 2.7Pa
800 deg, 30 min
Cooldown
KEK tried J-lab N-doping parameter.

## Slide 10
VT results of N-doping
VT4(reference) Rs=3.3nΩ
VT5(N-dope) Rs=1.8nΩ
VT6(add EP) Rs=1.2nΩ
VT4(reference measurement)
N-doping
15um EP  VT5
Additional 10um EP →VT6
Magnetic field canceled. (< 1mG)
Cooled down with thermal gradient
Very high Q up to high field
Q = 2.4e11@11MV/m, 1.4K
Q = 3.3e10@14MV/m, 2.0K
Quench at 19MV/m
No field emission
First success in Japan

## Slide 11
Heat treatment without EP (Preparation for N-infusion)

## Slide 12
Heat treatment (800 C, 3h) and VT preparation
800℃, 3hours heat treatment at J-PARC furnace
Transfer to KEK with double-packed
HPR
Assembly
120℃ baking
Vertical test
No EP was applied!

## Slide 13
Vertical test results (comparison before/after heat treatment)
Cavity performance was perfectly reproduced.
No degradation!!
Stop meas.
(No quench)
Stop meas.
(No quench)

## Slide 14
N-infusion

## Slide 15
Heat treatment
800 degree C
3 hours
120 degree C
N-infusion (3.3Pa = 25mTorr)
48 hours
Pressure is stabilized less than 0.1Pa
Different vacuum gauges at different positions show around 0.3 Pa offset.
Temperature is stabilized with +/- 5 degree.
Temp. offset ~ 5 degree between furnace and jigs.

## Slide 16
VT results for N-infusion
Q-slope above Eacc > 5 MV/m
VT11: 2.9 nΩ
VT12: 2.9 nΩ
Magnetic field canceled. (< 1mG)
Cooled down with thermal gradient
Transfer to KEK
HPR (No EP applied)
Assembly
Degradation was observed for > 5 MV/m
Eacc was limited at 33MV/m by quench at 225 degree equator
No field emission

## Slide 17
Summary
N-dope and N-infusion study is on going at KEK to realize high performance of SRF cavities.
Heat treatment was carried out using J-PARC furnace, which is pumped by a cryo-pump and TMPs.
N-doping was successful. High-Q was obtained for 10-15 MV/m.
Cavity performance was tested after heat treatment. No degradation was observed, even not applying EP.
N-infusion was carried out. Degradation occurred at more than 5 MV/m.
We will try to push to realize N-infusion technique for high performance SRF accelerators.

## Slide 18
Backup slide

## Slide 19
Typical vertical test setup
Flux gate sensor, Si temperature sensor, heater and solenoid coil were used.
Solenoid coil
Flux gate sensor
Si temperature sensor
(Equator and beamtube)
Heater
※ Pictures are for different measurement.
※ But setup of sensors and coil are same.