## Slide 1
Radiation Hardness, Sensitivity, Charge Collection Time
Update on Chronopixel R&D
Americas Workshop on Linear Colliders 2017
June 27, 2017
Christian Weber, Yale University
1.2mm
Notes: Thank you!
Chronopixel – Fully Monolithic pixel detector in CMOS technology
Will explain what that means
Present tests of it pertinent to the ALAS phase 2 operation after the High luminosity upgrade of the LHC

## Slide 2: Chronopixel
a fully monolithic active pixel sensor, designed for the International Linear Collider’s (ILC) Silicon Detector
Chronopixel prototype 3
2004 | – talks with Sarnoff Corporation regarding chip design begins – Yale (Baltay), Oregon (Brau, Sinev, Strom), Sarnoff Corporation
2007 | – prototype 1 conceptual design completed – 2 buffers, digital calibration
2008 | – prototype 1 fabrication (TSMC) completed – 180 nm process 60 mm pixels
2010 | – prototype 1 testing completed – Sarnoff contracted with prototype 2 development
2012 | – prototype 2 fabrication (TSMC) completed; delivery to SLAC (Sinev), testing begins – 90 nm process = 25 mm pixels
2013 | – prototype 3 discussion with Sarnoff; features defined – 90 nm process = 25 mm pixels
2014 | – prototype 3 design and then fabrication completed; chips delivered to SLAC (Sinev)
2015 | – current collaboration formed, prototype 3 testing continues at SLAC (Sinev) with – concurrent efforts at Yale
2004 | – talks with Sarnoff Corporation regarding chip design begins – Yale (Baltay), Oregon (Brau, Sinev, Strom), Sarnoff Corporation
2007 | – prototype 1 conceptual design completed – 2 buffers, digital calibration
2008 | 
2010 | – prototype 1 testing completed – Sarnoff contracted with prototype 2 development
2012 | – prototype 2 fabrication (TSMC) completed; delivery to SLAC (Sinev), testing begins – 90 nm process = 25 mm pixels
2013 | – prototype 3 discussion with Sarnoff; features defined – 90 nm process = 25 mm pixels
2014 | – prototype 3 design and then fabrication completed; chips delivered to SLAC (Sinev)
2015 | – current collaboration formed, prototype 3 testing continues at SLAC (Sinev) with – concurrent efforts at Yale
Development History
mm
Notes: Fullly Monolithic active pixel sensor, being developed for the ILC, since 2004

## Slide 3: CMOS
CMOS: complimentary metal-oxide semiconductor
process of implementing NMOS* and PMOS* on a single integrated circuit
and also type of hardware logic design that uses them in a complimentary fashion.
** N- or P-type Metal-Oxide-Semiconductor (Field Effect Transistor): two types of transistors
CMOS Allows for monolithic detectors: sensor and readout on same die
Notes: Cmos: complimantary metal-oxide semiconductor
Refers: technology and as well as chip design that uses them in complimentary fashion
Current pixel sensors: two chips, one sensing, one readout, bump bonding ($$$)
CMOS: can embedd readout electronics within the sensor itself
(thin, no bump bonding, smaller pixels etc)
Radiation hardness needs to be proven, and I am going to present measurements of our that that effect.
But first let me talk about features of the chronopixel

## Slide 4: Chronopixel features
  fully monolithic CMOS sensor no separate readout chip, electronics embedded within pixels
  small pixel pitch: 25 µm x 25 µm (compare to 400 µm x 50 µm of current ATLAS pixel modules)
  only digital readout, simplifies electronics considerably small pitch can compensate for lack of time-over-threshold µm
  adjustable sensor threshold voltage for classifying pixel as hit
  timestamping of hits
  store multiple timestamps on a pixel between readouts
  zero suppression: read out only x,y and time-stamps of hit pixels
single pixel layout
25 µm
25 µm
Notes: As mentioned, fully monolithic CMOS sensor, electronics in pixels
Small pixel pitch,
that can compensate the exclusively digitately readout, i.e. we have a binary hit/not hit classification for each pixel and not time over threshold
However, we can set adjust this threshold

## Slide 5: ILC
5 bunch trains every second
1312 bunches in a train, 554 ns apart
Silicon Detector (SiD)
convective cooling only
0.13 mW/mm2 tracker power dissipation limit
Notes: accommodate

## Slide 6: Chronopixel Operation
ILC bunch trains
200 ms
1312 bunches
0.7 ms
time (ms)
554 ns
ILC bunches
time (μs)
Set threshold / calibrate comparator
Information stored in capacitors
ms, lasts for ms
Clear memory
μs
Increment timestamp
Latch timestamp if hit
μs
Read out pixels
μs per timestamp
Chronopixel powered down
198 ms

## Slide 7: Chronopixel Prototype 3
monolithic CMOS design 90 nm feature size, 7 µm epitaxial layer 280 µm thick chip 10 ohmcm manufactured by TSMC
store up to 2 hits per pixel
implements 6 sensor diode options
Chronopixel prototype 3 development board
Chronopixel
prototype 3

## Slide 8: Sensor options in prototype 3
  same as in prototype 2 – for comparison similar capacitance to group 6
  deep NWELL diode in the window in P++ layer
  shallow NWELL diode, also in the window
  “Natural transistor” (NTN) in the P++ layer window transistor is formed directly on P+ epi layer large source and drain diffusion areas gate connected to both source and drain and form sensor output
  also NTN but with 2 fingers source and drain are narrow gate also connected to both, as in option 4
  same as 5, however gate is not connected to source and drain, but connected to external bias voltage
1
2
3
4
5&6
six different sensor options were implemented on the same chip – 8 columns for each option:
signal 1/C
capacitor noise 1/sqrt(C)
signal / noise 1/sqrt(C)

## Slide 9: Capacitance measurements
diode option | Capacitance (fF) | μV/e
1 | 9.0 | 18
2 | 6.2 | 26
3 | 2.7 | 59
4 | 4.9 | 33
5 | 4.9 | 33
6 | 8.9 | 18
Option 3:
Capacitance:
testing at SLAC (N. Sinev) for many years
signal 1/C
capacitor noise 1/sqrt(C)
signal / noise 1/sqrt(C)

## Slide 10: Noise measurements
Option # | Capacitance (fF) | Signal (μV/e) | Noise r.m.s (mV) | Noise r.m.s (# electrons)
1 | 9.0 | 18 | 1.12 | 63
2 | 6.2 | 26 | 1.08 | 42
3 | 2.7 | 59 | 1.7 | 29
4 | 4.9 | 33 | 1.21 | 37
5 | 4.9 | 33 | 1.23 | 38
6 | 8.9 | 18 | 0.98 | 54

## Slide 11: Noise and threshold considerations
# conduction electrons produced
cumulative probability
1 GeV Pion, incident on Si, 7 µm
Number of electron-hole pairs in Silicon generated by minimum ionizing particle is a probability distribution
Set threshold at ½ of the 1st percentile of #electrons generated for 99% detection efficiency event if charge is shared between two pixels
epi-layer (μm) | threshold | Min signal / noise For sensor #3
4 | 20 | 0.7
7 | 63 | 2.2
10 | 125 | 4.3
15 | 200 | 6.8
20 | 275 | 9.5
epi-layer (μm) |  | Min signal / noise For sensor #3
4 | 20 | 0.7
7 | 63 | 2.2
10 | 125 | 4.3
15 | 200 | 6.8
20 | 275 | 9.5
prototype 3
Sensor option 3:
signal 59mV/e
noise 29 e

## Slide 12: Charge collection speed simulations
Courtesy of G. Giacomini, BNL
not irradiated
irradiated to 1015 neq/cm2
20 ns
Minimum ionizing particle at , 1 V bias
`
charge collection via diffusion
radiation level determine
cooling improves charge collection time

## Slide 13: irradiation campaigns
4 MeV Protons, UMass Lowell
1 MeV Neutrons, UMass Lowell
1 MeV Protons, Yale

## Slide 14
see G.H.R Kegel et al, IEEE TNS vol39, No6 (1992)
Neutron production
Protons, 4 MeV
Lithium target
by bombarding 7Li with Protons
Neutrons

## Slide 15
Neutron production
by bombarding 7Li with Protons
for 4 MeV protons
see G.H.R Kegel et al, IEEE TNS vol39, No6 (1992)

## Slide 16
Neutron irradiation test
Lithium target
4 MeV proton incident on 7Li target to produce neutrons
proton beam current and neutron rate monitored during irradiation test
total number of neutrons created is eventually determined by radiation assay of target
Chronopixel still working after 1013 neq/cm2
see G.H.R Kegel et al, IEEE TNS vol39, No6 (1992)

## Slide 17
Proton irradiation test
4 MeV proton incident on Chronopixel
proton beam current monitored during irradiation test
Bragg peak after epi layer - within Si bulk
Proton fluence
Equivalent to neq/cm2 (hardness factor)
Chronopixel inoperable
H. Spieler, Semiconductor Detector Systems Ch 7; Oxford University Press (2005)
‘hardness factor’

## Slide 18: Total integrated dose test
Test resistance w.r.t. total ionizing dose received
1MeV protons
4 nA current (large dose rate!)
energy deposited within first 8 μm of silicon ( epi layer)
multiple irradiation runs
protons

## Slide 19: Total integrated dose test
Test resistance w.r.t. total ionizing dose received
1MeV protons
4 nA current (large dose rate!)
energy deposited within first 8 μm of silicon ( epi layer)
multiple irradiation runs
protons
After each irradiation run
anneal at 60°C for 80 min
test for change in count rate using Sr-90 source ( , MeV , minimum ionizing)

## Slide 20: Irradiation results
sensor type 1 •
sensor type 2 •
sensor type 3 •
sensor type 4 •
sensor type 5 •
sensor type 6 •
ATLAS phase 2 pixel detector, outer layer
ATLAS phase 1 pixel detector, inner layer

## Slide 21: ILC Chronopixel performance requirements
Parameter | ILC Requirement | Prototype Tests
Detector Sensitivity | 10 μV/electron | 59 μV/electron
Detector Noise | 25 electrons | 29 electrons
Comparator Accuracy | 0.2 mV RMS | 0.2 mV RMS
Sensor Capacitance | 10 fF | 2.7 fF
Clocking Speed | 3.3 MHz | 7.3 MHz
Charge collection time | 300 nsec | 20 nsec
Readout Rate | 25 Mbits/sec | 25 Mbits/sec
Power Consumption | 0.13 mW/mm2 | OK by estimate
Radiation Hardness | 1011 neutrons/cm2/yr | 1013neutrons/cm2 or 110 Mrad

## Slide 22: High-Luminosity LHC
increase in luminosity by a factor of 5
increased pileup
harsher radiation environment for the detector
challenge for particle tracking and radiation hardness for the detector components
need pixel replacement
M. Lamont @ Recontre workshop, Vietnam
CMOS
Chronopixel
LF CPIX
3D sensors
Planar sensors
Insertable B-Layer
Options:
HL-LHC
ATLAS phase 2

## Slide 23: Timing: ILC, HL-LHC, and Chronopixel
ILC bunch trains
200 ms
1312 bunches
0.7 ms
time (ms)
554 ns
ILC bunches
time (μs)
Set threshold / calibrate comparator
Information stored in capacitors
ms, lasts for ms
Clear memory
μs
Increment timestamp
Latch timestamp if hit
μs
Read out pixels
μs per timestamp
Chronopixel powered down
198 ms
continuously operating
25 ns
HL-LHC: continuous set of bunches
HL-LHC bunches
time (μs)
time (ms)
+ Read out all data after each bunch train
+ Store data for 0.012 ms, read out only on ‘trigger’

## Slide 24: Pixel bandwidth
Want to keep up with at least 99.9% of events.
So need to transfer at least 9 hits out of column within 1 µs
9 hits each at
9 bit timestamp
11 bit column id
11 bit row id
Bandwidth: 9*31 bit / 1 µs 280 Mbit / s per column
Similar for out of module bandwidth
On average 29 hits per module
Bandwidth: 29*31 bit / 1 µs 900 Mbit / s per module
ATLAS sensor module size 40.3 mm x 33.9 mm
@25µm pixel pitch: 1612 x 1356 pixels
(may stitch 4 smaller modules)

## Slide 25: Radiation Hardness
Radiation hardness requirements for pixel layers in ATLAS:
 | ATLAS LHC | ATLAS HL-LHC | 
 |  | Outer (cm) | Inner (cm)
NIEL (neq /cm2) |  |  | 
Ionizing dose (Mrad) |  |  | 
 | ATLAS LHC | ATLAS HL-LHC | 
NIEL (neq /cm2) |  |  | 
Ionizing dose (Mrad) |  |  | 
Increase in luminosity at LHC will cause an increase in pile up from now to .
Increased radiation hardness requirements for detector components
1 Gy = 100 rad
Notes: Radiation hardness is under investigation
Present studies related to the hardness w.r.t. the total ionizing dose
But first let me talk about the properties of our Chronopixel

## Slide 26: Chronopixel Performance Requirements
Parameter | ILC Requirement | HL-LHC Requirement | Prototype Tests
Detector Sensitivity | 10 μV/electron | 10 μV/electron | 59 μV/electron
Detector Noise | 25 electrons | 25 electrons | 29 electrons
Comparator Accuracy | 0.2 mV RMS | 0.2 mV RMS | 0.2 mV RMS
Sensor Capacitance | 10 fF | 10 fF | 2.7 fF
Clocking Speed | 3.3 MHz | >40 MHz | 7.3 MHz
Charge Collection Time | 300 nsec | 25 nsec | 20 nsec(simul)
Read Out Rate | 25 Mbits/sec | 1000 Mbits/sec | 25 Mbits/sec
Power Consumption | 13 mW/mm2 * 1% duty cycle | ~10 mW/mm2* 100% duty cycle | OK by estimate
Radiation Hardness | 1011 n/cm2/year | 1014n/cm2/year | 1013n/cm2
Readout Logic | All Hit Pixels | Hits w/t=t(trigger) | 
Notes: I changed here the LHC readout rate requirement, added the LHC Power requirements, and changed the ILC requirement to make it comparable to the LHC one

## Slide 27: Conclusion
Collaborators:
Jeff Ashenfelter – Yale (staff)
Keith Baker – Yale (faculty)
Charlie Baltay – Yale (faculty)
Tom Barker – Tomtronics (CEO) / Yale (staff)
Jim Brau – Oregon (faculty)
Nick Sinev – Oregon (staff)
David Strom – Oregon (faculty)
Christian Weber – Yale (grad student)
working Monolithic Active Pixel Sensor
satisfies ILC requirements in general
Next up
beam tests to measure in time efficiency

## Slide 28: Backup

## Slide 29: ATLAS (pixel) detector
ATLAS detector
Inner Tracker
Pixel Detector
Pixel Module
close to interaction point (radius Layer 0 : 5cm)
exposed to largest particle fluence and large radiation dose
accrues radiation damage over time
Notes: ATLAS detector – number of sub systems
Among them: Inner tracker – aiding in track building
Innermost part: Pixel Detector
Made up of large number of pixel modules’
Accrue radiation damage over time -> finite lifespan at given luminosity, however Luminosity is set to increase

## Slide 30: Charge collection speedup
Improve charge collection speed by increasing depletion region
  need high resistivity silicon (up to 10 kOhm cm)
Charge collection still partially by diffusion
Could improve resolution
  If charge spreads to adjacent pixels, not originating from below sensor diode
3D Simulations under way to study these effects (Nick Sinev)
x (µm)
y (µm)

## Slide 31: electronics logic schematic
electronics logic schematic – prototype 3
Each pixel has electronics to detect charged particle hit and to record the time (time stamp) of each hit.