## Slide 1
Martina Martinello
LCWS 2017 – Strasbourg, France
24th October 2017
High-Q at high gradient at FNAL

## Slide 2: N-doping vs 120C baking
N-doping: very high Q-factors at 15-20 MV/m, quench field usually < 30 MV/m
120C baking: capability to reach high gradients 35-45 MV/m with Q < 1010
Anti-Q-slope
A. Grassellino et al., Supercond. Sci. Technol. 26, 102001 (2013) – Rapid Communications
Notes: High Q at high gradients may reduce both capital and operational cost of the accelerators

## Slide 3: N-doping vs 120C baking
N-doping: very high Q-factors at 15-20 MV/m, quench field usually < 30 MV/m
120C baking: capability to reach high gradients 35-45 MV/m with Q < 1010
Anti-Q-slope
A. Grassellino et al., Supercond. Sci. Technol. 26, 102001 (2013) – Rapid Communications
N doping: nitrogen throughout several microns
A. Grassellino et al, Proceedings of SRF 2015
N Doping at T> 800C manipulate mean free path constantly throughout several microns, giving the highest Q
Notes: High Q at high gradients may reduce both capital and operational cost of the accelerators

## Slide 4: N-doping vs 120C baking
N-doping: very high Q-factors at 15-20 MV/m, quench field usually < 30 MV/m
120C baking: capability to reach high gradients 35-45 MV/m with Q < 1010
Anti-Q-slope
A. Grassellino et al., Supercond. Sci. Technol. 26, 102001 (2013) – Rapid Communications
120C bake, vacancies in first ~ 60 nanometers
mfp ~ 2-16 nm
mfp ~ 70 nm
120C bake known to manipulate mean free path at very near surface on clean bulk, giving the highest gradients
A. Romanenko et al, Appl. Phys. Lett. 102, 232601 (2013)
Notes: High Q at high gradients may reduce both capital and operational cost of the accelerators

## Slide 5: Motivation behind experiments
Composition and mean free path in first nanometers of cavity surface have been shown to be crucial for both Q and gradient performance
N Doping (high-Q)
+
120C baking (high gradients)
N-infusion: high-Q at high gradient
at 35 MV/m

## Slide 6: Example of N-infusion processing sequence
Bulk electro-polishing
High T furnace (with caps to avoid furnace contamination):
  800C 3 hours HV
  120C 48 hours with N2 (25 mTorr)
NO chemistry post furnace
HPR, VT assembly
Protective caps and foils are BCP’d prior to every furnace cycle and assembled in clean room, prior to transporting cavity to furnace area
A. Grassellino et al., arXiv:1305.2182
A. Grassellino et al 2017 Supercond. Sci. Technol. 30 094004
160 C
48 h
96 h
25 mTorr
10-5 mTorr

## Slide 7: Cavity evolution- EP

## Slide 8: Cavity evolution – 120C baking

## Slide 9: Cavity evolution – 120C N-infusion

## Slide 10: Cavity evolution – probing the parameter space
Increasing T ~40C turns cavity into “doped shape”!

## Slide 11: Cavity evolution – probing the parameter space
Increasing T ~40C turns cavity into “doped shape”!
Increasing duration x 2 turns cavity into “doped shape”, even higher Q!

## Slide 12: Cavity evolution – 120C N-infusion
What gives the Q improvement at high field with N-infusion at 120C?

## Slide 13: What gives the Q improvement at high field with 120C infused?
Improvement stems from both lower residual and lower BCS surface resistance
Standard 120C baking
120C N-infusion
Standard
120C baking
120C N-infusion
A. Grassellino et al 2017 Supercond. Sci. Technol. 30 094004

## Slide 14: What gives the Q improvement at high field with longer duration/higher T N-infused?
Improvement stems from both lower residual and lower BCS surface resistance
120C infused 48h

## Slide 15: What gives the Q improvement at high field with longer duration/higher T N-infused?
Improvement stems from both lower residual and lower BCS surface resistance
120C infused 48h
120C infused 96h

## Slide 16: What gives the Q improvement at high field with longer duration/higher T N-infused?
Improvement stems from both lower residual and lower BCS surface resistance
120C infused 48h
120C infused 96h
160C infused 48h

## Slide 17: What gives the Q improvement at high field with longer duration/higher T N-infused?
Improvement stems from both lower residual and lower BCS surface resistance
The decreasing of RBCS with the field allows the manifestation of the anti-Q-slope
anti-Q-slope

## Slide 18: Nitrogen role in 120C N-infusion
No (clear) nitrides formation at the RF surface
Small () N2 enriched layer below native oxide
SIMS data suggest that performances are related to the first nm from the RF surface
Being investigated with subsequent HF rinsing experiment
120C infused
120C baking
SEM 120C N-infused Nb
Courtesy of Y. Trenikhina
Courtesy of Y. Trenikhina

## Slide 19: Nitrogen role in 140/160C N-infusion
No (clear) nitrides formation at the RF surface
Higher N2 background than not infused samples, through the whole penetration depth
Very similar to N2 signal after EP in N-doped samples
No (clear!) presence of nitrides at the surface
Being investigated with subsequent HF rinsing experiment
160C infused
140C infused
SEM 160C N-infused Nb
Courtesy of Y. Trenikhina
Courtesy of Y. Trenikhina
120C baking

## Slide 20: 120 C N-infusion: high at high gradients
N-Infusion successful also on 9-cell cavities!
Single-cell
A. Grassellino et al 2017 Supercond. Sci. Technol. 30 094004
2 times higher!
9-cells

## Slide 21: 120 C N-infusion: high at high gradients
9-cells
Compared to this table values for E-XFEL, results of 9-cell N-infused cavities would lay in top 1%

## Slide 22: ILC possibility of cost reduction
8 cavities
~10 m
  ILC: 16,000 cavities in 31 km linac
  European XFEL
Baseline design
Image from linearcollider.org. Tunnelflug video by European XFEL. Cost analysis by N. Solyak
Q0 still very important!
*N-infusion cost reduction takes into account also the difference cost of the processing chain
Notes: We’re doing cost savings studies to try to make the ILC more affordable and increasing the gradient has the largest impact, but Q0 also has a strong impact

## Slide 23: N-infusion easily affected by furnace contamination
Example of N-infused cavity contaminated by furnace environment
Quite high level of hydrocarbons may be absorbed by the cavity
Notes: We’re doing cost savings studies to try to make the ILC more affordable and increasing the gradient has the largest impact, but Q0 also has a strong impact

## Slide 24: N-infusion easily affected by furnace contamination
Example of N-infused cavity contaminated by furnace environment
Quite high level of hydrocarbons may be absorbed by the cavity
Notes: We’re doing cost savings studies to try to make the ILC more affordable and increasing the gradient has the largest impact, but Q0 also has a strong impact

## Slide 25: Strategies to implement the N-infusion technology
1. Very clean furnace environment
2. R&D to investigate other regime that are less affected by contamination
High-T N treatment that allows post chemistry and capable to create a thin N-enriched layer
Probe the parameter space to find an optimal spot for N diffusion rather than C
Etc..
Notes: We’re doing cost savings studies to try to make the ILC more affordable and increasing the gradient has the largest impact, but Q0 also has a strong impact

## Slide 26: E-XFEL 120C baked cavities results
Only about 30% of the E-XFEL production cavities reach 11010 above 20 MV/m. Why?

## Slide 27: E-XFEL 120C baked cavities results
Only about 30% of the EXFEL production cavities reach 11010 above 20 MV/m. Why?
New understanding of flux expulsion/dissipation could explain the mismatch

## Slide 28: Fast Cooldown Helps Flux Expulsion
Fast cool-down lead to large thermal gradients which promote efficient flux expulsion
Slow cool-down → poor flux expulsion
A. Romanenko et al., Appl. Phys. Lett. 105, 234103 (2014)
A. Romanenko et al., J. Appl. Phys. 115, 184903 (2014)
M. Martinello et al., J. Appl. Phys. 118, 044505 (2015)
S. Posen et al., J. Appl. Phys. 119, 213903 (2016)
T1
T2
Q0
BSC/BNC
New understanding of expulsion

## Slide 29: High-T Treatment to Promote Expulsion
New understanding of expulsion
Magnetic Flux
Trapping
Magnetic Flux
Expulsion
S. Posen et al. “Efficient expulsion of magnetic flux in SRF cavities for high Q0 applications,” Journal of Applied Physics 119, 213903 (2016)
900°C furnace treatment
Notes: In addition to the development of the nitrogen infusion process, recent SRF R&D efforts have led to significant progress in understanding of magnetic flux. We knew already that practical magnetic shielding is imperfect and that when cooling a cavity in a realistic 5-10 mG background magnetic field, that the field can potentially be trapped in the superconductor, leading to Q0 degradation, but it can also be expelled from the material. We learned just in the last couple years that proper treatment of the material can promote expulsion, preventing Q0 degradation. We also learned that even if the flux is trapped, different treatments lead to different sensitivities to trapped flux.

## Slide 30: Q Degradation due to Trapped Flux
2 K, 16 MV/m, 1.3 GHz
M. Martinello et al., Appl. Phys. Lett. 109, 062601 (2016)
15 mG of trapped flux can degrade performance, lowering Q below 1010
Notes: In addition to the development of the nitrogen infusion process, recent SRF R&D efforts have led to significant progress in understanding of magnetic flux. We knew already that practical magnetic shielding is imperfect and that when cooling a cavity in a realistic 5-10 mG background magnetic field, that the field can potentially be trapped in the superconductor, leading to Q0 degradation, but it can also be expelled from the material. We learned just in the last couple years that proper treatment of the material can promote expulsion, preventing Q0 degradation. We also learned that even if the flux is trapped, different treatments lead to different sensitivities to trapped flux.

## Slide 31: Q Degradation due to Trapped Flux
2 K, 16 MV/m, 1.3 GHz
15 mG of trapped flux degrades performance, but Q still higher than 1.51010
M. Martinello et al., Appl. Phys. Lett. 109, 062601 (2016)
Notes: In addition to the development of the nitrogen infusion process, recent SRF R&D efforts have led to significant progress in understanding of magnetic flux. We knew already that practical magnetic shielding is imperfect and that when cooling a cavity in a realistic 5-10 mG background magnetic field, that the field can potentially be trapped in the superconductor, leading to Q0 degradation, but it can also be expelled from the material. We learned just in the last couple years that proper treatment of the material can promote expulsion, preventing Q0 degradation. We also learned that even if the flux is trapped, different treatments lead to different sensitivities to trapped flux.

## Slide 32: Magnetic Flux – Sensitivity and Expulsion
Flux expulsion
Sensitivity to trapped flux
Preservation of Q in CM environment
900°C furnace treatment
Magnetic Flux
Trapping
Magnetic Flux
Expulsion
M. Martinello et al. “Effect of interstitial impurities on the field dependent microwave surface resistance of niobium,” Appl. Phys. Lett. 109, 062601 (2016)
S. Posen et al. “Efficient expulsion of magnetic flux in SRF cavities for high Q0 applications,” Journal of Applied Physics 119, 213903 (2016)
2 K, 16 MV/m, 1.3 GHz
In order to maintain high-Q at high gradient in a cryomodule, it is extremely important to maximize flux expulsion and to minimize remnant field
Notes: In addition to the development of the nitrogen infusion process, recent SRF R&D efforts have led to significant progress in understanding of magnetic flux. We knew already that practical magnetic shielding is imperfect and that when cooling a cavity in a realistic 5-10 mG background magnetic field, that the field can potentially be trapped in the superconductor, leading to Q0 degradation, but it can also be expelled from the material. We learned just in the last couple years that proper treatment of the material can promote expulsion, preventing Q0 degradation. We also learned that even if the flux is trapped, different treatments lead to different sensitivities to trapped flux.

## Slide 33: ILC cost reduction – SRF R&D in US (FNAL, ANL, Jlab, Cornell)
Funds for ILC cost reduction for US collaboration have recently been received ($1M for one year) from DOE HEP
FNAL-lead collaboration, includes: FNAL, ANL, Jlab, Cornell
Agreed on the first year plan:
  Demonstrate increase in Q at 35 MV/m via flux expulsion
    FNAL owns about a dozen of cavities that were ILC qualified, dressed ready for cryomodule; we will undress them, re-baseline them, then apply the treatment pioneered at FNAL (and now applied to all LCLS-2 cavities) to increase magnetic flux expulsion (900C bake); re-test to demonstrate on ~10 nine cell cavities Q ~1.5e10 at 35 MV/m – Fermilab, ANL and Jlab
  In parallel continue to push single cell R&D for high Q at high gradient via doping/infusion – FNAL, ANL, Jlab, Cornell
  Apply best High Q/high gradient recipe to several nine cells – FNAL, Jlab
  Dress best nine cell cavity and demonstrate high Q at 35 MV/m in cryomodule configuration (horizontal test stand)
  Install high power klystron at FNAL Vertical test Facility to study field emission reduction via high power pulsing (HPP)

## Slide 34: Conclusions
N-infusion suitable treatment to obtain high-Q at high gradient
Modification of the superficial mean-free-path at the nanometer scale
Successful results obtained also on 9-cell cavities, potentially useful for ILC cost reduction
More R&D needed to increase reliability of the process
US collaboration (FNAL, ANL, JLAB, Cornell) on SRF R&D effort for ILC cost reduction

## Slide 35: Team Effort
Results shown here are due to many hardworking people
Thanks to SRF department for contributions with graphs, slides, etc.

## Slide 36
Thank you for your attention!