## Slide 1: (Selected) SRF R&D activity at CEA Saclay
| SRF group meeting @ KEK
C. Z. Antoine (O. Napoly, F. Eozenou, T. Proslier…)

## Slide 2: Ultimate limits in SRF-1
Niobium cavities
  Performances
    Eacc  HRF
    Q0 ( 1/RS)  TC => Nb3Sn, MgB2, NbN…
    Limit = magnetic transition of the SC material @ Hpeak
  Superconductivity only needed inside :
    Thickness ~ < 1 µm => thin films
    (onto a thermally conductive, mechanically resistant material, e.g. Cu)
  Today :
    Thin films exhibit too many defects
    Only Bulk Nb has high SRF performances
  Issues : getting “defect free” superconductors (yes but not all defects are detrimental…)
H field mapping in an elliptical cavity
HPeak
0
HMax.

## Slide 3: Ultimate limits in SRF-2
H
T
HC1
HC2
TC
Mixed state w.Vortex
(i.e. N. cond. flux line + screening currents)
Screening current over l, no magnetic field deeper
Meissner state
  SC phase diagram
    All SC applications except SRF: mixed state w. vortex
    Vortices dissipate in RF !
    SRF => Meissner state mandatory !
    HC1 = limit Meissner/mixed state
    Nb: highest HC1 (180 mT)
    “Superheating field”(?) :
  Metastable state favored by H // to surface
    Difficult to get in real life !

## Slide 4: What is the limit (Hp/HC1/HSH) ?
  Real world cavities behavior is dominated by a few number of defects
  It is very important to measure the penetration field of samples in realistic conditions
T2
T2C
HC1
HSH
H
H//
H
T2
T2C
HC1
HSH
H
H//
H
  ~100 µm in 1 ns (~RF period)
  Compare with l (field penetration depth)
    Nb : ~ 40 nm
    MgB2 ~ 200 nm
  Avalanche : high RF dissipation
MgB2: http://www.nature.com/srep/2012/121126/srep00886/full/srep00886.html?message-global=remove&WT.ec_id=SREP-20121127

## Slide 5: EFFECTs of local defects
  Vortices enter more easily at lower temperature (counter intuitive !)?
    @ T~TC : H is low => low dissipations => easy to thermally stabilize
    @ T<<TC : H is high=> even if small defect => high dissipations => Favors flux jumps
Dissipations :
=> We have to reduce defect density (yes but which ones?)
Nb3Sn
HC1Nb3Sn (~27mT)
(50 mT pour le bulk)
Recent results from Cornell CW (Posen, 2015 (17 MV/m))
Cornell, 1997
pulsed
Nb HC1
(170 à 200 mT)
HSHNb3Sn
(~ 400 mT @ 0 K)
Hays. "Measuring the RF critical field of Pb, Nb, NbSn". in SRF 97. 1997.
~ 2K

## Slide 6: After niobium : nanocomposites multilayers
  Dielectric layer
    Small  vortex (short -> low dissipation)
    Quickly coalesce (w. RF)
    Blocks avalanche penetration
    => Multilayer concept for RF application
  Nanometric I/S/I/ layers deposited on Nb
    SC nanometric layers ( 100 nm) => HC1 => Vortex enter at higher field
    Nb surface screening => allows high magnetic field inside the cavity => higher Eacc
    SC w. high TC than Nb (e.g. NbN): => Q0multi >> Q0Nb
Structures proposed by A. Gurevich in 2006, SRF tailored
Cavity's internal surface
→
Happlied //
HNb
S-I-S
dsc
Notes: A. Gurevich, "Enhancement of RF breakdown field of SC by multilayer coating". Appl. Phys.Lett., 2006. 88: p. 12511.
Couche fine : pas favorable énergétiquement à la nucléation d’un vortex => augmentation artificielle du HC1.
Couches trop fines pour écranter totalement le champ, seulement atténuation : il en faut plusieurs => structures à optimiser

## Slide 7: What is the limit (Hp/HC1/HSH) ?
  Real world cavities behavior is dominated by a few number of defects
  It is very important to measure the penetration field of samples in realistic conditions
T2
T2C
HC1
HSH
H
H//
H
T2
T2C
HC1
HSH
H
H//
H
  Local magnetometry
    ~ Same geometry as cavities
    No shape/edge effect (vs DC/ Squid magnetometry)
    No demagnetization effect
    Measures actual penetration field wherever it is HP/HC1/HSH

## Slide 8: Experimental Details
T
TC
HC1
HMelting
H
HC2
Ia/Ha
Meissner state
Vx lattice
Vx ~ liquid
  Low frequency ≡ DC :
    0 < Ha< HC1 => R=O, Meissner state
    HC1< Ha< HM =>Vx are trapped, R=O, Campbell regime
    HM< Ha< HC2 =>Vx are moving liquid like, R≠O, Flux flow regime
    Third harmonic signal arise from flux line tension (affects the e- inside the Cu coil),
    It does not depend on dissipation inside Nb, BUT depends on # of Vx trapped there (and length).
maximum field without Vx (max Eacc)
maximum pinning
flux line moving in AC field
Vx pinned in the SC

## Slide 9: Nb – Insulator – NbN model
  NbN coating by Magnetron Sputtering
  NbN single layers series
    NbN SL / “thick” Nb layer
      Magnetron sputtered
      MgO as dielectric layer
    Far from perfect…
Nb (nm) | MgO (nm) Calc(actual) | NbN (nm) Calc(actual) | TC (K)
250† | 14 | 0 | 8.9
250† | 14 | 25 | 15.5
500 | 10 (10.3) | 50 (65) | 15*
500 | 10 (8.4) | 75 (72) | 14.1*
500 | 10 (9.8) | 100 (94) | 14*
500 | 10 | 125 | 14.3*
500 | 10 (6.7) | 150 (132) | 15.9*
500 | 10 (10.4) | 200 (164) | 15*
† Not same batch, deposited on the same conditions, but substrate = sapphire
*As determined with magnetometry, see below.

## Slide 10: Sputtered (defective) materials…
  Typical defects…
    Low HC1
    Thickness ≠ uniform
    …
Nb Thickness ~ 425nm
| PAGE 10
250 nm Nb on saphire
DC Squid magnetometry @ 4.5 K
~ 18 mT
As expected for MS samples
    NbN 100nm
NbN Thickness ~ 105nm
    NbN 50nm
Rippled interfaces

## Slide 11: Far from perfect….
  Morphology
    Rough surface
    NbN 50 nm
    NbN 200 nm
    NbN 100 nm
    MgO needle ? (capping material)

## Slide 12: Comparaison with theory
x
x
x
x
x
x
Nb with defects*, with BC1=50 mT
* e.g. morphologic defects that allow earlier vortex penetration See SST paper cited earlier
Ideal Nb substrate with BC1=170 mT
x
x
x
x
x
x
  Theoritical predictions from T. Kubo (KEK)
  The enhancement of the field penetration increases with thickness of NbN
  It reaches a saturation at thicknesses > 100 nm

## Slide 13: Comparaison with theory
x
x
x
x
x
x
Nb with defects*, with BC1=50 mT
* e.g. morphologic defects that allow earlier vortex penetration See SST paper cited earlier
Ideal Nb substrate with BC1=170 mT
x
x
x
x
x
x
  Theoritical predictions from T. Kubo (KEK)
  The enhancement of the field penetration increases with thickness of NbN
  It reaches a saturation at thicknesses > 100 nm

## Slide 14: CLOSEUP OF 3rd HARMONIC SIGNAL
Voltage signal
Phase signal
1
2
T~T
T >>T
  For a given Happl, we observe 3 ≠ transition temperatures
3
    T~T: within noise level
    T >>T: dramatic transition

## Slide 15: ROLE OF THE DIELECTRIC LAYER !
Thin SC layer NbN
Insulator MgO
Thick SC layer Nb
      H // surface => surface barrier†
      A defect locally weakens the surface barrier
      1st transition, vortex blocked by the insulator ~100 nm => low dissipation.
      2nd transition, propagation of vortex avalanches (~100 µm) => high dissipation.
      Dielectric layer = efficient protection !!!
†B. Bean and J. D. Livingston, Phys. Rev. Lett. 12, 14 (1964).
  Why do we have two transitions ?
Defect
H app
Field lines
First transition
Second transition

## Slide 16: HC1 (Eaccmax) and RS (Q0max) estimation
  RF test (collaboration IPNO)
  Local magnetometry:
Notes: Pas possible de mesurer direct sur une cavité (on ne sait pas encore déposer de telles structures sur des formes complexes)
On mesure indirectement
Par magnétométrie : le champ de transition limite (donne une estimation du champ acc maximum)
Par cavité TE011 (5,88 GHz) : la Rs à bas champ (donne une estimation du Q0)
Magnétométrie : Les résultats au dessus de la ligne orange sont à prendre avec des précautions. On espère les confirmer avec les développements prévus cette année (bobine + petite ou échantillons plus grands)
RF La grande inconnue de ces multi couche c’était la résistance résiduelle qui aurait pu s’avérer monstrueuse et mettre tout par terre. Le premier échantillon, très rugueux présentait une résistance résiduelle seulement 5 fois plus grande que celle du Nb, le deuxième beaucoup + lisse est quasiment identique à celle du Nb . Dans ces échantillons la moitié du courant seulement passe dans les couches, l’autre moitié dans le Nb… on a donc bon espoir de faire beaucoup mieux

## Slide 17: Conclusion and outlook
  Scientifically:
    Very challenging upstream, discovery, R&D
    Efficiency of multilayer concept demonstrated
    Field enhancement => higher SRF performances
    Protection against “avalanches” => can accommodate defective (real) material
    Results close from theory => will help optimization
  Future :
    Developing deposition techniques e.g. ALD, ECR, HPIMS….
    Up-grade of existing Nb cavities
  Change of paradigm in SRF technology at hand

## Slide 18: THANK YOU FOR YOUR ATTENTION

## Slide 19: TiO2 .Atomic layer deposition
Extract from http://www.youtube.com/watch?feature=player_detailpage&v=XMda8TXLIFk

## Slide 20: What do we measure ?
Determination of Hc1
  Low field => one transition
  High field => two transitions
    1st transition with low dissipation
    2nd transition very strong dissipation
Why do we have two transitions ?
1st transition
2nd transition
H = 25 mT
H = 7 mT
NbN 200nm

## Slide 21: What kind of defects ?
Morphologic defects (pores, steps, facets…)
Site with depressed superconductivity (NC, SC but local change of k, x...)
~1 µm
~1 nm
Micro- to nano-roughness (go to fractal approach ?)
Crystalline defects :
Interfaces (inclusions) > GB > cells > (=dislocations) > vacancies or interstitials




°
.

3D
0D
2D
1D
Strain on the crystalline lattice
Plays on l, k...
Early penetration / Flux trapping => same battle!!!

## Slide 22: Why bulk niobium ?
  Bulk Niobium:
      grains >~ 50 µm to mms, good crystallographic quality
  Niobium ~1-5 µm/Copper :
       <~ 100 nm, many crystallographic defects, grain boundaries…
      sometimes better low field performance (thermal configuration and/or cost)
  It is changing !!!: New emerging thin films techniques
Typical sputtered Nb cavities
1.5 GHz
Typical Good bulk Nb cavity
1.3 GHz

## Slide 23: Nb-MgO-NbN trilayers
  Transition field (HSH here ?)
  NbN single layers series
    NbN SL / “thick” Nb layer
      Magnetron sputtered
      MgO as dielectric layer
  The enhancement of the field penetration increases with thickness of NbN
  It reaches a saturation at thicknesses > 100 nm
Saturation ?
Maybe it is still worth trying to go to thicker samples
Maybe this sample quality is not good !

## Slide 24: SRF R&D @ CEA Saclay: Layout
Polishing
  Chemical polishing / Electropolishing
  Damage layer / Mechanical polishing
Characterization tools
  Local magnetometry
  Point contact Tunneling
  Cp measurement
Future superconductors
  ALD/Doping studies
  Multilayers
Miscealenous
  Quench location
  Flux trapping studies
Notes: Longueurs caractéristiques x0, l0, l
<< x : GL Linéarisées
éléments de la théorie BCS
Comportement résistif en AC/RF
Longueurs caractéristiques x0, l0, l
ℓ<< x : GL Linéarisées
éléments de la théorie BCS
Comportement résistif en AC/RF