## Slide 1: High-Q and high-gradient research updates from Cornell University
Dr. Mingqi Ge
On behalf of the SRF group of Cornell University
ALCW2018
May 31, 2018

## Slide 2: Outline
Vertical electropolishing (VEP) updates
Bipolar electropolishing (BEP) updates
Low-temperature doping updates

## Slide 3: Outline
Vertical electropolishing (VEP) updates
Bipolar electropolishing (BEP) updates
Low-temperature doping updates

## Slide 4: Motivation of Vertical Electropolishing
VEP has lower cost compared to horizontal EP;
VEP requires smaller space for the system set-up;
VEP’d SRF cavities have similar performance compared with HEP’d cavities.

## Slide 5
Cornell VEP system for the ILC R&D project
(high-gradient research)
ILC spec. @ 2K
Cornell Vertical electropolished 9-cell and single-cell SRF cavities achieved the ILC specification at 2K (Eacc >35MV/m with Q0>0.8e10)
Cornell VEP for 9-cell set-up
@ 2K

## Slide 6
Cornell VEP system for the LCLS-II R&D project
(high-Q0 research)
The nitrogen-doped 9-cell and single-cell SRF cavities after VEP all achieved the LCLS-II specification (Eacc>16MV/m , Q0>2.7e10 at 2K)
LCLS-II spec. @ 2K

## Slide 7
Chart: Before flip
| 9.0 | 9.0 | 8.0 | 8.0 | 7.0 | 7.0 | 6.0 | 6.0 | 5.0 | 5.0 | 4.0 | 4.0 | 3.0 | 3.0 | 2.0 | 2.0 | 1.0 | 1.0
eq | 36 | 48 | 60 | 64 | 70 | 88 | 78 | 80 | 94
iris | 40 | 56 | 84 | 94 | 100 | 100
Chart: After flip
| 9.0 | 9.0 | 8.0 | 8.0 | 7.0 | 7.0 | 6.0 | 6.0 | 5.0 | 5.0 | 4.0 | 4.0 | 3.0 | 3.0 | 2.0 | 2.0 | 1.0 | 1.0
eq | 82 | 82 | 112 | 94 | 114 | 110 | 108 | 110 | 108 | 106 | 108 | 124 | 94 | 120 | 88 | 108 | 84 | 122
Gravity effect causes VEP removal un-uniform;
Cavity has to be flipped in a VEP;
Ninja Cathode has been designed to compensate the removal un-uniform;
Equator : 104±14um
Motivation of Ninja cathode development
(collaborated with KEK and Marui)
Cell number
Cell number
Removal (um)
Removal (um)
Iris ave.;
Iris ave.;
Eq. ave.;
Eq. ave.;
Upper half cell
lower half cell
top
Chart: 
| 9.0 | 9.0 | 8.0 | 8.0 | 7.0 | 7.0 | 6.0 | 6.0 | 5.0 | 5.0 | 4.0 | 4.0 | 3.0 | 3.0 | 2.0 | 2.0 | 1.0 | 1.0
eq | 30 | 28 | 36 | 42 | 38 | 36 | 52 | 44 | 46
iris | 30 | 28 | 32 | 34 | 32 | 40 | 44
Upper
Lower

## Slide 8
Ninja cathode development in collaboration with KEK and Marui
Surface preparation of NR1-2:
NR1-2: CBP (30μm)+BCP (60μm)+800C baking (2hrs),
Two VEPs (20μm each) using the Ninja cathodes of type-I & II,
120C baking (48hrs) and RF test,
NR1-2 treated by the Ninja cathode achieved the ILC spec.
ILC spec. @ 2K

## Slide 9: Outline
Vertical electropolishing (VEP) updates
Bipolar electropolishing (BEP) updates
Low-temperature doping updates

## Slide 10: Motivation of Bipolar-EP
Regular EP contains HF.
HF is toxic !
Regular EP will require >10,000 liters HF acid for ILC project (~8000 1.3GHz 9-cell SRF cavities).

## Slide 11
Bipolar-EP development collaborated with Faraday Inc.
(HF-free EP technique using H2SO4 acid)
an anodic forward pulse to grow an oxide layer on niobium surface,
voltage time off to dissipate the heat, remove reaction products, and replenishes reacting species;
a cathodic pulse with reversed voltage to remove the oxide layer on the niobium surface, thus eliminating the need for HF.
BEP setup of 9-cell and single-cell SRF cavities

## Slide 12
9-cell cavity BEP results
Surface coated with thick and golden oxide layer after 63um BEP of the 9-cell cavity.
No 800C and 120C baking after BEP
Optical inspection images:
1st Run:
2nd Run: BEP 8.5um, surface looks similar to the conventional EP surface;
3rd Run: BEP 7um, surface has light yellow layer.
Baseline test: cavity quenched at 22MV/m,
BEP degraded gradient ~ 4MV/m,
Gradient was limited by quench and FE,
Low Q0 due to the oxide layer on surface.
Quench
FE
Max Eacc in baseline test

## Slide 13: Surface resistance analysis of the 9-cell cavity results
BCS resistance (RBCS) is ~10-15 which is regular to a normal VEP
Residual resistance (R0) has large scattering from 8 to 41 .

## Slide 14
Single-cell cavity-string BEP results
Optical Inspection comparison
Cornell VEP
BEP
(BEP 64um; no 800C and 120C baking)
Baseline test: Eacc ~20MV/m limited by quench,
BEP improved two single-cell Eacc up to ~40MV/m,
Q0 is flat when Eacc is between 5-30MV/m,
high-field Q-slope started after 30MV/m.
ILC spec. @ 2K
Max Eacc in baseline test

## Slide 15
Post treatment study after BEP
HF rinsing to remove bad oxide layer;
120C baking to improve Q
LET1-14:
120C baking: Q0 degraded at low, medium fields; no change at high fields. Eacc~ 40MV/m.
HF rinsing: Q0 was improve at low fields; no change at high fields. Eacc~ 40MV/m.
LET1-15:
HF rinsing: Q0 was improved at low, medium fields; no change at high fields. Eacc~ 40MV/m.
120C baking : Q0 was improve at low fields; no high-field Q-slope. Eacc quenched at 38MV/m.
ILC spec. @ 2K
ILC spec. @ 2K

## Slide 16: Conclusions of BEP study
Gradient of the BEP’d cavities can achieve ~40MV/m,
Q0 varies from ~8e9 to 1.2e10 based on BEP parameters,
The post treatments can reduce surface resistance of BEP’d cavity down to conventional VEP level.

## Slide 17: Outline
Vertical electropolishing (VEP) updates
Bipolar electropolishing (BEP) updates
Low-temperature doping updates

## Slide 18: Motivation of Low-temperature doping
High-temperature (800C) doping cavity has high-Q, but gradient of most cavities does not achieve the ILC specification;
Low-temperature (120-160C) doping might be a solution for producing high-Q and high-gradient cavities.
ILC spec. @ 2K
Average quench field: ~20MV/m

## Slide 19: Low-temperature doping at Cornell

## Slide 20: One more thing…

## Slide 21: Latest results of 2.6GHz Nitrogen-doped single-cell SRF cavity
2/6 Doping recipe;
Q-value is comparable with a 1.3GHz EP’d cavity (non-doped);
RBCS ~11 nΩ at 16MV/m;
R0 ~ 8 nΩ
Epk/Eacc = 1.86
Bpk/Eacc = 4.25 mT/ (MV/m)
1.3GHz
2.6 GHz
@ 2K, Q0 > 1e10 at 16MV/m
M. Martinello et al., SRF2017, Lanzhou, China, 2017.
1.3 GHz cavity need Q0> 3e10 at 2K to obtain same cryogenic loss per length.
Q0=1.5e10

## Slide 22: Cornell SRF group: P. Bishop, H. Conklin, F. Furuta, T. Gruber, A. Holic, J. Kaufman, P. Koufalis, G. Kulina, M. Liepe, J. Maniscalco, T. Oseroff, R. Porter, J. Sears, S. Zeryck.
Acknowledgement
Thanks for your attention!

## Slide 23: Surface resistance analysis of low T doping results