## Slide 1: Status and expected progress on SRF cavities
| Réunion d'information ILC -9avril 2018
C. Z. Antoine

## Slide 2: INTRoduction SRF limits

## Slide 3: Ultimate limits in SRF-1
Niobium cavities
  Performances
    Eacc  HRF
    Q0 ( 1/RS)  TC => Nb3Sn, MgB2, NbN…
    Limit = magnetic transition of the SC material @ Hpeak
  Superconductivity only needed inside :
    Thickness ~ < 1 µm => thin films
    (onto a thermally conductive, mechanically resistant material, e.g. Cu)
  Today :
    Thin films exhibit too many defects
    Only Bulk Nb has high SRF performances
  Issues : getting “defect free” superconductors (yes but not all defects are detrimental…)
H field mapping in an elliptical cavity
HPeak
0
HMax.

## Slide 4: Ultimate limits in SRF-2
H
T
HC1
HC2
TC
Mixed state w.Vortex
(i.e. N. cond. flux line + screening currents)
Screening current over l, no magnetic field deeper
Meissner state
  SC phase diagram
    All SC applications except SRF: mixed state w. vortex
    Vortices dissipate in RF !
    SRF => Meissner state mandatory !
    HC1 = limit Meissner/mixed state
    Nb: highest HC1 (180 mT)
    “Superheating field”(?) :
  Metastable state favored by H // to surface
    Difficult to get in real life !

## Slide 5: What is the limit (Hp/HC1/HSH) ?
  Real world cavities behavior is dominated by a few number of defects
  It is very important to measure the penetration field of samples in realistic conditions
T2
T2C
HC1
HSH
H
H//
H
T2
T2C
HC1
HSH
H
H//
H
  ~100 µm in 1 ns (~RF period)
  Compare with l (field penetration depth)
    Nb : ~ 40 nm
    MgB2 ~ 200 nm
  Avalanche : high RF dissipation
MgB2: http://www.nature.com/srep/2012/121126/srep00886/full/srep00886.html?message-global=remove&WT.ec_id=SREP-20121127

## Slide 6: EFFECTs of local defects
  Vortices enter more easily at lower temperature (counter intuitive !)?
    @ T~TC : H is low => low dissipations => easy to thermally stabilize
    @ T<<TC : H is high=> even if small defect => high dissipations => Favors flux jumps
Dissipations :
=> We have to reduce defect density (yes but which ones?)
Nb3Sn
HC1Nb3Sn (~27mT)
(50 mT pour le bulk)
Recent results from Cornell CW (Posen, 2015 (17 MV/m))
Cornell, 1997
pulsed
Nb HC1
(170 à 200 mT)
HSHNb3Sn
(~ 400 mT @ 0 K)
Hays. "Measuring the RF critical field of Pb, Nb, NbSn". in SRF 97. 1997.
~ 2K

## Slide 7: Bulk Niobium Present status

## Slide 8: Typical production scores for 9-cells
https://agenda.linearcollider.org/event/7645/contributions/40185/attachments/32340/49084/Pekeler_XFEL-CavityProduction_ResearchInstruments.pdf
https://www.google.fr/url?sa=t&rct=j&q=&esrc=s&source=web&cd=1&cad=rja&uact=8&ved=0ahUKEwjH57Di8qzaAhULuRQKHbUeBh4QFggsMAA&url=https%3A%2F%2Fwww.sciencedirect.com%2Fscience%2Farticle%2Fpii%2FS0168900214013977&usg=AOvVaw2_X7xJ6spZFAA0bhvMpfxf
Polycrystalline bulk Nb
Large graine bulk Nb

## Slide 9: Reducing cost
Many trails explored…
  Large grain material
    Economy in Nb Weigth
  Nitrogen (Oxygen ?) doping/infusion
    Today Nb is optimized for thermal conduction (stabilization), not for superconductivity
    Modification of the surface without loosing the bulk properties
  Multilayer :
    Route to realistic material with higher Q0 and Eacc (and even defects)
    Protection against vortex avalanche
  Getting rid of the damage layer
    Only explored at lab level

## Slide 10: Large grain material

## Slide 11: Typical sheet preparation
15-20 steps

## Slide 12: large grain disk preparation
[Saito, 2007]
8 steps
  Economy in weigth:
  ≠ ~ 6 Kg/ 9-cell
  ~ 3 k€ / 9-cell (compare w. 20 k€)
  ~ 15% of the cost

## Slide 13: Large grain forming
[Singer, 2008]
=> a lot of forming failure
=> a whole new industrial process need to be developed
But….
  Non uniform forming
  asymmetric deformation
  risk of tearing (irises)
  risk of holes during welding
  larges steps @ GB

## Slide 14: Large grain conclusion
  RF performances : ~ same as smaller grain cavities
      Medium Q ~ a little better for EP cavities
  Savings for (very) large Nb sheet production (small elliptical cavities only)
      Less fabrication steps
      Ingot => disks : no losses of material in the corners
      High purity material with intrinsically good crystalline quality
      But not fitted for  > 30 cm (typical ingot )
  Increased costs and delay for Cavity forming
      More fabrication steps, higher failure risks
      Large cost savings on material, …might be lost on fabrication

## Slide 15: Nitrogen (Oxygen ?) doping/infusion

## Slide 16: Baking/doping/infusion what is the difference?
(l  RRR)
Bulk Nb
Nb/Cu
4,5 K
  N doping
  high temperature annealing (oxide disappears)
  high temperature N2 => degradation
  EP (~80 µm) => very high Q0, but Eacc ↓↓
  At 1rst order : modification of m.f.p. l
  Not For ILC !!!
  Not necessarily related to N
  Very well recrystallized material @ Saclay in 2001
T~ 2K ?
≡ 5-6 x1010 @ 2 K

## Slide 17: Effect of temp on
https://arxiv.org/pdf/physics/0401141.pdf

## Slide 18: Baking/doping/infusion what is the difference?
  Baking
  120 °C, 48 h => oxide degrades, Oi diffuses ~100 nm
  Change in mean free path => better RS
  prevents hydride precipitation ?
  N infusion
  800°C annealing (oxide disappears)
  120 °C, 48 h in presence of N2 => Ni diffuses ~10 nm
  Change in mean free path => better RS
  prevents hydride precipitation ?

## Slide 19: Issues
Martinello et al, FNAL
Gonella et al, CORNELL U.
~10 nm => interstitials
~100 nm => dislocation cells
      Related to crystalline sub-structure, not specified/monitored yet
  Variability lab to lab
  Same recipe, but not same results,
  Needs adaptation : high temperature treatment ≠
  Higher sensitivity to trap flux
  Upon cooldown if ⱻ defects, magnetic remnant flux gets trapped
  very high surf resistance in RF !

## Slide 20: Multilayers

## Slide 21: After niobium : nanocomposites multilayers
  Dielectric layer
    Small  vortex (short -> low dissipation)
    Quickly coalesce (w. RF)
    Blocks avalanche penetration
    => Multilayer concept for RF application
  Nanometric I/S/I/ layers deposited on Nb
    SC nanometric layers ( 100 nm) => HC1 => Vortex enter at higher field
    Nb surface screening => allows high magnetic field inside the cavity => higher Eacc
    SC w. high TC than Nb (e.g. NbN): => Q0multi >> Q0Nb
Structures proposed by A. Gurevich in 2006, SRF tailored
Cavity's internal surface
→
Happlied //
HNb
S-I-S
dsc
Notes: A. Gurevich, "Enhancement of RF breakdown field of SC by multilayer coating". Appl. Phys.Lett., 2006. 88: p. 12511.
Couche fine : pas favorable énergétiquement à la nucléation d’un vortex => augmentation artificielle du HC1.
Couches trop fines pour écranter totalement le champ, seulement atténuation : il en faut plusieurs => structures à optimiser

## Slide 22: What is the limit (Hp/HC1/HSH) ?
  Real world cavities behavior is dominated by a few number of defects
  It is very important to measure the penetration field of samples in realistic conditions
T2
T2C
HC1
HSH
H
H//
H
T2
T2C
HC1
HSH
H
H//
H
  Local magnetometry
    ~ Same geometry as cavities
    No shape/edge effect (vs DC/ Squid magnetometry)
    No demagnetization effect
    Measures actual penetration field wherever it is HP/HC1/HSH

## Slide 23: Experimental Details
T
TC
HC1
HMelting
H
HC2
Ia/Ha
Meissner state
Vx lattice
Vx ~ liquid
  Low frequency ≡ DC :
    0 < Ha< HC1 => R=O, Meissner state
    HC1< Ha< HM =>Vx are trapped, R=O, Campbell regime
    HM< Ha< HC2 =>Vx are moving liquid like, R≠O, Flux flow regime
    Third harmonic signal arise from flux line tension (affects the e- inside the Cu coil),
    It does not depend on dissipation inside Nb, BUT depends on # of Vx trapped there (and length).
maximum field without Vx (max Eacc)
maximum pinning
flux line moving in AC field
Vx pinned in the SC

## Slide 24: Nb – Insulator – NbN model
  NbN coating by Magnetron Sputtering
  NbN single layers series
    NbN SL / “thick” Nb layer
      Magnetron sputtered
      MgO as dielectric layer
    Far from perfect…
Nb (nm) | MgO (nm) Calc(actual) | NbN (nm) Calc(actual) | TC (K)
250† | 14 | 0 | 8.9
250† | 14 | 25 | 15.5
500 | 10 (10.3) | 50 (65) | 15*
500 | 10 (8.4) | 75 (72) | 14.1*
500 | 10 (9.8) | 100 (94) | 14*
500 | 10 | 125 | 14.3*
500 | 10 (6.7) | 150 (132) | 15.9*
500 | 10 (10.4) | 200 (164) | 15*
† Not same batch, deposited on the same conditions, but substrate = sapphire
*As determined with magnetometry, see below.

## Slide 25: Sputtered (defective) materials…
  Typical defects…
    Low HC1
    Thickness ≠ uniform
    …
Nb Thickness ~ 425nm
| PAGE 25
250 nm Nb on saphire
DC Squid magnetometry @ 4.5 K
~ 18 mT
As expected for MS samples
    NbN 100nm
NbN Thickness ~ 105nm
    NbN 50nm
Rippled interfaces

## Slide 26: Far from perfect….
  Morphology
    Rough surface
    NbN 50 nm
    NbN 200 nm
    NbN 100 nm
    MgO needle ? (capping material)

## Slide 27: Comparaison with theory
x
x
x
x
x
x
Nb with defects*, with BC1=50 mT
* e.g. morphologic defects that allow earlier vortex penetration See SST paper cited earlier
Ideal Nb substrate with BC1=170 mT
x
x
x
x
x
x
  Theoritical predictions from T. Kubo (KEK)
  The enhancement of the field penetration increases with thickness of NbN
  It reaches a saturation at thicknesses > 100 nm

## Slide 28: Comparaison with theory
x
x
x
x
x
x
Nb with defects*, with BC1=50 mT
* e.g. morphologic defects that allow earlier vortex penetration See SST paper cited earlier
Ideal Nb substrate with BC1=170 mT
x
x
x
x
x
x
  Theoritical predictions from T. Kubo (KEK)
  The enhancement of the field penetration increases with thickness of NbN
  It reaches a saturation at thicknesses > 100 nm

## Slide 29: CLOSEUP OF 3rd HARMONIC SIGNAL
Voltage signal
Phase signal
1
2
T~T
T >>T
  For a given Happl, we observe 3 ≠ transition temperatures
3
    T~T: within noise level
    T >>T: dramatic transition

## Slide 30: ROLE OF THE DIELECTRIC LAYER !
Thin SC layer NbN
Insulator MgO
Thick SC layer Nb
      H // surface => surface barrier†
      A defect locally weakens the surface barrier
      1st transition, vortex blocked by the insulator ~100 nm => low dissipation.
      2nd transition, propagation of vortex avalanches (~100 µm) => high dissipation.
      Dielectric layer = efficient protection !!!
†B. Bean and J. D. Livingston, Phys. Rev. Lett. 12, 14 (1964).
  Why do we have two transitions ?
Defect
H app
Field lines
First transition
Second transition

## Slide 31: HC1 (Eaccmax) and RS (Q0max) estimation
  RF test (collaboration IPNO)
  Local magnetometry:
Notes: Pas possible de mesurer direct sur une cavité (on ne sait pas encore déposer de telles structures sur des formes complexes)
On mesure indirectement
Par magnétométrie : le champ de transition limite (donne une estimation du champ acc maximum)
Par cavité TE011 (5,88 GHz) : la Rs à bas champ (donne une estimation du Q0)
Magnétométrie : Les résultats au dessus de la ligne orange sont à prendre avec des précautions. On espère les confirmer avec les développements prévus cette année (bobine + petite ou échantillons plus grands)
RF La grande inconnue de ces multi couche c’était la résistance résiduelle qui aurait pu s’avérer monstrueuse et mettre tout par terre. Le premier échantillon, très rugueux présentait une résistance résiduelle seulement 5 fois plus grande que celle du Nb, le deuxième beaucoup + lisse est quasiment identique à celle du Nb . Dans ces échantillons la moitié du courant seulement passe dans les couches, l’autre moitié dans le Nb… on a donc bon espoir de faire beaucoup mieux

## Slide 32: Dammage layer

## Slide 33: Damage layer / rolling
  High dislocation density (damage) incriminated in:
    Apparition of hot spots on operating cavities
    High density of hydride precipitates
    High sensitivity to trapped flux
  Damage layer seems to essentially originate from rolling
    Surface texture resistant to recrystallization
    Not fully eliminated after 150µm removal (patchy nature)
  Postulate :
    Strain left by forming and welding can be easily removed by recrystallization treatment
    => mechanical polishing of flat sheet easy and inexpensive !!!
Finite element simulation of 2% reduction of 3.5 mm sheet with 1 cm diameter rolls (Courtesy Non-Linear Engineering, L.L.C.).
[R. Crook et al, Black Laboratory] &
http://accelconf.web.cern.ch/AccelConf/srf2009/posters/tuppo071_poster.pdf
NB : in case of billet slicing damage layer is ≠ and needs to be assessed

## Slide 34: Damage as seen by electron diffraction
200 µm
Surface of the sheet
a) As received
b) After 2 steps polishing 20 + 25 min
(300 µm removed)
20 µm
UGC
c) After forming
New damage layer < 1µm
Core of the sheet
Polishing on flat surface is quick and easy.
Mechanical chemical preparation inspired from metallographic polishing can produce damage layer 100 nm
Notes: Sheet cuts , prepared with metallographic polishing (5 steps,  damage <<100 nm)

## Slide 35: Conclusion and outlook
  Production already asserted to produce specification
  Reducing cost R&D :
    Today limited to only 2 directions : large grain and N infusion
    Already promising
    Physics not fully understood => risks
  Longer term R&D
    Promising trails for improvement also exist
    better control of the material production is required

## Slide 36: THANK YOU FOR YOUR ATTENTION

## Slide 37: What do we measure ?
Determination of Hc1
  Low field => one transition
  High field => two transitions
    1st transition with low dissipation
    2nd transition very strong dissipation
Why do we have two transitions ?
1st transition
2nd transition
H = 25 mT
H = 7 mT
NbN 200nm