## Slide 1: CLIC Fabrication
Joel Sauza Bedolla1,2
On behalf of the X-Band Production Team
1Lancaster University Engineering Department: Graeme Burt
2CERN, BE-RF Section: Nuria Catalan Lasheras
International Workshop on Future Linear Colliders (LCWS19), Sendai, Japan
30/10/2019

## Slide 2: Summary
CLIC fabrication in a nutshell
Discs
  TD26 Prototype
  TD31 Prototype
  Diffusion bonding issues
Other technical solutions
  Halves
  Rectangular discs
Conclusions

## Slide 3: CLIC Fabrication in a nutshell
RF design
Mechanical design
Manufacturing
Quality
Assembly
High Power Test
3D Models
Detailed design
Ultra Precise
Milling and Turning
Physics
HFSS
Diffusion bonding
Brazing
Xboxes
Metrology
Bead-Pull

## Slide 4: TD26
N1
Post-Mortem
More details on bonding issues section
N2
Waiting High Power test
N3
Waiting High power test
N4
Assembly on-going
More details next slide
Tuned
Baked
Tuned
Unbaked

## Slide 5: TD26-N4
Brazing of cooling blocks and waveguides
Brazing of tuning pins
Diffusion bonding executed at TMD technologies (UK)
  1040 °C x 1h 30 min x 0.06MPa x H2

## Slide 6: TD31
N1
Assembly on-going
Bonding completed
Brazing on-going
N2
Assembly on-going
Bonding completed Brazing on-going
N3
Manufacturing completed
N4
Manufacturing completed
New tooling tested
New tooling tested
Baseline for CLIC-380GeV

## Slide 7: TD31
Bead Pull measurements before bonding are better than we usually see. Phase advance (N1) nearly fulfils the requirements after tuning.
Due to extremely good quality
Also due to the good alignment and RF contact of the tooling.
140 discs produced. 0 defects

## Slide 8: TD31 – N1 and N2
No banana effect
Reduced disc to disc alignment
Straightness: 15 µm
N2
Diffusion bonding executed at Bodycote (FR)
  1040 °C x 1h 30 min x 0.06MPa x H2
Straightness: 46 µm
A bump during transport
No banana effect
Reduced disc to disc alignment
N1

## Slide 9: Diffusion bonding issues
The process is stable and it works
  The structures are leak-tight!
  We have some issues with straightness but the main cause is the transport from the assembly table to the furnace.
Two years ago, it was decided to assess the contribution of diffusion bonding
  Careful attention to metrology
  Cross-check with Bead-Pull Measurements
  Post-mortem analysis
1040 °C
1h 30 min
0.06 MPa
H2
Optimization

## Slide 10: Diffusion bonding issues
Identical bonding cycles on different days (same supplier) for TD26 N1, N2 and N3.
N4 different supplier (diameter after bonding was not measured)
External diameter reduction in average 12 µm
Observed in structures N1, N2 and N3. Double checked on structure N1.
The total length of the structure is smaller 25 µm
10 µm external diameter
Copper sublimation
Is the iris bigger?
Have the noses change?
Internal Volume change
Is there a frequency change?
RF Change

## Slide 11: Diffusion bonding issues
Bonding of TD31 N1 and N2 performed by the same supplier (TD26-N1-N2-N3).
However, the oven has been completely refurbished in-between.
Same trend than TD26: diameter reduction in average 11 µm

## Slide 12: TD26-1
Post-Mortem analysis
Cutting plan (EDM):
  Same reference for all the discs
  Shape of the nose (horizontal)
  Shape of the nose (vertical)
  Irises
  Flatness of the waveguide
G00
G01
G02
G03
G14
G15
G16
Already performed
Contamination from cutting

## Slide 13: TD26-1: Shape of the nose (horizontal)
Datum references have changed with respect to original measurements.
Shape seemed to improve according to disc position. G00 is worst than G02
First traces of EDM cutting residuals observed on G03

## Slide 14: TD26-1: Shape of the nose (vertical)
A cone shape is observed
The error was diminishing up to G03
Contamination of EDM cutting on G14
G01
15 µm

## Slide 15: Halves
Long development process:
  First trial (bonding - CERN): Good RF before bonding. After boding, a gap between the halves (10-200 µm) and a shift between the irises of 70 µm (systematic error)
  Second trial (brazed – SLAC): A gap between irises was introduced to minimize field of filling material leaking to the structure. Alignment with pins. RF conditioning ok. Breakdown activity near the brazing region.
  A third trial (brazed through irises – SLAC): not yet tested but there is a visual misalignment between the irises.

## Slide 16: Halves
Last development TD26:
  Two identical halves: 285 mm x 146 mm x 14 mm, damped (no SiC), gap.
Form tolerance: 4 µm on Zone A (zone near the iris of the whole length)
Electron beam welding design:
  Hard copper (no heat treatments above 245 °C) showed shorter RF conditioning
  Welding lips
Less components to assembly but bigger risks for manufacturing companies
  Challenging but feasible

## Slide 17: Halves
We do care about the alignment. Special tooling: Herzian deformation of high precision rings.
Ready to be produced!

## Slide 18: Rectangular discs
First trial successful at 95% (it was leaking)
  Caused by the SiC geometry
  Not related to the bonding problem: the SiC was copper coated.
Second trial successful at 99% (it was not leaking)

## Slide 19: Rectangular discs
Lancaster University PROton Boosting Extension (PROBE) structure
High gradient (54 MV/m), side coupled, standing wave, S-Band for Proton Computed Tomography (pCT) scan
Bonding done. Leak test after brazing of components.
Straightness of 25 µm

## Slide 20: Conclusions
TD26:
  N1: Post-mortem finished
  N4: Brazing operations on-going
TD31
  N1 and N2: Brazing operation on-going
Bonding issues:
  The diameter reduction (copper sublimation) of 10 µm is confirmed: 6 structures
  The shape of the nose is changing on both horizontal (collapsing) and vertical shapes (cone shape)
  The cells are deforming due to bonding
    Weight is excessive? Already reduced from 0.1 MPa to 0.06 MPa
    Temperature is too high?
    Time is too long?
Halves: Ready for production
Rectangular discs: Bonding performed on the PROBE structure. Leak test in following weeks.

## Slide 21: Thank you
Questions?