## Slide 1: Update on Progress of Vertical EP at Marui and KEK
International Workshop on Future Linear Colliders
(LCWS2019)
31st October 2019
Vijay Chouhan
Marui Galvanizing Co. Ltd/KEK
Y. Ida, K. Nii, T. Yamaguchi (Marui)
H. Hayano, S. Kato, M. Monjushiro, T. Saeki, M. Sawabe (KEK)
H. Ito (Sokendai)
H. Oikawa (Utsunomiya University)

## Slide 2: Contents
Introduction of Horizontal and Vertical Electropolishing (EP)
VEP Results of Single-Cell Cavity
Parametric Study with 9-Cell Cavity
VEP Results of 9-Cell Cavity
Summary & Future Work

## Slide 3: Horizontal & Vertical Electropolishing
Horizontal EP (HEP): Cavity in horizontal position during the EP process
Vertical EP (VEP): Cavity in vertical position during the EP process
VEP is performed with a simple setup.
Massive Horizontal EP Setup with Rotating Cavity
Turning of EP bed
Vertical EP at Marui

## Slide 4: 1.3 GHz Single and Nine-Cell Coupon Cavities
Measurable coupon current, in-situ observation, post VEP surface analysis
Single-Cell Coupon Cavity
Nine-Cell Coupon Cavity

## Slide 5
We have applied several models of Ninja cathodes to find an optimized structure and VEP parameters.
Metal Wings (Ver-1)
Insulating Wings (Ver-2)
Partial Metal Wings (Ver-3)
Insulating Wings + Large Cathode Surface Area + Meshed Cover (Ver-5)
Ninja cathode is inserted in the cavity and then its blades are expanded.
Ninja cathode v5: Enhanced cathode surface area, cathode housing covered with meshed sheet, insulating wings
Optimized Design of Unique Ninja Cathode
The cathode is rotated during the VEP process.

## Slide 6: VEP with Conventional Rod Cathode
Major Issues in VEP:
Non-uniform removal
Rough surface/Bubble traces
The higher removal at the top iris is due to accumulation of H2 gas bubble on the surface.
It was confirmed with lab EP experiments.
Coupon Currents
Higher EP current at the upper half cell
Removal Trend
Top Iris Viewport
Acid flow rate ~ 5L/min
Voltage ~9 V
Current Density (mA/cm2)
Elapsed Time (min)
Top Iris
Bottom Iris
Bubble Footprints at Upper Iris
500 µm
V. Chouhan et al., Phys. Rev. Accel. Beams 20, (2017) 083502

## Slide 7: VEP with Ninja Cathode
The cathode and optimized parameters yield smooth surface and symmetric removal.
Hence, the cathode was opted for further VEP and RF tests.
Meshed housing guides hydrogen bubbles along the cathode and reduces bubble accumulation in the cavity cell
Cathode rotation might make uniform flow on the surface
Larger cathode surface reduces cathode screening by bubbles
Voltage: ~13 V, Acid flow rate: ~5 L/min, Cathode rotation: 20 rpm, Temperature < 20 ºC, Cavity cooling by water spray
Removal Thickness
At 20 rpm
Optical Images
Top Iris
Equator
Bottom Iris
200 µm
Current Density (mA/cm2)
Elapsed Time (min)
Coupon Currents

## Slide 8: VEP for RF Test Comparison
Side View
Top
View
Ninja-5
Single-Cell Cavity with Support-jig
Equator
12 mm x 9 mm
Removal rate: 0.22 µm/min
Cavity Surface after VEP
Removal Thickness Profile
Ninja Cathode-v5
Smooth and glossy surface
VEP Current Profile
Voltage: 16-17 V
Cathode rotation: 20 rpm
Acid flow rate ~ 5 L/min
Temperature ~ 20 ºC
Uniform removal in the cell
TB1-TSB02 Cavity
`
𝛳=0˚
𝛳=180˚
Top View
Avg. removal: 36 µm

## Slide 9: SRF Performance (Single-Cell Cavity)
Field gradient of 32 MV/m (Q0=8×109) was achieved after VEP.
The accelerating gradient after VEP was as good as achieved after HEP.
at 2K
TB1-TSB02 Cavity
Cavity Performance after HEP and VEP
VEP1（36µm）
↓
HPR &
120ºC baking
↓
Annealing (750ºC)
↓
VEP2（10µm）
↓
HPR &
120ºC baking
↓
Vertical test
VEP Process
Eacc=32 MV/m; Q0=8×109

## Slide 10
VEP of 9-Cell Cavity
VEP test was conducted with similar parameters as optimized with the single-cell cavity.
Condition | Value
Cathode Type | Ninja v-5
Cathode Rotation | 20 rpm
Cavity Temperature | 15–22 °C
Voltage | 15 V
Acid flow rate | ~5 L/min

## Slide 11: Results of VEP
Equator Surface after VEP
Removal Trend
Avg. removal: 50 µm
VEP yields rough equator surface and asymmetric removal in the upper cells.
The optimized parameters for the single cell cavity are adequate for a 4-cell-scale cavity.
But these parameters are not adequate to apply to the 9-cell cavity.

## Slide 12: Parametric Study with 9-Cell Coupon Cavity
V Chouhan et al., Phys. Rev. Accel. Beams 22, (2019) 103101

## Slide 13: Effect of Cathode Rotation
Cathode Housing
Acid Flow Rate = 5 L/min
Cathode rotation of 20 rpm reduces the difference in the coupon currents in the top cell.
Top Cell Filled with bubbles

## Slide 14: Novel Acid Flow Method (Dual Flow)
Cathode Housing
Acid was flowed separately in the cavity and cathode housing.
5 L/min in the cavity, and different flow rates in the cathode housing
5 L/min
10 L/min
20 L/min
Adequate flow rates:
Cavity: 5 L/min
Cathode housing: 10 L/min
No intentional flow in cathode housing
10 L/min in cathode housing

## Slide 15: Effect of Temperature
Polarization (J-V) curves were obtained at different temperatures of the cavity.
Bubble Quantity/Cathode screening
Strong cathode screening
Higher Temperature
Higher EP Current
Higher Bubble Quantity
Lower Electric Field
Higher Onset Voltage
Etching
Polishing
Oscillation
Onset Voltage
The optimized voltage can be chosen for a set cavity temperature.

## Slide 16: J-V Curves under Optimized Conditions
Polarization curves at ~15 ºC.
The EP plateaus are apparent for all the coupons and cavity.

## Slide 17: VEP Conditions (Dual Flow)
3 min
3 min
On/Off voltage cycles were applied to reduce returning bubbles from the acid tank to the cavity.
Condition | Value
Acid flow type | Dual flow
Flow rate in cathode housing | 10 L/min
Flow rate in cavity | 5 L/min
Cathode Type | Ninja v-5
Cathode Rotation | 20 rpm
Cavity Temperature | < 15 ºC
Voltage | 17.5 V
Voltage-on/off period | 3/3 min

## Slide 18: Surface Morphologies
The coupon surfaces were smooth after VEP with the optimized conditions.
SEM Images
Top Cell
Center Cell
Bottom Cell
VEP was conducted for an average removal thickness of 25 µm.

## Slide 19: Bulk and Light Removal (Removal Trend)
VEP with Unoptimized Conditions
VEP for 100 µm
VEP for 20 µm
Flow rate: Cathode housing-10L/min, Cavity-5L/min
Removal asymmetry significantly reduced.
HEP for 40 µm
Cell-2
Cell-3
Cell-4
Cell-5
Cell-6
Cell-7
Cell-8
Top Beam pipe
Bottom Beam pipe
VEP with Optimized Conditions

## Slide 20: Surface after Bulk Removal
12 mm x 9 mm
Flow rate: Cathode housing-10L/min, Cavity-5L/min
Surface was smooth in all the cells.
A pristine cavity can be processed with VEP.

## Slide 21: Field Flatness
Degradation in the field flatness after bulk removal is similar as observed after HEP.
No degradation in the field flatness after 10 and 20 µm removal.
VEP condition | Removal thickness (µm) | Field Flatness before VEP (%) | Field Flatness after VEP (%)
Unoptimized | 51 | 91 | 67
Optimized | 100 | 95 | 91
Optimized | 20 | 97 | 98
Optimized | 10 | 99 | 99
Field Flatness before VEP (20 µm)
Field Flatness after VEP (20 µm)
Field Flatness before and after VEP

## Slide 22: SRF Performance (Nine-Cell Cavity)
Horizontal EP (baseline RF test)
VEP for 100 µm
750ºC bake
VEP for 20 µm
750ºC bake
Field Flatness Tuning (99%)
VEP for 10 µm and 120ºC
RF Test
Field Flatness: 99%
At 2 K
The SRF performance after the HEP and VEP was the same.
Limited by quench
Eacc=28.3 MV/m; Q0=6.7e9

## Slide 23: Flipping System for VEP
We are also working on another method to improve the removal uniformity.
The cavity is flipped upside down periodically.

## Slide 24: Preliminary Result of VEP with Flipping System
Coupon surface
Top Iris
Equator
Bottom Iris
Top Cell
Center Cell
Bottom Cell
Uniformity is significantly better.
Condition | Value
Voltage | 14 V
Acid flow rate | 5–10 L/min
Cathode | Ninja Cathode (metal wings)
Cathode Rotation | 20 rpm
Cavity Temperature | 20–30 ºC
Flipping frequency | Flipped every 20 min of EP
Surface is rough. Parameter optimization is necessary.
Removal Trend
Unoptimized conditions w/o flipping
Unoptimized conditions w/ flipping

## Slide 25: Summary and Future Work
The VEP process was successfully optimized with the single-cell coupon cavity. The optimized parameters and cathode yield desired surface and removal uniformity.
A single-cell cavity showed good and the same SRF performance after HEP and VEP. The field gradient reached 32 MV/m at Q0=8e9.
A parametric study was conducted with the 9-cell coupon cavity. A novel dual flow method was developed and VEP parameters were optimized. The asymmetry was significantly reduced and smooth surface was attained for the 9-cell cavity as well.
The 9-cell cavity after bulk removal with VEP showed a good SRF performance (E=28.3 MV/m; Q0= 6.7e9). The performance is the same as the baseline performance.
The VEP parameters for 9-cell cavity will be further tuned to improve removal uniformity.
VEP is planned with a bigger acid tank that could avoid circulation of bubbles from the tank to the cavity. Parameters will be optimized for the VEP with flipping method.

## Slide 26: Thank You
Acknowledgement WING Co. Ltd., Japan
&
Higashinihon Kidenkaihatsu Co. Ltd., Japan

## Slide 27: Backup Slides

## Slide 28: Effect of Dual-Flow Method
No Intentional Flow in Cathode Housing
Optimized Dual Flow
Coupon currents for the top cell with no cathode rotation
Total Flow Rate: 15 L/min
Total Flow Rate: 15 L/min (Cavity-5L/min ; Cathode Housing-10 L/min)
The difference in the current was higher when no intentional flow was applied in the cathode housing.