## Slide 1: Material R&D at the Technical University of Darmstadt on N-doped Nb and Nb3Sn for SRF cavities
Márton Major, Ruben Grewe and Nils Schäfer
Technische Universität Darmstadt, Darmstadt, Germany

## Slide 2
Possible superconducting materials for RF cavities
Material | Critical Temp. Tc [K] | Normal-state resistivity ρn [μΩcm] | Critical Field Hc(0) [T] | Lower Critical field Hc1(0) [T] | Upper Critical field Hc2(0) [T] | Penetration depth (0) [nm] |  [meV] | Type
Nb | 9.23 | 2 | 0.2 | 0.18 | 0.28 | 40 | 1.5 | II
Pb | 7.2 |  | 0.08 | N/A | N/A | 48 |  | I
NbN | 16.2 | 70 | 0.23 | 0.02 | 15 | 200-350 | 2.6 | II, B1 comp.
NbTiN | 17.3 | 35 |  | 0.03 |  | 150-200 |  | II, B1 comp.
Nb3Sn | 18 | 20 | 0.54 | 0.05 | 30 | 80-100 | 3.1 | II, A15
V3Si | 17 |  |  |  | 24.5 | 179 |  | II, A15
Mo3Re | 15 |  | 0.43 | 0.03 | 3.5 | 140 |  | II, A15
MgB2 | 40 | 0.1-10 | 0.43 | 0.03 | 3.5-60 | 140 | 2.3/7.2 | II- 2 gaps
YBCO | 93 |  | 1.4 | 0.01 | 100 | 150 | 20 | d-wave
Pnictides | 30-55 |  | 0.5-0.9 | 30 | >100 | 200 | 10-20 | 
Whistler 2015, SRF Tutorial - Pushing Nb Performance - A.-M. Valente-Feliciano

## Slide 3
Possible superconducting materials for RF cavities
Material | Critical Temp. Tc [K] | Normal-state resistivity ρn [μΩcm] | Critical Field Hc(0) [T] | Lower Critical field Hc1(0) [T] | Upper Critical field Hc2(0) [T] | Penetration depth (0) [nm] |  [meV] | Type
Nb | 9.23 | 2 | 0.2 | 0.18 | 0.28 | 40 | 1.5 | II
Pb | 7.2 |  | 0.08 | N/A | N/A | 48 |  | I
NbN | 16.2 | 70 | 0.23 | 0.02 | 15 | 200-350 | 2.6 | II, B1 comp.
NbTiN | 17.3 | 35 |  | 0.03 |  | 150-200 |  | II, B1 comp.
Nb3Sn | 18 | 20 | 0.54 | 0.05 | 30 | 80-100 | 3.1 | II, A15
V3Si | 17 |  |  |  | 24.5 | 179 |  | II, A15
Mo3Re | 15 |  | 0.43 | 0.03 | 3.5 | 140 |  | II, A15
MgB2 | 40 | 0.1-10 | 0.43 | 0.03 | 3.5-60 | 140 | 2.3/7.2 | II- 2 gaps
YBCO | 93 |  | 1.4 | 0.01 | 100 | 150 | 20 | d-wave
Pnictides | 30-55 |  | 0.5-0.9 | 30 | >100 | 200 | 10-20 | 
Whistler 2015, SRF Tutorial - Pushing Nb Performance - A.-M. Valente-Feliciano

## Slide 4
Nb–N phase diagram
Brauer and Kern, Z. anorg. Allg. Chem. 507 (1983) 127
Layout of the Nb-N phase diagram (  )
*Zou et al., Sci. Rep. 6 (2016) 22330
Springer Handbook of Condensed Matter and Materials Data (W. Martienssen, H. Warlimont, Eds., 2005)
Musenich et al., J. Alloys Compd. 209 (1994) 319
Temperature (°C)
a:Nb-N solid solution, bcc 9.2 K
b: Nb2N, hexagonal 9.5 K
g: Nb4N3, tetragonal 12.2 K
d: NbN, cubic NaCl type 16.5 K
e: NbN, hexagonal < 1.2 K (11.6 K*)
Tc
Brauer, J. Less-Common Met. 2 (1960) 131
Phase

## Slide 5
Nb–N phase diagram
Lengauer et al., Acta mater. 48 (2000) 2633

## Slide 6
Nitrogen doping of SRF cavities
Standard state-of-the art preparation
This was the highest Q possible up to 2012
Record after nitrogen doping – up to 4 times higher Q!
Grassellino et al., Supercond. Sci. Technol. 26 (2013) 102001
1.3 GHz
Whistler 2015, SRF Tutorial - Pushing Nb Performance - Alexander Romanenko

## Slide 7
Nitrogen doping of SRF cavities
Whistler, SRF Tutorial - Pushing Nb Performance - Alexander Romanenko
Trenikhina et al., MOPB055, SRF2015
Injection of small nitrogen partial pressure at the end of 800C degassing-> drastic increase in Q.
Nitride (Nb2N phase) layer electro polished (EP) down (5μm was removed by EP).

## Slide 8
High temperature UHV furnace
Built in 1983 in Wuppertal by G. Müller
Now located at S-DALINAC
Two vacuum systems
  Insulating vacuum (green)
  Hot-pot vacuum (red)
< 10-4 mbar at 1750 ˚C
Hot pot and heat shield made of niobium
Heaters made of tungsten
40 kW power supply
Water cooled

## Slide 9
Niobium samples
5x5x2.7 mm3

## Slide 10
Nb sample N-doping (IKP) new procedure

## Slide 11
SIMS of N-doping (IKP) new procedure
Int. (c/s)
Sputter time (s)
14N

## Slide 12
SIMS of N-doping (IKP) new procedure
16O

## Slide 13
Int. (a.u.)
Int. (a.u.)
2q (deg)
XRD of N-doped Nb samples (IKP, new procedure)
b-Nb2N
a-Nb
d-NbN

## Slide 14
2N180005-2: 1h 100 mbar N2, 1550 °C
Int. (a.u.)
2q (deg)

## Slide 15
X-ray diffraction: phases and texture
Nb 110
Nb 200
Nb 211
Nb 220
Nb 310

## Slide 16
T2: Annealed Nb sample
2q (deg)
Int (a.u.)
Nb 110
Nb 200
Nb 211
Nb 220
Annealed in UHV at approx. 1200 oC (nominal) for approx. 1 h

## Slide 17
Pole figures

## Slide 18
T1 (Not polished Nb): Pole figures of 200 Bragg-peak
After annealing (1200 °C 1h)
Virgin
Log colour scale

## Slide 19
Nb 200 reflection (2q = 55.7°)
2N180005-2: 1h 100 mbar N2, 1550 °C

## Slide 20
NbN-111 reflection (2q = 35.67°)
2N180005-2: 1h 100 mbar N2, 1550 °C

## Slide 21
Quality factor measurement

## Slide 22
Quality factor measurement Variable input coupler

## Slide 23
Q0
Eacc (V/m)
Quality factor measurement

## Slide 24
Possible superconducting materials for RF cavities
Material | Critical Temp. Tc [K] | Normal-state resistivity ρn [μΩcm] | Critical Field Hc(0) [T] | Lower Critical field Hc1(0) [T] | Upper Critical field Hc2(0) [T] | Penetration depth (0) [nm] |  [meV] | Type
Nb | 9.23 | 2 | 0.2 | 0.18 | 0.28 | 40 | 1.5 | II
Pb | 7.2 |  | 0.08 | N/A | N/A | 48 |  | I
NbN | 16.2 | 70 | 0.23 | 0.02 | 15 | 200-350 | 2.6 | II, B1 comp.
NbTiN | 17.3 | 35 |  | 0.03 |  | 150-200 |  | II, B1 comp.
Nb3Sn | 18 | 20 | 0.54 | 0.05 | 30 | 80-100 | 3.1 | II, A15
V3Si | 17 |  |  |  | 24.5 | 179 |  | II, A15
Mo3Re | 15 |  | 0.43 | 0.03 | 3.5 | 140 |  | II, A15
MgB2 | 40 | 0.1-10 | 0.43 | 0.03 | 3.5-60 | 140 | 2.3/7.2 | II- 2 gaps
YBCO | 93 |  | 1.4 | 0.01 | 100 | 150 | 20 | d-wave
Pnictides | 30-55 |  | 0.5-0.9 | 30 | >100 | 200 | 10-20 | 
Whistler 2015, SRF Tutorial - Pushing Nb Performance - A.-M. Valente-Feliciano

## Slide 25
Possible superconducting materials for RF cavities
Material | Critical Temp. Tc [K] | Normal-state resistivity ρn [μΩcm] | Critical Field Hc(0) [T] | Lower Critical field Hc1(0) [T] | Upper Critical field Hc2(0) [T] | Penetration depth (0) [nm] |  [meV] | Type
Nb | 9.23 | 2 | 0.2 | 0.18 | 0.28 | 40 | 1.5 | II
Pb | 7.2 |  | 0.08 | N/A | N/A | 48 |  | I
NbN | 16.2 | 70 | 0.23 | 0.02 | 15 | 200-350 | 2.6 | II, B1 comp.
NbTiN | 17.3 | 35 |  | 0.03 |  | 150-200 |  | II, B1 comp.
Nb3Sn | 18 | 20 | 0.54 | 0.05 | 30 | 80-100 | 3.1 | II, A15
V3Si | 17 |  |  |  | 24.5 | 179 |  | II, A15
Mo3Re | 15 |  | 0.43 | 0.03 | 3.5 | 140 |  | II, A15
MgB2 | 40 | 0.1-10 | 0.43 | 0.03 | 3.5-60 | 140 | 2.3/7.2 | II- 2 gaps
YBCO | 93 |  | 1.4 | 0.01 | 100 | 150 | 20 | d-wave
Pnictides | 30-55 |  | 0.5-0.9 | 30 | >100 | 200 | 10-20 | 
Whistler 2015, SRF Tutorial - Pushing Nb Performance - A.-M. Valente-Feliciano

## Slide 26
Nb-Sn phase diagram
Charlesworth JP, Macphail I, Madsen PE. Experimental work on the niobium-tin constitution diagram and related studies. Journal of Materials Science. 1970 Jul 1;5(7):580-603.

## Slide 27
Challenge: Vapor-pressure of Sn

## Slide 28
Challenge: Vapor-pressure of Sn
Nb
Nb3Sn
Nb
Sn
Nb
Sn
Nb
Sn
Nb
800 – 1200 °C
+ 3 – 24 h
Nb
Nb3Sn

## Slide 29
Nb3Sn co-sputtering
Nb
Nb3Sn
Sn Target
Nb Target
Argon
Heater
MFC
Butterfly valve
Substrate
Exhaust

## Slide 30
50 – 100nm grain size
Nb3Sn morphology

## Slide 31
Stoichiometry

## Slide 32
Stoichiometry 20W Sn / 105W Nb

## Slide 33
XRD: Temperature Study

## Slide 34
R-T measurements: Power Study

## Slide 35
Acknowledgement
Thank you for your attention!
Funded by BMBF Projects 05H15RDRBA and 05H18RDRB2
Lambert Alff Matthias Mahr
Stefan Flege
Norbert Pietralla Jens Conrad Michaela Arnold
Florian Hug

## Slide 36
Recrystallization of Nb
Fig. 1. Plot of Vickers Hardness Number HV, against percentage reduction in thickness for cold-rolled niobium.
Thompson and Flewitt, J. Less-Common Metals, 21 (1970) 456
Fig. 2a. Plot of hardness against annealing temperature for niobium deformed by 94% and
annealed for five hours.
TM = 2477 °C
Recrystallization starts ~ 590 °C, maximum ~ 630 °C (0.32 TM)

## Slide 37
Sample holder
Virgin
After some cycles
Pulverised after 10th N-cycle
Sample

## Slide 38
Nitridation: 1500°C, 1 bar N2, 1 h
M. Mahr, bachelor thesis

## Slide 39
Lengauer et al., Acta mater. 48 (2000) 2633
M. Mahr, Bachelor thesis (2017)
Optical metallography on cutout of sampleholder

## Slide 40
Fabbricatore et al., J. Appl. Phys., 66 (1989) 5944
Sample | T (˚C) | P (mbar) | t (h) | Tc (K)
1 | 1427 | 40 | 3.5 | 13.1
2 | 1427 | 130 | 3 | 14.6
3 | 1427 | 200 | 1.5 | 14.3
4 | 1427 | 200 | 3 | 14.9
5 | 1727 | 130 | 3 | 15.6
Table. Reaction conditions for the niobium nitride samples. The cavity was nitrided together with the sample No. 2.
Test samples 0.1 mm thick, cavity wall 1 mm thick. Furnace: T up to 2000 ˚C, pressure: UHV (10-8 mbar) – atmosphere. Cleaning: 2h UHV @ 1427 ˚C, then nitridation (Table). The resulting nitrides have a light gold colour and are very hard and brittle.
No d-NbN was found only g, and phases with lower N content (a, b). High residual resistance. Possible cause: columnar growth of nitrides with amorphous material between the grains. Seen previously for sputtered NbN films on stainless steel [Wagner et al., J. Appl. Phys. 45 (1974) 465]
NbN coating of SRF cavities