## Slide 1
University of Wuppertal
In-Situ EXAFS Investigation of N2 Treatment of Nb
P. Rothweiler*, J. Kläs, R. Wagner,
D. Lützenkirchen-Hecht**
* patrick.rothweiler@uni-wuppertal.de
** dirklh@uni-wuppertal.de

## Slide 2: Motivation
Nowadays most Nb-cavities are treated with N2 to improve Q-factor
  “nitrogen-doping”
Effects still not well understood: especially position of “doped” nitrogen in the Nb-lattice unclear
Very low doses of N2
  Too low for e.g. XRD
  Þ in-situ measurements during doping procedure
*Fermilab today

## Slide 3: X-Ray Absorption Spectroscopy
XANES = X-ray Absorption Near-Edge Spectroscopy
EXAFS = Extended X-ray Absorption Fine-Structure
Element Specific: Absorption edges are element-specific
Valence Probe: XANES gives chemical state and formal valence of selected element.
Various Samples: samples can be solids, solutions, amorphous solids, soils, surfaces, etc.
Low Concentration: concentrations down to 10 ppm for XANES, 100 ppm for EXAFS detectable!
Local Structure Probe: EXAFS gives atomic species, distance, and number of near-neighbor atoms around a selected element..
In-situ measurements: Suited for real in-situ studies with time resolution!
XANES
EXAFS

## Slide 4: X-Ray Absorption Spectroscopy
Measure energy-dependence of X-ray absorption coefficient µ(E) of a core-level of selected element (i.e. Nb)
Good example of wave-particle dualism: Photoelectron acts like a wave!
Interference effects on absorption coefficient
Fourier-Transform of the oscillations gives bond length in R-space
Main Idea: Inserted N-atoms will slightly modify interference pattern of Nb
Constructive
Destructive Interference

## Slide 5: Experimental setup
In-situ heating chamber, fully remote controlled
Kapton windows for X-ray measurements
RT < T < 1200°C
p < 10-6 mbar (at 900°C ca. 2x10-6 mbar)
Nb foils of 6 – 25 µm thickness
Measured in transmission
Treatment up to 30 mbar N2 (Kr, Ar,…) for minutes … to … several hours
Slightly higher pressure and time (= exposure) because of very small effects

## Slide 6: In-situ Measurements: Time dependence
Plot Fourier-Trafo in R-Space
Reduction in NN-amplitude Þ caused by lattice vibrations
Constant after first minutes of baking Þ no effects of e.g. poor vacuumconditions etc.
Phase 2: N2 - exposure
Further reduction in NN-amplitude caused by N-gas exposure
Þ Effect of N2 visible
Uptake causes blurring
Phase 1: Heating in vacuum

## Slide 7: Used model and EXAFS data fitting with two phases
Nb: bcc-crystal
N2-uptake at octahedral interstitial site
Neighboring atoms are (slightly) displaced
Model of hard spheres
Linear Fit of unit cells with and without N2
Up to 2% of unit cells with N2
  Bcc (2 Nb-Atoms/unit- cell): 1 atom%
Octahedral site competitive with ionic N-size of 70 pm

## Slide 8: Ex-situ measurements at Room-Temperature: Exposure dependence
Verification of in-situ measurements
Fit of the first two coordination shells
Investigation on effect of different exposure intensities on Nb-Nb bond distances (R1, R2) and mean squared displacement (s12, s22)
Increases agree qualitatively with model
But: large uncertainties

## Slide 9: High precision (ex-situ) EXAFS measurements at 100 K
High precision
  Reduction of lattice vibrations
  Smaller uncertainties in R
  Smaller σ² (linear shift)
Main result:
Trends from RT measurements are fostered

## Slide 10: Summary and Outlook
N2 -uptake on interstitial octahedral sites
Investigations of time- and pressure-dependence
In- and ex-situ measurements agree with each other
100 K measurements show same trends
Kr- and Ar-uptake: do not show any detectable effects
Next steps:
Improvement of fit model
  More shells / paths
Measurements with samples from real cavities using surface sensitive EXAFS Þ samples from the community are welcome!

## Slide 11: Acknowledgements
MWF NRW
Department in Wuppertal: R. Frahm, B. Bornmann, P. Pagel, R. Wabnitz, …
DELTA (TU Dortmund, Germany)
PSI – Villingen, Swiss Light Source
DESY photon science Hamburg
BMBF: financial support (05H15PXRB1, 05H18PXRB1, 05K16PX1)
MWF NRW: financial support

## Slide 12: Addional material: Nb - foils
X-ray diffraction, E = 16 keV:
Polycrystalline, textured foils
SEM:
Smooth, wavy surfaces