## Slide 1: FPCCD radiation damage test plan @ATF
2020/9/9
Yasuhiro Sugimoto
@ILC detector seasonal meeting

## Slide 2: introduction

## Slide 3: FPCCD
FPCCD (Fine Pixel CCD) is one of the sensor candidates for ILD vertex detector
FPCCD has very small pixels of ~5um square
The sensitive layer is fully depleted
Because of its huge number of pixels, the hit occupancy remains at an acceptable level even if one full train hits are accumulated

## Slide 4: Pros and cons of FPCCD
Advantage
Small pixel size 
  Very high spatial resolution
  Excellent two-track separation capability
Read out between beam trains 
  Free from EMI noise from bunched beam
  Low power consumption due to relatively slow readout
Disadvantage
Large number of hits 
  Large data size
  CPU time for track reconstruction
Long charge transfer length (few cm) 
  Charge Transfer Inefficiency (CTI) due to the radiation damage caused by pair-background e+/e-

## Slide 5: Status of FPCCD sensor R&D
Small prototypes
  6um pixels, 6mm square sensor size
  4 readout ports/sensor, with different horizontal register size
  Standard and thin (50um) wafers
  Neutron radiation damage test has been done  More improvement of charge transfer inefficiency (CTI) is desirable
Large prototypes
  62x12 mm2 sensor size (active area)
  8 readout ports/sensor, with 3 pixel sizes (6, 8, 12 um)
  Standard and thin (50um) wafers
  With and without notch channel
No new prototypes recent few years
Large (left) and small (right) prototype
Thinned (50um) large prototype

## Slide 6: Recent topics
Cosmic ray test of FPCCD sensors
  Small (6mmx6mm) prototype sensors with 6um pixels
  ~3 weeks data acquisition
  Charge spread of the signal has been studied
    For ~normal incident (<10 degrees) charged particles, the maximum number of the hit pixels was 4
    This result implies an excellent 2-particle separation capability of FPCCD sensors
(from master thesis by S.Yanagawa, Tohoku U.)

## Slide 7: Radiation damage test

## Slide 8: History of CCD radiation damage test
CCD | Irradiated by | Year | 
Standard CCD | Sr-90 (β) | 2000 | 
Standard CCD | Cf-252 (neutron) | 2000 | 
Standard CCD | 140 MeV electron | 2003 | LNS (ELPH)
FPCCD | ~65 MeV neutron | 2014 | CYRIC
FPCCD | 80 MeV electron | 2021 (?) | ATF

## Slide 9: Electron energy
NIEL hypothesis
  Bulk damage of Si (damage in the Si, which causes traps of signal charge and increase of dark current) is proportional to Non Ionizing Energy Loss of incident particles
NIEL of electrons saturates at ~50 MeV
Electron of ~80 MeV, which is available at ATF, is suitable for bulk damage test

## Slide 10: Electron irradiation at ATF
Irradiate FPCCD sensors by electrons from ATF linac at the dump line
Electron energy ~80 MeV (=energy at the exit of 3m S-band accelerator)
Spread the beam by multiple scattering with a thin target (1~20% X0, depending on the available distance between the target and the test detector)  FWHM > 10cm at the test detector
Put a small magnet (B=3kG, L=12cm) just downstream of the target to separate the main beam from very low energy e+/e- and X/g-rays

## Slide 11: Study items
Study of radiation damage of FPCCD against electron (comparison with neutron irradiation)
  CTI
  Dark current
  Flat-band voltage shift
    Electron irradiation gives larger effect than neutron irradiation
  Time dependence of these effects
Annealing below 100℃
  If it is confirmed, there could be a possibility of in-situ annealing

## Slide 12: Experiment plan
Irradiation dose: 0.2x1011/cm2, 0.5x1011/cm2, 1.0x1011/cm2, 2.0x1011/cm2, and 5.0x1011/cm2, step by step
We can study the radiation effect of the sensors just after the irradiation in a laboratory at KEK  Advantage of irradiation facility at KEK
Interval of ~6 month between each irradiation to study sensor’s characteristics, including time dependence of the damage, in detail after each irradiation
Necessary machine time
  ~8 hours for each irradiation (including assembling and dis-assembling of the apparatus: irradiation itself takes less than 1 hour)
  The 1st irradiation: Spring 2021

## Slide 13: Future prospects
ATF review committee in September 2020
  Operation schedule of ATF will be discussed
  It could be shut down until ILC project approval
  We have propose this experiment plan as one of ATF utilization plans to support continuation of ATF operation
If ATF survives, and our proposal is approved, we need
  Additional budget for apparatus for irradiation and sensor characterization
  Set up sensor characterization apparatus at Fuji-B1
  Human resources  Collaborators are very welcome